Pinky Saikiaa, Subrat Jyoti Boraha

aJoya Gogoi College, Khumtai, Golaghat, Assam-785619

Email: pompipinkysaikia@gmail.com, subratjb@gmail.com

Abstract:

Nanoscience and nanotechnology arouse considerable interest in the recent time and has become one of the most important and exciting forefront area of research because of their wide range of applications in the field of catalysis, sensors, electronics, medicine, bio-sciences, drug delivery, opto-electronics, abatement of pollution etc. It is highly multidisciplinary which deals with all branches of science. Nanomaterials are the chemical substances having the internal structure or surface structure in the range of 1-100 nm. They possess various important properties such as high surface area, surface energy, crystal structure, physiochemical stability etc. Due to these properties, they have many applications in different field. In this chapter, we have discussed only recent application of carbon based nanomaterials, metal-oxide based and clay/LDH based nanomaterials in the field of catalysis.

Keywords: Nanoparticles; Metal-oxide nanoparticle; Clay supported nanomaterials; LDH; Characterizations; Catalysis

1. Introduction:

Nanomaterials are a set of substances with at least one dimension is in nanometer range (1-100 nm) which includes nanoparticles, nanofibers (rods, tubes) and nanoplates [1]. Nanoparticles exhibit improved physico-chemical properties which correspond neither to those of free atoms or molecules making up the particles nor to those of bulk solids with same chemical composition. Nanotechnology involves the use of nanomaterials in various areas like chemical and textiles industries, sensors, catalysis, biotechnology, electronics, medicine to provide better and improved technologies to the society [2-9]. Nanoparticles are characterized by a large value of the surface to volume ratio, which signifies that a large fraction of the atoms are exposed on the surface and can be involved in surface activities like catalysis [8-9]. Due to their unique optical, magnetic, electrical, and other properties they have the potential for great impacts in electronics, medicine, and other fields [10]. These are also widely used in areas of medical diagnostics, areas of material modification, degradation of environmental pollutants and biotechnology which requires further modification of nonmaterial into different structure with different features. The most important feature is the catalytic application [1].

Nanomaterials can be synthesized mainly by two approaches-top down and bottom up approach (Figure 1) [11]. Top down approach includes- mechanochemical processing, electroexplosion, sputtering, laser ablation, lithography, electrospining etc. [11] whereas bottom up approach includes- chemical vapour deposition, plasma arcing, wet chemical methods etc. [11]

Figure 1: Schematic representation of synthesis of nanomaterials

In recent years, Nanomaterials synthesis and application is one of the important fields of research in Nanoscience and Nanotechnology due to their potential applications in science and industry [12].On the other hand, use of nanomaterials in catalysis is the another driving force for the development of the chemical industry. In recent years, the use of metal nanomaterials as heterogeneous catalysts is an important field of research [13-16] due to their high catalytic activity and selectivity for specific reactions. Nanocatalysts were used for catalytic chemical reactions such as the oxidation reaction [13], the reduction reaction [14], coupling reaction [15,16] and the electrochemical reaction [17-21]. They have attracted more attention to researchers as they act as a bridge between atoms and bulk materials. In addition to this, they have some properties like the surface and interface effect, small size effect, quantum size effect and macroscopic quantum tunnel effect, potential applications like catalysis, biology, medicine and so on.

Catalytic nonmaterials can be classified into the three types as shown in Figure 2.

Figure 2: Types of Nanomaterials used as catalyst

The catalytic nanomaterials can be characterized by different technique such as small-angle X-ray scattering, BET analysis, X-ray diffractometry, Temperature-Programmed oxidation-reduction and electron microscopic methods [22-24]. Table 1 shows different characterization technique for nanomaterials.

Table 1: Commonly Used Characterization Techniques for Nanomaterials [24]

| Transmission electron microscopy* (TEM) | Shape, size and crytallinity |
| --- | --- |
| X ray diffraction* (XRD) | crystal structure |
| UV-vis-nIR Spectroscopy* | light absorption and scattering |
| photoluminescence spectroscopy* (PL) | light emission |
| X ray photoelectron spectroscopy* (XPS) | chemical composition |
| Chemisorptions, physisorption | surface area |
| Scanning electron microscopy (SEM) | shape and assembly structure |
| Small angle X ray scattering* (SAXS) | characteristic distances of partially ordered nanomaterials |
| Energy dispersive X ray analysis (EDX) | chemical composition |
| Scanning tunneling microscopy*(STM) | Size, shape |
| Atomic force microscopy* (AFM) | Size, shape |
| Ultraviolet photoelectron spectroscopy (UPS) | electron valence band |
| X ray emission spectroscopy* (XES) | electron band gap |
| Near-edge X-ray absorption fine structure* (NEXAFS) | chemical composition |
| Extended X-ray absorption fine structure* (EXAFS) | chemical composition and bonding environment |

In this chapter we have discussed about the recent applications of some nanomaterials in the field of catalysis.

2.1 Application of carbon based nanomaterials:

Carbon is unique amongst all other element found in the universe; it is the sixth most common element in the universe and the 4th most common element in the solar system and 17th most common element in the Earth’s crust [25]. Due to the ability of carbon to catenate carbon science become one of the most important fields of research in the field of nanoscience, materials science, engineering and biology also [26].Different types of low dimensional allotropes of carbon such as graphite, activated carbon, carbon nanotubes and the C60 family of buckyballs, polyaromatic molecules [27-30] and graphene [31-33]has attracted substantial attention in the field of research due to their different application such as electronics and semiconductor industry, data storage devices, sensors and bioelectronics,composite materials, energy research, catalysis,biomedicine and theranostics [34].

2.1.1. Graphite:

The word Graphite was derived from the Greek word “graphein” [35]. Graphite is characterized by lustrous black sheen features with physically greyish-black and opaque in nature [26]. In Graphite carbon atoms are arranged in hexagonal ring structure in which atoms are held together by strong covalent bond and the layers are held together by van der Waals forces which results the capability of layers to move past each other exhibiting soft and slippery physical properties[26]. It possesses the flaky like morphology as shown in Figure 3.

Figure 3: Field emission scanning electron and polarized light micrographs of the platy morphology of flake graphite [26].

Due to the delocalization of -electrons of carbon atom Graphite has an ability to conduct electricity [26]. Graphite possesses both metal and non-metallic properties, high thermal and electrical conductivity due to which it is used for the preparation of electrode and electrical arc lamp [36].

2.1.2. Buckminsterfullerene:

It was discovered in 1985 by Harry Kroto and Richard Smalley of University of Sussex and Rice University [26]. Due to their unique photo physical and photochemical properties they attracted significant attention in the field of research [26]. Fullerene consists of sp2 bonded carbon atom of different size in the form of hollow sphere as shown in Figure 4 [37]. Fullerene has the ability to act as sensitizer and is also used for blood sterilization and photodynamic cancer therapy [34]. It has diverse application in the field of nanomedicine such as antimicrobial, antiviral, and antioxidant agents [38,39].On the other hand, Fullerene can also be used for the production of cosmetics in human skin care.

Figure 4: Structure of Fullerene [39]

2.1.3. Carbon nanotube:

Carbon nanotubes are allotrope of carbon in the form of hollow cylinder consists of graphene sheets as shown in Figure 5[26,34,40]. Depending upon the no of grapheme sheet carbon nanotubes are classified into two types one is single wall carbon nanotube (SWCNT) which can be formed by rolling of single graphitic sheet; another is multiwall carbon nanotube (MWCNT) which can be formed by the rolling of few graphitic sheet with an interlayer spacing of 3.4Å [40]. Their diameter varies from 0.4 nm to 2.5 nm and few nm to 100 nm [34]. The layers in MWCNT are held together by van der Waals force. Due to their unique mechanical, electrical and structural diversity, fast electron transfer rate, high surface area, it exhibits superior strength, flexibility, electrical conductivity and magical behaviour towards various application including biosensor, medical diagnosis and treatment of various diseases, catalysis [40,41] etc.

Figure 5: Structure of CNT [40]

2.1.4. Graphene:

Graphene was first introduced by Mouras and co-workers as“graphitic intercalation compounds (GIC)”in 1987 [40]. Graphene consists of planner graphitic sheet consisting of sp2 hybridized carbon network with carbon-carbon bond distance of 1.42Å and an interlayer spacing of 3.4Å as shown in Figure 6 [40]. Due to their interesting optical, electrical, chemical properties, extremely large surface area, chemical purity and free π electrons it attracts attention in the field of research [34]. It has diverse used as biosensor, drug delivery, treatment of various diseases including cancer therapy etc [34,40-41].Various derivatives of graphene such as graphene oxide, reduced graphene oxide, few layer graphene oxide, chemically changed graphene oxide has been developed [34]. Among these graphene oxide and reduced graphene oxide have many application in sol-gel chemistry.Graphene oxide is used as biosensor, cellular imaging, nanoprobes, anticancer drug delivery [34].

Figure 6: Structure of Graphene sheet [40]

Due to the unique structural and electronic properties graphene are also used as catalyst in different reaction including oxygen reduction reaction (ORR), water splitting, Fischer-Tropsch synthesis (FTS), CO2 reduction, water treatment, air purification [43]. Different types of graphene based nanomaterials and their uses as catalyst are shown in Table 2.

Table 2: Different types of graphene based nanomaterials and their uses as catalyst [43]

| Catalyst | preparation method | characterization techniques | Application |
| --- | --- | --- | --- |
| Graphene | mechanical cleavage | TEM, AFM, XPS, Raman, DFT | ORR |
| PtM/rGO | Hydrothermal | HRTEM, XRD, ICP-MS, XPS | ORR |
| Pt/G-PCNF | thermal annealing | XRD, SEM, TEM, XPS | ORR |
| Ag/N-rGO | thermal annealing | XPS, EDS, Raman, TEM, XRD | ORR |
| NG | thermal annealing | SEM, BET, XRD, Raman, XPS | ORR |
| N−S/G | CVD | HRTEM, SEM, Raman, XPS, BET | ORR |
| N−P−O/G | gas exfoliated | Raman, XPS, SEM, HRTEM, DFT | ORR |
| N−S/G | CVD | HRTEM, XPS, DFT, SEM, Raman, BET | HER |
| Pt/CNT-G | thermal annealing | HRTEM, XPS, ICP, Raman, DFT, BET | HER |
| lanthanides/G | hermal annealing | SEM, TEM, XPS, BET, Raman | HER, ORR |
| N−P/G | thermal annealing | SEM, XPS, XRD, FTIR, Raman | HER, ORR |
| Co−N/G | thermal annealing | SEM, TEM, BET, XRD, XPS | OER, ORR |
| N-PC@G | thermal annealing | XRD, SEM, TEM, Raman, XPS, BET | OER, ORR |
| N-GQDs/g-C3N4 | Hydrothermal | SEM, XRD, UV−vis, BET, FTIR, XPS | water splitting |
| Cu2O/FLG | thermal annealing | ICP, XRD, UV−vis, AFM, TEM, XPS | water splitting |
| g-C3N4/rGO | DFT computation only research | DFT | water splitting |
| Pt/TiO2-rGO | Photoreduction | HRTEM, UV−vis, EPR, TA | water splitting |
| rGO/BiOCl | Hydrothermal | XRD, SEM, TEM, XPS, UV−vis | water splitting |
| Fe/rGO | Hydrothermal | HRTEM, XPS, Raman | F-T synthesis |
| Ru/G | CVD | TEM, XRD, XPS, UV−vis | F-T synthesis |
| CZZA/rGO | chemical reduction | BET, XRD, SEM, TPR, TPD | CO2 reduction |
| Cu/p-NG | thermal annealing | HRTEM, SEM, XPS | CO2 reduction |
| G(3D) | CVD | SEM, HRTEM, XPS, Raman, DFT | CO2 reduction |
| Cu2O/G/TNA | Electrochemical | SEM, XRD, Raman, XPS, UV−vis | CO2 reduction |
| Pt-rGO | Hydrothermal | XRD, XPS, TEM, AFM, SEM | CO2 reduction |
| ZnO/G |  | DFT | CO2 reduction |
| Mn-MGO | Hydrothermal | SEM, TEM, XRD, XPS | water treatment |
| NRGO@Co | thermal annealing | HRTEM, SEM, XRD, Raman, TGA | water treatment |
| NG | thermal annealing | XRD, FTIR, TGA, BET, XPS, Raman | water treatment |
| CN/RGO/ZS | bath precipitation | XRD, HRTEM, XPS, FTIR, UV−vis | water treatment |
| CN-G | thermal annealing | TEM, XPS, XRD, BET, FTIR, UV−vis | water treatment |
| TiO2/G/Cu2O | CVD | XRD, TEM, XPS, UV−vis | water treatment |
| MnO2/G | Hydrothermal | TEM, XPS, XRD, BET, ICP, FTIR | air purification |
| ZnO/G | Hydrothermal | SEM, HRTEM, XRD, SAED, XPS | air purification |
| TiO2/G | Hydrothermal | XRD, SEM, TEM, UV−vis, FTIR | air purification |
| Pd/N-rGO | Hydrothermal | XRD, FT-IR, XPS, TEM, Raman | Hydrogenation |
| Co/NG | thermal annealing | XRD, SEM, XPS, FTIR, Raman, BET | Oxidation |
| NG |  | DFT | Oxidation |
| Au/G |  | DFT | Hydrochlorination |
| Au3/(N)G |  | DFT | Hydrochlorination |
| B, N-G | thermal annealing | TEM, XPS, TPD, TGA, Raman, DFT | Hydrochlorination |

2.2. Application of metal oxide-based nanomaterials:

Due to some unique properties such as optical properties, higher ductility at elevated temperatures, cold welding properties, super paramagnetic behaviour, unique catalytic, sensitivity and selective activity metal oxide nanoparticles are widely used in the field of nanotechnology [43]. These are used for the development of functional nanomaterials and have lots of application from semiconductor to insulator [44]. Different types metal oxides such as CuO, ZnO, SnO2, Al2O3, MgO, Fe3O4, ZrO2, AgO, TiO2, CeO2 etc. are useful in the fields of materials chemistry, medicine, agriculture,information technology, biomedical, optical, electronics,catalysis, environment, energy, and sensor [45].The metal oxide nanomaterials are also used as gas sensing for different types of gases like carbon dioxide, CO, O2, O3, methane, nitric oxide, nitrogen dioxide, ammonia, hydrogen sulphide, hydrogen gas etc [45]

In the recent years noble metal-based nanomaterials have attracted attention in the field of nanotechnologydue to their unique chemical and physical properties [46].Different types of noble metal such as Au, Ag, Pt, and Pd supported on TiO2, CeO2, ZrO2and Clay etc. can be prepared by various methods such asimpregnation, co-precipitation, deposition and precipitation method [46].These are mainly used as a catalyst in degradation of pollutants, waste minimization, energy conversion, water splitting and different types of organic reactions like Sonogashira, Heck, Miyaura-Suzuki-type reactions and other C-C bond formation reactions [47]. Table 3 shows list of various noble metal oxide nanomaterials and their synthesis route and application as catalyst.

Table 3. List of various noble metal-metal oxide nanocomposite catalysts by synthetic route and application [47].

| Materials | Synthetic Routes | Applications |
| --- | --- | --- |
| TiO2 NP-Au | Photodeposition | Photooxidation of acetone and 2-propanol |
| Au @TiO2 | Hydrothermal | Photocatalytic CO2 reduction |
| Au/TiO2 | Anodization and photocatalytic reduction | Photoelectrochemical water splitting |
| Ag@Cu2O | Chemical reduction and room temperature aging | Photodegradation of methyl orange |
| Ag@ZnO | Polyol process and room temperature aging | Photodegradation of rhodamine-B |
| Au-ZnO | Hydrothermal method | Photodegradation of methylene blue |
| TiO2/Au | Deposition-precipitation method | Photocatalytic H2 generation |
| Pt/Cu2O-TiO2 | Photodeposition | Photocatalytic CO2 reduction |
| CeO2/rGO/Pt | Hydrothermal approach | Oxidation of methanol in DMFCs |
| Pt/rGO@TiO2 | UV photoreduction | Methanol oxidation |
| Pt/C-MnxO1+x | Polyol method | Methanol oxidation |
| Pt/MnO2/GS | Hydrothermal | Methanol oxidation |
| Pd/MNL/GS | Hydrothermal | DFAFC and DMFC |
| Pt/CeO2-NBs | Galvanic replacement reaction | Formic acid oxidation |
| Pt/SnO2 | Hydrothermally | Electrochemical H2 evolution |
| Pd-Mn3O4 | Hydrothermal | Electrochemical H2 evolution |
| Pd-Mn3O4/carbon black | Chemical reduction | Electrochemical O2 evolution |
| ZnO/Au | Hydrothermal and photoreduction | Photoelectrochemical water splitting |
| ZnO/Au | Self-assembly method | Dye sensitize solar cell |
| Pt/CeO2 | Solvothermal | CO oxidation |
| Pt/TiO2 | Heat treatment | CO oxidation |
| Au-SnO2 | Hydrothermally | 4-nitrophenol reduction |
| Fe2O3-Au | Chemical reduction | 4-nitrophenol reduction |
| Ag@Cu2O | Wet-chemically | Suzuki–Miyaura cross-coupling |
| Au/TiO2 | Hydrothermal method | Photocatalytic activity |
| TiO2 NP-Au | Deposition–precipitation method | Photoelectrochemical measurement |
| ZnO NP-Au | Chemical reduction method | Photodegradation of methylene blue |
| Fe3O4@Montmorillonite | Chemical reduction | C-C bond formation reaction |

2.3. Application of Clay based nanomaterials:

According to geologist clay is the geological materials with size greater than 4 μm [48]. Clays are aluminosilicate and arranged in layered structure. Each layer is composed of tetrahedral silica [SiO4]4-and octahedral alumina [AlO3(OH)3]6-[48]. These tetrahedral and octahedral layers are combined to form each layer and the apex of tetrahedrons andoctahedrons are occupied by oxygen whereas; the interlayer contains metal ion [48]. The layers are stacked together by van der Waals forces of interaction [48].

Clay minerals are classified into four major groups, including the montmorillonite/smectite group, kaolinite group, illite group, and chlorite group [49]. Table 4 shows different groups of clay minerals and their composition.

Table 4: Types of Clay Minerals [49]

| Group | Layer Type | Group Members | Layer Charge | General Chemical Formula | Remarks |
| --- | --- | --- | --- | --- | --- |
| Smectite | 2:1 | montmorillonite, saponite, pyrophyllite, nontronite, talc, vermiculite | 0.5-1.2 | (Ca, Na, H) (Al, Mg, Fe, Zn)2 (Si,Al)4O10(OH)2 xH2O | x indicate the variable amount of water molecules |
| Kaolinite | 1:1 | kaolinite, dickite, nacrite | ~ 0 | Al2Si2O5(OH)4 | group members are polymorphs |
| Illite | 2:1 | Illite | 1.4-2.0 | (K,H)Al2 (Si,Al)4O10 (OH)2 xH2O | x indicate the variable amount of water molecules |
| Chlorite | 2:1:1 | amesite, cookeite, chamosite, daphnite | Variable | (Fe, Al, Li, Mg, Zn, Cr)4-6(Al, Si)4 O10(OH, O)8 | sometimes placed as a separate group in phyllosillicate |

Among the various clay minerals, Montmorillonite clay is the most widely studied clay of the smectite group [50-51]. It is a hydrated 2:1 layered aluminosilicate of the smectite group and composed of two tetrahedral silicate sheets, which are bonded to either side of an octahedral aluminate sheet. Isomorphous substitution of Si4+ and Al3+ by lower valence cations such as Mg2+ results in charge imbalance in the clay structure. It is balanced by hydrated exchangeable cations which occupy the position between clay layers. The montmorillonite clay structure is pictorially is shown in Figure 7. The modified montmorillonite clay has attracted much attention of the chemists because of their large applications in various catalytic reactions [51]. Montmorillonite clay can be modified by treatment with mineral acid under controlled conditions to give partially delaminated clay with higher surface area and contain micro and mesopores with diameters 0-10 nm. This highly porous material can be advantageously used as a support for generation of metal nanoparticles.

Figure 7:  Structure of Montmorillonite clay [51]

Clay based nanomaterials can be characterized by different techniques such as x-ray diffraction (XRD), scanningelectron microscopy (SEM), transmission electron microscopy (TEM), atomicforce microscopy (AFM),UV-Vis spectroscopy,FourierTransform Infrared (FTIR) spectroscopy,nuclearmagnetic resonance (NMR) spectroscopy, Thermogravimetric analysis (TGA),Differential scanning calorimetry (DSC) etc [48].

Due to their unique physicochemical properties such as large surface areas, swelling, ion exchange and active broken-edge M-O− bonds clay-based nanomaterials have many applications in the field of absorption, adsorption and catalysis etc [52]. The Bronsted and Lewis acid character and cation exchange capacity of clays leads them to use as catalyst for organic transformationreaction such as esterification of β-keto esters, Friedel-Crafts reactions, addition, oxidation, epoxidation, hydrogenation, allylation, alkylation, acylation, diazotization, rearrangement, isomerization, cyclization condensation, hydrogenation reaction[52]. Different types of clay-based nanomaterials such as TiO2-pillared clay supported V2O5 catalyst can be used for the selective oxidation of H2S containing water and ammonia [52]. Clay based catalyst are also useful for the conversion of biomass-based and biomass-derived feedstocks to useful feedstocks [52]. Al/M pillared montmorillonite clays (where M= Fe, Cu, Mn) are employed for the degradation of organic pollutants [52].

In recent years anionic clay-based materials like Hydrotalcite type materials are more useful in many application starting from adsorption to catalysis [53-55]. Layered double hydroxide (LDH) also known as anionic clays are 2D nanomaterial as shown in the following Figure 8 with structural formula of [M 2+1- xM3+x(OH)2](An−)x/n.mH2O (where, M2+ and M3+ are divalent and trivalent metals, respectively; An− is the interlayer anion).

Figure 8: Schematic representation of Layered Double Hydroxide

They have attracted attention in the field of research due to their unique properties such as high surface area, uniform atomic level distribution, acid-base bifunctionality, high thermal stability, memory effect [53-55]. LDH based nanomaterials are used as photocatalyst or photoelectrocatalyst for the conversion of solar energy to clean chemical reagent [54].These are also used as environmental catalyst for the treatment of green house gases such as N2O, CO2, CH4 oxidation to useful feedstocks [54]. Now-a-days oxygen evolution reaction becomes one of the great challenges for researcher for example, Ni-Fe LDH, Ni-Co LDH, Co-Fe LDH and Ni/Co/Fe LDHs are used as electrocatalyst for water splitting reaction to hydrogen and oxygen evolution [55].

The clay supported metal nanoparticles have found wide range of applications in various fields such as catalysis, biology, electrochemical sensor and electronics etc. Due to growing environmental concern, researchers have attracted for heterogeneous system of metals in catalysis. Clay supported silver nanoparticles have been used as active catalysts for various organic transformations like three component coupling reaction, rearrangement reaction, cycloaddition reaction, oxidation reaction etc [56-58]. Cu0 -nanoparticles supported on montmorillonite clay used for different catalytic reactions such as alcohol oxidation, C-N cross coupling, coupling of alkyl azide and terminal alkyne to form 1,2,3-triazole and other C-C bond formation reaction [59, 60]. Gold nanocrystals stabilized on modified montmorillonite have been used as highly efficient catalyst for the three-component coupling reaction aldehyde, amine and alkyne to synthesize propargylamine which is a biologically active molecule. Clay supported Pd-nanoparticles have been used active catalyst for Suzuki–Miyaura coupling reaction in aqueous medium with recyclability of the catalyst [50]. Fe3O4 magnetic nanoparticles supported on modified montmorillonite have been used as active catalyst for BV Oxidation, synthesis of dihydropyrimidones [59-61]. Schematic representations of some of the reactions [56-61] are listed below.

Scheme1: Synthesis of propargylamine using Silver nanoparticles supported on modified montmorillonite (Ag-NPs@mmt)

Scheme 2: Three-component coupling reaction of aldehyde, amine and alkyne catalysed by gold nanocrystals stabilized on montmorillonite.

Scheme 3:  Clay supported Pdo-nanoparticles catalyzed Suzuki–Miyaura reaction between iodobenzene and phenylboronic acid

Scheme 4: 1,3-dipolar cycloaddition of azide and terminal alkynes catalysed by clay supported Cu(0)- nanoparticles.

Scheme 5: Montmorillonite clay supported Fe3O4 nanoparticles (Fe3O4@mmt)catalysed three-component condensation reaction to synthesize DHPMs (Dihydropyrimidones)

Scheme 6: Baeyer-Villiger Oxidation catalysed by magnetic Fe3O4nanoparticles stabilized on montmorillonite using H2O2 as oxidant.

3. Conclusion:

The carbon based nanomaterials like graphene, carbon nanotube has undoubtedly make attention towards the field of nanoscience research due to their unique properties and has diverse used in optics, electronics, and energy storage as well as in the field of catalysis.

Supported metal nanoparticles and other non-metal based nanocomposites have led to generation of new and novel sustainable catalyst for future research work and these nano catalysts are far better compared to conventional catalyst. Supported nano catalyst exhibited high surface area and are used for different organic and inorganic transformations like oxidation, reduction, coupling reaction and synthesis biologically important compounds etc. Due to their high efficiency, such nano catalysts may be useful large-scale synthesis of fine and bulk chemicals.

In addition to this clay-based nanomaterials have also many applications in the field catalysis due to their unique physicochemical properties such as large surface areas, swelling, ion exchange and active broken-edge M-O− bonds. LDH based nanomaterials also act as an efficient environmental catalyst for the treatment of green house gas to useful feedstock and become another diverse field of research.

4. References:

[1] N. Sharma, H. Ojha, A. Bharadwaj, D.P. Pathak. Preparation and catalytic applications of nanomaterials: A review.RSC Adv., 2015, 5, 53381-53403.

[2] K. J. Klabunde, S. Winecki, Nanoscale Materials in Chemistry, Wiley, New York, 2001, 1-13.

[3] C. N. R. Rao, G. U. Kulkarni,  P. John Thomas,  P. P. Edwards .Metal nanoparticles and their assemblies. Chem. Soc. Rev., 2000, 29, 27.

[4] C. P. Poole Jr., F. J. Owens, Introduction to Nanotechnology, Willy-Interscience, 2003.

[5] J. M. Campelo,  D. Luna, R.  Luque, J.M Marinas, A.A Romero Sustainable Preparation of Supported Metal Nanoparticles and Their Applications in Catalysis. Chem.Sus. Chem., 2009, 2, 18-45.

[6] H. Brune,  H. Ernst, A. Grunwald, W. Grünwald.  Nanotechnology assessment and perspectives, Springer,2006.

[7]Y. Na, S. Park, S. B. Han, H. Han, S. Ko, S. Chang. Ruthenium-Catalyzed Heck-Type Olefination and Suzuki Coupling Reactions: Studies on the Nature of Catalytic Species.   J. Am. Chem. Soc., 2004, 126, 250-258.

[8] P.P.Sarmah, D.K. Dutta. Chemoselective reduction of a nitro group through transfer hydrogenation catalysed by Ru0-nanoparticles stabilized on modified Montmorillonite clay. Green Chem., 2012, 14, 1086-1093.

[9] S.J. Borah, D.K. Das. Modified Montmorillonite Clay Stabilized Silver Nanoparticles: An Active Heterogeneous Catalytic System for the Synthesis of Propargylamines Catal. Lett., 2018, 148(12), 3669-3677.

[10] A. Alagarasi. INTRODUCTION TO NANOMATERIALS, 2016

[11] R.J.Varghese, E.M. Sakho, S.  Parani, S. Thomas, O.S. Oluwafemiand, J. Wu. 2019. DOI: https://doi.org/10.1016/B978-0-12-813337-8.00003-5.

[12] M. Ghoranneviss, A.Soni, A. Talebitaher, N. Aslan. Journal of Nanomaterials. Volume 2015, http://dx.doi.org/10.1155/2015/892542.

[13]D.K. Dutta, J.B. Borah, P.P. Sarmah, Catal. Rev.2015, 57, 257–305.

[14]T. Yasukawa, A. Suzuki, H. Miyamura, K. Nishino, S. Kobayashi.  J. Am. Chem. Soc. 2015,137, 6616–6623.

[15] S. Zhang, X.T. Shen, Z.P. Zheng, Y.Y. Ma, Y.Q. Qu.  J. Mater.Chem. A 2015, 3, 10504–10511.

[16] S. Zhang, J. Li, W. Gao, Y.Q. Qu. Properties of oxides on the catalytic activity of Pd for C-C coupling reactions. Nanoscale 2015, 7, 3016–3021.

[17]W.J. Zhou, Z.H. Zhou, S.Q.Song, W.Z. Li, G.Q. Sun, P. Tsiakaras, Q. Xin. Pt based anodecatalysts for direct ethanol fuel cells. Appl. Catal. B Environ. 2003, 46, 273–285.

[18] A.V. Tripkovic, K.D. Popovic, B.N. Grgur, B. Blizanac, P.N. Ross, N.M. Markovic. Methanolelectrooxidation on supported Pt and PtRu catalysts in acid and alkaline solutions. Electrochim. Acta, 2002, 47, 3707–3714.

[19]J.H. Choi, K.J. Jeong, Y.J. Dong, J.H.  Han, T.H. Lim, J.S. Lee, Y.E. Sung. Electro-oxidationof methanol and formic acid on PtRu and PtAu for direct liquid fuel cells. J. Power Sources 2006,163, 71–75.

[2]. Y. Shen, K.J. Xiao, J.Y. Xi, X.P. Qiu. Comparison study of few-layered graphene supportedplatinum and platinum alloys for methanol and ethanol electro-oxidation. J. Power Sources 2015,278, 235–244.

[21] M.L. Xiao, L.G. Feng, J.B.Zhu, C.P.Liu, W. Xing, Rapid synthesis of a Pt -Ru nano-spongewith different surface compositions and performance evaluation for methanol electrooxidation. Nanoscale 2015, 7, 9467–9471.

[22] J. Virkutyte, S Rajender ,RSC Adv., 2012,2, 1533-1539 .

[23]S. Noor, K. K.Sudipta, S. R. Anupam, M Paramita, R Susmita, Catal. Sci.Technol.,2013,3, 3303-3316.

[24] Y. Li, G. A. Somorjai. Nanoscale Advances in Catalysis and Energy Applications. Nano Lett. 2010, 10, 2289–2295. DOI: 10.1021/nl101807

[25]Y. Zhang, Q.Z.Yin . Carbon and other light element contents in the Earth’s core based on first-principles molecular dynamics. Proc. Natl. Acad. Sci. USA 2012, 109, 19579–19583.

[26] S.  Nasir, M. Z. Hussein, Z.  Zainal, N. A. Yusof. Carbon-Based Nanomaterials/Allotropes: A Glimpse of Their Synthesis, Properties and Some Applications. Materials 2018, 11, 295; doi:10.3390/ma11020295.

[27]M.M.Titirici, R.J.White, , N. Brun, V.L. Budarin, D.S. Su, F. Del Monte, J.H.Clark, M.J. MacLachlan.Sustainable carbon materials. Chem. Soc. Rev. 2015, 44, 250–290.

[28] Loos, M. Allotropes of Carbon and Carbon Nanotubes. In Carbon Nanotube Reinforced Composites; Elsevier:Amsterdam, The Netherlands, 2015; pp. 73–101.

[29] Deng, J.; You, Y.; Sahajwalla, V.; Joshi, R.K. Transforming waste into carbon-based nanomaterials. Carbon, 2016, 96, 105–115.

[30] Rodríguez-Reinoso, F. The role of carbon materials in heterogeneous catalysis. Carbon, 1998, 36, 159–175.

[31]Allen, M.J.; Tung, V.C.; Kaner, R.B. Honeycomb carbon: A review of graphene. Chem. Rev. 2010, 110, 132–145.

[32] Geim, A.K.; Novoselov, K.S. The rise of graphene. Nat. Mater. 2007, 6, 183-191.

[33] K.S.  Novoselov, V.I. Fal, L. Colombo, P.R. Gellert, M.G. Schwab, K. Kim. A roadmap for graphene. Nature, 2012, 490, 192–200.

[34] K. D. Patel, R. K. Singh, Hae-Won Kim. Carbon-based nanomaterials as an emerging platform for theranostics. Mater. Horiz., 2019, DOI: 10.1039/c8mh00966j.

[35]A. Conly. Mining carbon to decrease the carbon footprint. Scientia, 2017, 112, 17-20.

[36]Bowers, B. History of Electric Light and Power; Peter Peregrinus Ltd.: London, UK, 1982; 55, 71-72.

[37] H.W. Kroto, J.R. Heath, S.C. O’Brien, R.F.Curl, R.E. Smalley. C60: Buckminsterfullerene. Nature, 1985, 318,162-163.

[38] Q. Liu, L. Wei, J. Wang, F. Peng, D. Luo, R. Cui, Y. Niu, X. Qin, Y. Liu, H. Sun, J. Yang and Y. Li, Nanoscale, 2012, 4, 7084-7089.

[39]  Y. Huang, M. Liu, J. Chen, C. Gao and Q. Gong, Eur. Polym. J., 2012, 48, 1734-1744.

[40] K. Yang, D. Maiti, X. Tong, X. Z. Mou.Carbon Based Nanomaterials for Biomedical Applications: A Recent Study. Frontiers in Pharmacology, 2018.

[41] P. Hu, C. Huang, L. Zhang, Sci. China Ser. B, 51, 2008,  866–871.

[42] Introduction to nanomaterials: synthesis and applications R. Jose Varghese, El hadji Mamour Sakho, Sundararajan Parani, Sabu Thomas, Oluwatobi S. Oluwafemi  and Jihuai Wu

[43] M.Hu, Z. Yao, X. Wang. Graphene-Based Nanomaterials for Catalysis. Ind. Eng. Chem. Res. 2017, 56, 3477-3502. DOI: 10.1021/acs.iecr.6b05048.

[44] M. S. Chavali, M.P. Nikolova. Metal oxide nanoparticles and their applications in nanotechnology. SN Applied Sciences ,2019, 1:607.

[45] F. D. Leila, D. Joshua ,  Swartz and David W. Wright. The Biomimetic Synthesis of Metal Oxide Nanomaterials. Nanomaterials for the Life Sciences Vol. 2: Nanostructured Oxides. Edited by Challa S. S. R. KumarCopyright © 2009 WILEY-VCH Verlag GmbH & Co. KGaA, Weinheim. ISBN: 978-3-527-32152-0

[46] C. Ray, T. Pal. Recent advances of metal-metal oxide nanocomposites and their tailored nanostructures in numerous catalytic applications.

[47] I. Ahmad, F. A. Fazal Rahim. Clay Based Nanocomposites and Their Environmental Applications.Nanomaterials and their Fascinating Attributes, 2018, Vol. 2, 166-190.

[48] F. Uddin.  Clays, nanoclays, and montmorillonite minerals. Metall. Mater. Trans., A Phys. Metall.Mater. Sci., 2008, 39(12), 2004-2814

[49] C. H. Zhou. An overview on strategies towards clay-based designer catalysts for green and sustainable catalysis. Appl. Clay Science, 2011, 53  87–96.

[50] B.J. Borah, S.J. Borah, K. Saikia, D.K. Dutta. Efficient Suzuki–Miyaura coupling reaction in water: Stabilized Pd0-Montmorillonite clay composites catalyzed reaction.  Applied Catalysis A: Gen, 2014, 469, 350.

[51] F. Wang, F. Pan, G. Li, P. Zhang, N. Wang. Construction of spherical montmorillonite supported Cu-based catalyst doping with a covalent organic framework for 4-nitrophenol removal. Applied Clay Science, 2021, 214, 106278.

[52]. L.A.Galeano, M. Angel Vicente, A.Gil. Catalytic Degradation of Organic Pollutants in Aqueous Streams by Mixed Al/M-Pillared Clays (M = Fe, Cu, Mn). Catalysis Reviews: Science and Engineering, 2014, 56:239-287.

[53]. C. Li, M. Wei, D. G. Evans, X.  Duan. Layered Double Hydroxide-based Nanomaterials as Highly Efficient Catalysts and Adsorbents. Small, 2014. DOI: 10.1002/smll.201401464.

[54] P. Saikia, R.L. Goswamee. Catalytic partial oxidation of CH4 to syn gas (H2/CO) in presence of N2O over periclase type SiO2@Ni(Mg,Al)O catalyst synthesized by non aqueous route. Catal.Commun., 2019, 119:1-5.

[55] Zhengyang Cai, Xiuming Bu,   Ping Wang,  Johnny C. Ho,  Junhe Yangand  Xianying Wang. Recent advances in layered double hydroxide electrocatalysts for the oxygen evolution reaction. J. Mater. Chem. A, 2019, 7, 5069-5089.

[56] J. Safaei Ghomi, M. Ghasemzadeh. Silver iodide nanoparticle as an efficient and reusable catalyst for the one-pot synthesis of benzofurans under aqueous conditions. J. Chem. Sci.,2013 125, 1003.

[57] H. Cong, C.F. Becker. Silver nanoparticle-catalyzed Diels-Alder cycloadditions of 2'-hydroxychalcones. J. Am. Chem. Soc., 2010, 132, 7514.

[58] H. Ahmed, M.K. Hossain. Supported nanocatalysts: recent developments in microwave synthesis for application in heterogeneous catalysis. Material Advances, 2022, 3, 859.

[59] B. J.Borah, D.K.Dutta, P.P.Saikia, N.C.Barua, D.K.Dutta. Stabilization of Cu(0)-nanoparticles into the nanopores of modified montmorillonite: An implication on the catalytic approach for “Click” reaction between azides and terminal alkynes. Green Chem., 2011, 13,3453.

[60] P.K. Saikia, P.P. Sarmah, D.K. Dutta. Stabilized Fe3O4 magnetic nanoparticles into nanopores of modified montmorillonite clay: a highly efficient catalyst for the Baeyer–Villiger oxidation under solvent free conditions Green Chem.,2016 18, 2843.

[61] D.K. Dutta. Recent advances in metal nanoparticles supported on Montmorillonite as catalysts for organic synthesis J. Mat. Nanosci. 2019, 6(1), 19-31.