PLANTMASS MEDIATED SYNTHESIS OF METAL TUNGSTATE NANOPARTICLES: A SHOT REVIEW ON ITS SYNTHESIS, CHARACTERIZATION, AND PHOTOCATALYTIC APPLICATIONS

R. Karthiga*,                                                                                                S.Karthikarani, T. Pandimeena

PG and Research Department of Chemistry,                                               Department of Physics,

Cardamom Planters' Association College,                                                  Cardamom Planters' Association College,

Bodinayakanur,                                                                                            Bodinayakanur,

Theni, Tamilnadu, 625531 India.                                                                Theni, Tamilnadu, 625531 India

skarthika1121@gmail.com

Abstract

Recently, metal oxide nanoparticles (NPs) have been shown to have substantial commercial potential. The intrinsic qualities of nanomaterials, such as their exact size, shape, composition, increased surface-to-volume ratio, and purity of individual components, make them intriguingly adaptable materials. This paper presents a full explanation of contemporary green synthesis research that is more advantageous than traditional chemical synthesis in terms of cost, pollution reduction, and environmental and human health safety. In particular, the role of Tunstate nanoparticles (NPs) as photocatalysts has gained great interest because of their potential electronic structural configuration, light absorption capabilities, and charge transport characteristics. Plant-based green technologies have been created for the production of nanoparticles because to the high concentration of hazardous substances and the harsh conditions utilised in chemical and physical processes. The definition of metal oxides as photocatalysts, their structural characteristics, the prerequisites for photocatalysts, the classification of photocatalysts, and the mechanism of the photocatalyst are all covered in this article. The diverse life on our planet is in grave risk from water contamination caused by many substances like metal ions, textile dyes, medical waste, other residential activities, and industrial operations. Numerous methods are used for purifying water that is contaminated, notably adsorption, ion exchange, flotation, coagulation-flocculation, electrochemical precipitation, chemical precipitation, and reverse osmosis. The development of new and improved processes that boost the effectiveness of water treatment depends significantly on nanotechnology. Since oxides of metals act as a diverse group of nanomaterials, extensive research is being done to figure out them and use them to purify contaminated water of contaminants. This review studies photocatalytic wastewater treatment using different metal oxide nanoparticles. The influence of several particular characteristics such as the catalyst synthesis technique, the starting dye concentration, the quantity of nanocatalyst needed for degradation, the initial pH of the dye solution, the kind of light source employed, and the exposure period. Special emphasis was given to the light required to remove the dye. Based on a preliminary study of the extant literature, some broad findings were reached. The study compares suspended and supported catalysts in-depth, discusses their general/specific requirements, key factors affecting degradation, and performance evaluation methods. In order to attain increased removal effectiveness in an efficient fashion, several appropriate test conditions must be adopted to breakdown these resistant dyes. Future research directions are also given.

Keywords: green synthesis, degradation, metal tungstate, doping, coupling.

Introduction

One of the ideas that has advanced the fastest in recent years is nanotechnology, which has brought great technological as well as scientific breakthroughs. A range of new systems, structures, devices, and nanoplatforms with potential applications could be developed created using nanomaterials with distinctive physicochemical properties [1], [2].  In contrast to their enormous surface area and volume, nanomaterials have increased thermal conductivity, catalytic reactivity, nonlinear optical efficiency, and chemical stability [3]. Plenty of researchers have been motivated to look for novel synthesis techniques by this feature. Although conventional methods (physical and chemical processes) take less time to create a large number of nanoparticles, they call for toxic materials like preservatives to maintain their stability, which is toxic to the environment. Considering this, plant-based green technology is gaining popularity as an environmentally friendly, non-toxic, and safe alternative, because the green synthesis of nanoparticles mediated by plant extracts is economically favourable, and provides natural coatings in the form of proteins [4], and allows the careful synthesis of different shapes and sized nanoparticles. Plant based biomass synthesis of nanoparticles is a method of producing nanoparticles using biologically derived materials.

This review discusses traditional synthetic methodologies with an emphasis on current improvements in synthesis methods for greener metals, metal oxides, and other relevant NPs. The methods and environmental factors that affect the surface shape, degradability, and other characteristics of these green synthetic NPs are subsequent studied. An evaluation of the current status and future prospects in the synthesis of nanoparticles using various green technologies concludes the study. This study focuses on novel and enhanced environmentally friendly synthesis techniques for metal oxide nanoparticles that are responsive to a variety of stimuli, producing outstanding and cost-effective nanomaterials [5], that can be used in a variety of applications and are biodegradable. This environmentally friendly synthesis not only creates incredibly efficient nanocarriers, but also accomplishes its goals without endangering the environment or other living things.

Green chemistry is employed in the biological synthesis of NPs because it is non-toxic, ecologically friendly, and energy efficient. The fundamentals of green chemistry, including preventative, safer chemical synthesis, the use of renewable raw materials, reducing derivatives, etc., emerged as a consequence of biological synthesis. From the biological approach, NPs are created from sources such as fungi, bacteria, plants, animals, etc. The synthesis of NPs from plant extracts offers more advantages than from other biological sources since it demands more expensive culture maintenance and microbial separation [6]. Nanoparticles is frequently employed as an artificial component due to its safety and viability. Alkaloids, proteins, carbohydrates, enzymes, phenolic acids, and other substances used in stabilisation and reduction processes can all be found in plants. Plants function as biological substrates that reduce the need for chemicals to act as reducing, capping, and stabilising agents to make metal nanoparticles from the appropriate precursor solutions since they contain so many essential phytochemicals. [7]. Leaf extracts are commonly employed in green synthesis since leaves contain various metabolites, and this process is safe, biocompatible, and ecologically beneficial[8], [9].

Rapid industrialization, new development processes, and a rising population have continually harmed the global environment [10], [11]. Organic pollutants from diverse sources such as industry, agriculture, and chemicals have seriously contaminated water, which creates a hazard to people and aquatic life [12]. Organic dyes have been extensively employed in numerous fields, such as the textile, leather, paper, and pulp industries, and they end up in industrial effluent. Several studies have been carried out on the degradation of these organic dyes under the effect of photocatalysts [13–15], however, there are various approaches to obtain the ultimate solution.

Beneath the impact of ultraviolet (UV) or visible wavelengths, the catalyst is utilised to accelerate the chemical reactions of the photocatalyst. The phrases "photo" and "catalysis" derive from ancient Greek. In photocatalysis light is the "photo" which speeds up the rate of the reaction by using an external material ("catalyst") which is not itself consumed in the process. A catalyst lowers the activation energy needed for a chemical reaction and speeds up the process. So far, there are three different methods to create visible light photocatalysts: (i) generate a donor level above the valence band by doping some elements with wide-gap semiconductors in typical photocatalysts, (ii) create a new valence band using some elements, (iii) manage the band structure by generating the solid solution shown in Fig. 1. Recently there have been many studies on the second strategy and new materials such as SrWO4[16], Tb3 /La2(WO4)3[17], BiWO4 [18], MnWO4 [19], WO3/g-C3N4/V2O5 [10], WO3 [20]. WO3 is an excellent photocatalytic material and is directly connected to visible light photocatalytic materials. Due to faults in the production process of WO3, the material is somewhat biased towards n-type semiconductors.

Fig .1 Mechanism of photodegradation of WO3 with metal doping

Since WO3 has an experimental bandgap energy (Eg) of 2.5 to 3.0 eV, it is possible that it can absorb the majority of visible light and so function as a visible light-driven photocatalyst. The band gap of several metal tungstates is given in Fig. 2. [21]. The formation of pairs of electrons and holes under light is one of the properties of the material as a photocatalyst. The recombination duration of this pair is longer with a capable photocatalyst. In addition, these electron and hole pairs form hydroxyl radicals (OH-) and superoxide radicals (O2-), which have been proved to be good scavengers for the photocatalytic elimination of harmful dyes.

Fig.2. Band gap of transition metal tungstate

Direct mechanism for dye degradation

Because of their propensity to absorb part of the visible light, another process of photocatalytic dye degradation may occur in the visible light. This technique requires excitation of the dye in a visible light photon (λ > 400 nm) from the ground state (Texture dye) to the triplet excited state (Texture dye*). This excited state dye is further transformed to a half-oxygenated radial cation (Turkture) by electron injection into the conduction band of NPs  [22]. As a consequence of the interaction between these trapped electrons and oxygen dissolved in the system, superoxide radical anions (O2−˙) are generated, which in turn induce the creation of hydroxyl radicals (OH˙). These OH radicals are largely responsible for the oxidation of the organic compounds given in the equations and Fig 3. below. [8], [23].

Coloured pollutant + hν → Coloured pollutant *

Coloured pollutant * + NPs → Coloured pollutant + + NPs −

Fig. 3. Mechanism of oxidation of the organic compounds using OH· radicals

Advantages of green synthesis

The chemical reduction agents employed in this approach are typically pricey, toxic, and lethal. An alternate green reducer that has a modest response is economical and simple to use, and works as a stabilizer is extremely wanted. The practical use of the above method is primarily due to the existence of bioactive compounds in plants, such as terpenoids, phenols, alkaloids, flavonoids, quinines, or tannins, which not only have antibacterial and antioxidant abilities, but also reduce metal ions and stabilize nanoparticles [24]. In addition, plant extracts not only have good biocompatibility, biodegradability, environmental friendliness, and cheap cost, but also form a stable protective barrier for MNPs and so prevent MNPs from aggregating  [25].

According to the growing acceptance of green approaches, numerous ways have been devised to generate ZnO NPs from diverse sources such as bacteria, fungus, algae, plants, and others. A collection of tables has been prepared to highlight works in this area (Table 1).

Table. 1. List of nano tungstates synthesized by different plant extract and their size and shape

| S.no | Plant | Tungstates | Size | Shape | Reference |
| --- | --- | --- | --- | --- | --- |
| 1 | Gelatin | WO3 | 40 | Hexagonal crystal | [26] |
| 2 | Rhamnusprinoides | WO3 | 60 | Spherical shape | [27] |
| 3 | Spondiasmombin | WO3 | 5.90 | Agglomerated | [28] |
| 4 | Agar-agar from red seaweed | CoWO4 | 84.3 | Strong agglomeration | [29] |
| 5 | Red algae (Rhodophyta). | CoWO4 | 13-30 | Nanospheres | [29] |
| 6 | Aloe vera | FeWO4 | 15.83 | Nanorods | [30] |
| 7 | Brassica rapa | CdWO4 | 27 | Rod shape | [31] |
| 8 | Azadirachta indica | NiWO4 | 31.1 | Agglomerated | [32] |
| 9 | Phyllanthus Amarus | NiWO4 | 33.49 | Flower | [33] |
| 10 | Hyphaene thebaica L | ZnWO4 | 24 | Rod | [34] |
| 12 | Lemon | ZnO-CuWO4 | 97.70 | Agglomerated | [35] |
| 13 | Starch | TiO2–Bi2WO6 | 13.5 | Nanoplates | [36] |
| 14 | Lignin | Ni-CoWO4 | - | Disordered plate | [37] |

1. Tungstate

1.1. Tungstate for detection of toxicity

Ghazal et al. described the synthesis of tungsten oxide nanosheets (WO3-NS) utilising the sol-gel process. For the manufacture of Na2WO4 as a tungsten source in gelatin soln., which acted as a novel green stabilizer, characterized by XRD, FESEM/EDX, Raman, UV and vis. DRS. Photocatalytic experiments were carried out using WO3-Nanosheets (650 °C) for the optical degradation of the dye at the surrounding temperature using a high-pressure mercury vapour lamp (50 W) as the light source. It analyses the elimination of MB dye at 95% in 187 minutes by degrading the organic portion of the dye. This finding demonstrated the great predilection of these nanoparticles for the removal and degradation of pigments, whose reaction kinetics were shown to be practically first order. In addition, WO3-NS ceased cytotoxicity in Huh-7 cells and demonstrated low cytotoxicity, showing the biocompatibility of the nanosheets at high concentrations. In addition, identical findings were seen even at high doses up to 31 μg/ml, whereas Huh-7 cells demonstrated excellent resistance in the MTT test.

Fig.4. FE-SEM image of WO3-NS calcined at 650◦C[26]

  - Tungstate for antibacterial performance:

Rhamnusprinoides extract of leaves and sodium tungstate precursor were employed to prepare tungsten trioxide nanoparticles with a monoclinic shape for investigating their potential as antibacterial agents. The author studied the synthesised WO3 using X-ray diffraction (XRD), scanning electron microscopy (SEM) and Fourier transform infrared spectroscopy (FTIR) to study its antibacterial activity. Synthesised WO3 nanoparticles showed amazing antibacterial activity both at doses of 250 mg/ml and 125 mg/ml. As demonstrated in Fig. 5, the inhibition zones of Listeria monocytopens (Lm), Staphylococcus aureus (Sa), Salmonella typhimurium (Sa), Escherichia coli (Ec) and Candida albicans (Ca) were analysed comparable to earlier results [38], [39]

Fig 5. SEM and Antibacterial activity of WO3 [27]

  - Tungstate for structural research through pH

Tijani et al., attempts to generate WO3 nanoparticles of regulated form and size, which were synthesized from ammonium paratungstate, (NH4)10W11O41•5H2O) and aqueous extract of spondiasmombin in a simple, easy, and economical approach [28]. In addition, solution pH and calcination temperature had a critical impact on the morphological arrangement and structural properties such as average crystallite size and surface area [40, 41]. Crystallite sizes were shown to rise with solution pH and calcination temperature. At the pH of the solution and the calcination temperature utilised, there was no change in the phase type of WO3, but only the monoclinic polymorph was formed [42]. Furthermore, the observed form may be attributed to the binding, binding and stabilizing action of the aqueous spondiasmombin biomolecules in the generated WO3 nanoparticles. And in general, it was revealed that the particle size of WO3 nanoparticles climbed in the order of 13.8 < 14.3 < 16.7 nm and 1, 4, 7 and 10 in the order of pH correspondingly. An acidic environment encourages the pure monoclinic symmetry of WO3. In summary, all the characterization techniques used in this work confirmed the successful synthesis and monoclinic phase formation of WO3 nanoparticles with a higher specific surface area and small crystal size compared to other manufacturing techniques found in the literature, and its SEM image was shown in Fig. 6.

Fig.6. HRSEM images of WO3 nanoparticles generated at optimal pH of 1 and calcined at temperature (a) 250 °C, (b) 350 °C,(c) 450 °C, (d) 550 °C, and (e) 650 °C with continuous holding time of 2 h[27]

- Transition metal doped Tungstate

2.1 Prolonged durability of electrodes by Cobalt tungstate

The author provides a protein sol-gel green technique utilising red algae (Rhodophyta) agar to synthesise cobalt tungstate (CoWO4) powders for battery-like electrodes. In contrast, CoWO4 is similarly generated by comparable protein chemistry utilising flavourless gelatin. The resulting powders were calcined at 800 °C for 2 h and afterwards investigated using XRD (Rietveld refinement), SEM/EDS, FTIR/Raman/UV-Vis-NIR spectroscopy, VSM and numerous electrochemical tests to examine the battery-like behaviour in an alkaline environment (3 MOH). The data reveal that samples prepared with gelatin had an average particle size of 150 nm and a crystallite size of 68 nm, compared to 284 nm (particles) and 84 nm (crystallites) for the agar-agar-treated materials. Magnetic testing at 300 K confirmed the paramagnetic behaviour of both samples. Analysis of samples made as 4.926 m of these curves revealed an effective magnetic moment per cobalt atom of 4.908 m with gelatin and agar, respectively. The performance of CoWO4 as a battery-like electrode is attributed to the surface faradic Redox reaction mechanism coupled with the reversible valence state between CO2 and CO3. The discharge curves demonstrate no notable fluctuations in electrochemical activity, with a highest specific capacity of 77 C g-1 and a specific current of 1 A g-1 [43]. The long-term endurance of the electrodes can be verified by the capacity retention of about 98% through 1000 charge-discharge cycles at 1 A g-1 was shown in Fig. 7 [44].

Fig 7.  Graphical abstract for capacity retention and charge-discharge cycles of cobalt tungstate [29]

2.2 Iron tungstate for selective determination of theophylline

Theophylline can be detected selectively and sensitively employing Aloe Vera extract from plants coated iron tungstate nanorods (AFW) immobilised Nafion (Nf) modified glassy carbon electrode (GCE) (AFW/Nf/GCE), according to the author [30]. Co-precipitation was used to generate AFW, that was then analysed using a number of techniques, namely elemental analysis (EDX), scanning electron microscopy (SEM), X-ray diffraction (XRD), Fourier transform infrared spectroscopy (FT-IR), and electrochemical tests. Comparing theophylline oxidation on AFW/Nf/GCE to bare GCE and iron tungstate (FW) modified GCE, it is interesting to note that the former showed increased electrocatalytic activity. With a low limit of detection (LOD) of 0.0028 mM, theophylline oxidation in the electrochemical sensor also demonstrated a linear response range from 0.1 to 160 mM [45]. As can be seen in Figure 9, this sensor demonstrated excellent selectivity, stability, and reproducibility in the biological and food samples under study. It has been successfully used to identify theophylline specifically in urine, black tea, and human serum samples.

Fig.8. SEM images for a) iron tungstate and b) aloe vera plant decorated iron tungstate

Fig.9 (a) shows the AFW/Nf/GCE's DPV response in 0.1 MPBS (pH 7.0) with theophylline concentrations ranging from 0.1 to 160 µM, and (b) shows the inset calibration plot showing the linear relationship between peak current and theophylline concentration.

2.3 Bismarck brown R photodegradation of Via Brassica rapa leaf of CdWO4

According to Fatima et al., CdWO4 was synthesised and in situ functionalized utilising Brassica rapa leaf extract for the Bismarck brown R rod-shaped f-CdWO4 for adsorption and photocatalytic activity. The functional properties of CdWO4 has been demonstrated via XRD, SEM, TEM, and FT-IR techniques. The average particle size was found to be 54 nm using XRD and TEM imaging. The length and average width of the nanorods were both 120 nm. Considering the influence of dosage, starting concentration, contact time, solution pH, and temperature, a batch adsorption test was conducted. In 15 minutes, 1.5 gL-1 of f-CdWO4 was able to remove 80% of Bismarck brown R dye from an initial concentration of 10 mg L-1. At an acidic pH, the improved adsorption capacity of f-CdWO4 was optimised. At 30 °C, f-CdWO4 had the highest Langmuir adsorption capacity at 46.5 mg-1. The surface functionalization of CdWO4 was blamed for the improved absorption capability of Bismarck brown R f-CdWO4. Excellent photocatalytic activity towards Bismarck Brown R was also shown by f-CdWO4. The degradation process of Bismarck brown R is shown in Fig. 10. CdWO4 for adsorption and photocatalytic activity for the Bismarck brown R

Fig.10. Proposed simplified degradation scheme of Bismarck brown R

2.4. Nickel tungstate for photocatalytic activity of dye

Particles of nickel tungstate (NiWO4) altered with Azadirachta indica extract of plants were synthesised by a co-precipitation technique developed by Karthiga et. al [32] and others and characterised by UV-vis-DRS, FT-IR, XRD, SEM, TEM and EDX techniques and SEM findings suggested that the plant extract altered NiWO4 included of tiny spheres in Fig. 11. Based on XRD observations, bare NiWO4 created through the co precipitation approach had an average crystallite size of 31.11 nm, whereas NiWO4 infused with plant extract exhibited a smaller average crystallite size of 12.12 nm. Methylene blue (MB) was used as a model organic polluter for the investigation of NiWO4 nanoparticles photocatalytic activity [46]. under visible light illumination. At a PNT dosage of 0.05 g/L and an MB concentration of 10 µM, optimal photodegradation is reached after 180 minutes under tuned reaction conditions. According to Fig. 12, PNT was more effective than Gram (+ve) and Gram (-ve) microorganisms.

Fig. 11. SEM image of NiWO4 and plant extract modified NiWO4

Fig. 12. The zone of inhibition of PNT against (a) Staphylococcus, (b) Salmonella (c) Klebsiella (d) Aspergillus niger[47]

2.5. ZnWO4 for the visible light photocatalytic activity of dye

Fig. 13 shows how Hyphaene thebaica fruit extract can be used to produce zinc tungstates via green chemistry, according to K. Hkiri et al. The biosynthesized powder was found to have good crystallinity and to be completely free of impurities and secondary phases, based on structural analysis. Numerous elements with oxygen vacancies were discovered by RBS spectroscopy, which is in perfect accord with both the EDS and anticipated outcomes. Scanning and transmission microscopes were used for the morphological analysis, which revealed that the zinc tungsten was made up of spherical nanoparticles that were evenly distributed and contained some rod-like particles [34], [48]. To assess the photocatalytic efficiency of biosynthesised ZnWO4, MB was employed as an organic dye. Under visible light irradiation, a series of reactions with various starting concentrations were carried out using a 1 g/L ZnWO4 catalyst. As the initial dye concentration increased from 1.10-5 mol/L to 3.10-5 mol/L, the degradation efficiency of MB fell from 98.4% at 90 min to 90% at 270 min. Additionally, data on scavenger activity showed that the main reactive species involved in the photodegradation of MB dye are O2 and OH radicals. The photodegradation of MB on zinc tungsten photocatalysts was explained using a hypothetical reaction mechanism based on experimental and theoretical evidence. It was demonstrated that oxygen vacancies can increase the photocatalytic energy by producing more oxidised groups and preventing electron-hole recombination (Fig. 14), in addition to lowering the energy needed for the electronic transition from VB to CB by forming defective energy levels in the ZnWO4 band gap. Therefore, oxygen vacancies should be responsible for the increased visible light absorption of biosynthesized ZnWO4. Recycling experiments showed persistent photocatalytic activity of ZnWO4 produced through green chemistry. As a result, a ZnWO4 catalyst that may be used as a photocatalytic catalyst for pollutant degradation may be produced by a fruit extract of Hyphaene thebaica.

Fig. 14.Photocatalytic degradation methylene blue mechanism of ZnWO4 [49]

3. Coupling

3.1 ZnO-CuWO4 for environmental and biological fields

This research shows that an environmentally friendly choice for separating CR from aqueous solution is the ZnO-CdWO4 nanoparticle. When creating ZnO-CdWO4 nanoparticles, the leaf extract was used as a reducing, capping, and stabilising agent. A considerable number of functional sites on the adsorbent surface are also provided by the phytochemicals present in the leaf extract, increasing the adsorption capacity. According to the determined estimated ΔGo, ΔSo and ΔHo values, which show the best agreement with the Freundlich isotherm model, CR adsorption was spontaneous and exothermic. The better fit of the CR adsorption to the pseudosecondary kinetic model further suggested that it was driven by a chemisorption mechanism (Fig. 15). The shape of the ZnO-CdWO4 surface and FT-IR spectra of Congo red-charged ZnO-CdWO4 demonstrate the involvement of electrostatic and hydrogen bonding during CR absorption. We identified the real rate-determining phase in the CR adsorption process using interparticle diffusion and Boyd plots. As a result, the intraparticle diffusion mechanism illustrated the basic regulation of CR molecule adsorption on the ZnO-CdWO4 surface [50]. As a result, in this study, the use of ZnO-CdWO4 NPs for the adsorptive removal of Congo red represents a novel and promising approach to the treatment of water. Due to the dominance of competing adsorption processes, the co-occurrence of pollutants may have reduced the adsorption removal of CR dye. ZnO-CdWO4 is a viable candidate for both environmental and biological applications due to the cooperative action of metal oxides and plant phytochemicals. Its potential as a photocatalyst, antioxidant, antibacterial, and anticancer agent needs more study. In conclusion, it was found that ZnO-CdWO4 produced via green synthesis is a cost-efficient, highly efficient, and sophisticated material to address numerous environmental issues.

Fig 15. Scheme for various reduction of dye[51]

Fig .16. SEM and TEM image of  ZnO-CdWO4Nanocomposite

3.2.TiO2/Bi2WO6 photocatalytic processing of biomass

This research examines a novel photocatalytic technique to reduce complicated biomass into smaller molecular units for use in the manufacturing of biofuel feedstocks[52]. After the hydrothermal process, the TiO2-Bi2WO6 nanocomposite photocatalyst was employed for various TiO2 ratios, viz. 15 and 25 wt% were created. The photodegradation efficiency of the organic molecule is determined. The composite loaded with 25% TiO2 was determined to represent a maximum photocatalytic efficiency of 99.9%. The structural and optical characteristics of the produced photocatalytic nanomaterial were studied. Rhodamine B elimination in Fig.17 revealed a band gap of 2.7 eV for the 25% TiO2 composite with remarkable visible light photoactivity. Additionally, we find that this combination has four times the photocatalytic activity of pure Bi2WO6 [53]. A biopolymer, usually starch, is photocatalytically fragmented using this chemical to create smaller molecular precursors. Starch monomerization is discovered through a colorimetric analysis of reducing sugars from decomposing biomass. The produced linear chain's molecular fragments underwent additional Raman, FTIR, and ESI-MS analysis. The results show that TiO2/Bi2WO6 nanocomposite photocatalytic pretreatment of starch results in the formation of organic precursors, which are typical raw materials for anaerobic methanation and ethanol fermentation microorganisms. As a result, we draw the conclusion that the processes of biomass hydrolysis and partial acetogenesis can both benefit from biomass photocatalytic pretreatment. This idea offers a sustainable method of turning biomass waste into biofuel [36].

Fig. 17. Mechanism of photodegradation of TiO2–Bi2WO6[36]

4. Bimetal doping using tungstate

4.1. Ni-CoWO4 for electrochemical application

In this study, the secondary metal (M2) in the bimetallic tungsten compounds (M2M1WO4, M2 = Ni, M1 = Co) is evaluated for its role in the pseudocapacitance. It was discovered that the bimetallic tungsten (NiCoWO4) functionalized lignin supercapacitor had a high SPC value of 862.26 mF cm-2, which was 141 times greater than the monometallic tungsten (CoWO4) functionalized lignin supercapacitor's SPC value of 6.1 mF cm-2 [37]. Due to the larger oxidation state that is accessible in the bimetallic tungsten secondary metal M2 (M2M1WO4, M2 = Ni, and M1 = Co), the pseudo capacitance is significantly increased, which improves electron conductivity. Due to the combined effects of lignin-encapsulated bimetallic tungsten NPs, the lignin/NiCoWO4 supercapacitor also exhibits the highest energy density of 5.75 Wh kg-1 and the highest power density of 854.76 kW kg-1. The capacitance retention increased as the fraction of bimetallic tungsten NP in the composite electrode grew. The retention was 100% even after 2000 cycles at the optimal lignin: NiCoWO4: PVDF mass ratio (15:75:10), and their morphological investigations are presented in Fig. 18. An examination into supercapacitor discharge times showed that retention was increased at shorter discharge intervals and considerable SPC at longer discharge periods. As a result, NiCoWO4's pseudocapacitive nanomaterial's electroactive site consumption rate was inversely proportional to discharge time. Lignin's molecular structure is changed by carbonation, which results in high charge transfer impedance and decreased electrochemical efficiency [54]. It has been demonstrated that the choice of the negative electrode's surface area and dielectric permittivity, as well as the kind of charge storage regulating system—dominant EDLC or pseudo-capacitance—all have a substantial impact on the capacitive performance of the bimetallic tungsten supercapacitor. In order to successfully apply and design bimetallic tungstate-based nanobioelectronic devices that advance green technology, our study provides new knowledge [9].

Fig 18. SEM image for; (a) CoWO4 (low magnification), (b) CoWO4 (high magnification), (c) Ni-CoWO4 (low magnification), and (d) Ni-CoWO4 (high magnification).[37]

CONCLUSION

In this work, we offer evidence for the synthesis of multi-metallic NPs from diverse plant extracts and the examination of these NPs by UV-vis, XRD, FT-IR, SEM and TEM. In this review, the importance of the optical band supporting photocatalytic activity was described. NPs made from plant extracts have been particularly efficient in decomposing hazardous organic dyes and cleansing contaminated water. Recent breakthroughs in the research of metallic NPs reveal that mixing them with semiconductors is a feasible strategy to build efficient materials that react to visible light. It is realistic to think that such endeavours will permit unfailing success in the development of metallic NPs and make them a key element of visible light photocatalysts. However, they are still inferior in terms of usage and stability. To boost the photocatalytic effectiveness, scavengers must be frequently added to make these photocatalysts photocatalytically stable. In the context of applied nanotechnology, the enhancement of dependable and environmentally acceptable methodologies for the production of metal NPs is a vital step. The future of research should thus concentrate on boosting the production of nanoscale metal particles, the utilisation of inexpensive raw materials and the development of simple energy-saving technologies. As a consequence, it is feasible that the green synthesis of nanoscale metals has extensive applicability and great development potential. We think that this study will enable new researchers working in this area to understand how metal nanoparticles are created and how they are employed.

Reference

[1]	S. C. Capaldi Arruda, A. L. Diniz Silva, R. Moretto Galazzi, R. Antunes Azevedo, and M. A. Zezzi Arruda, “Nanoparticles applied to plant science: A review,” Talanta, vol. 131, pp. 693–705, Jan. 2015, doi: 10.1016/j.talanta.2014.08.050.

[2]	H. Mirzaei and M. Darroudi, “Zinc oxide nanoparticles: Biological synthesis and biomedical applications,” Ceram. Int., vol. 43, no. 1, pp. 907–914, Jan. 2017, doi: 10.1016/j.ceramint.2016.10.051.

[3]	H. Agarwal, S. Venkat Kumar, and S. Rajeshkumar, “A review on green synthesis of zinc oxide nanoparticles – An eco-friendly approach,” Resour. Technol., vol. 3, no. 4, pp. 406–413, Dec. 2017, doi: 10.1016/j.reffit.2017.03.002.

[4]	H. Abdul Salam, R. Sivaraj, and R. Venckatesh, “Green synthesis and characterization of zinc oxide nanoparticles from Ocimum basilicum L. var. purpurascens Benth.-Lamiaceae leaf extract,” Mater. Lett., vol. 131, pp. 16–18, Sep. 2014, doi: 10.1016/j.matlet.2014.05.033.

[5]	R. Khursheed et al., “Biomedical applications of metallic nanoparticles in cancer: Current status and future perspectives,” Biomed. Pharmacother., vol. 150, p. 112951, Jun. 2022, doi: 10.1016/j.biopha.2022.112951.

[6]	S. K. Chandraker, M. K. Ghosh, M. Lal, T. K. Ghorai, and R. Shukla, “Colorimetric sensing of Fe 3+ and Hg 2+ and photocatalytic activity of green synthesized silver nanoparticles from the leaf extract of Sonchus arvensis L.,” New J. Chem., vol. 43, no. 46, pp. 18175–18183, 2019, doi: 10.1039/C9NJ01338E.

[7]	M. Sharma, J. Singh, and S. Basu, “Efficient metal ion adsorption and photodegradation of Rhodamine-B by hierarchical porous Fe-Ni@SiO2 monolith,” Microchem. J., vol. 145, pp. 708–717, Mar. 2019, doi: 10.1016/j.microc.2018.11.042.

[8]	T. Bavani et al., “One-pot synthesis of bismuth yttrium tungstate nanosheet decorated 3D-BiOBr nanoflower heterostructure with enhanced visible light photocatalytic activity,” Chemosphere, vol. 297, p. 133993, Jun. 2022, doi: 10.1016/j.chemosphere.2022.133993.

[9]	I. P. Sahu, D. P. Bisen, R. K. Tamrakar, K. V. R. Murthy, and M. Mohapatra, “Luminescence studies on the europium doped strontium metasilicate phosphor prepared by solid state reaction method,” J. Sci. Adv. Mater. Devices, vol. 2, no. 1, pp. 59–68, Mar. 2017, doi: 10.1016/j.jsamd.2017.01.001.

[10]	B. Parasuraman, B. Kandasamy, V. Vasudevan, and P. Thangavelu, “Enhanced dye degradation performance enabled by swift electron mediator decorated WO3/g-C3N4/V2O5 hybrid nanomaterials,” Environ. Sci. Pollut. Res., Jun. 2023, doi: 10.1007/s11356-023-28200-w.

[11]	A. N. MARQUES JUNIOR et al., “Tracking atmospheric dispersion of metals in Rio de Janeiro Metropolitan region (Brazil) with epiphytes as bioindicators,” An. Acad. Bras. Cienc., vol. 90, no. 3, pp. 2991–3005, Sep. 2018, doi: 10.1590/0001-3765201820170905.

[12]	M. G. Neelavannan, M. Revathi, and C. Ahmed Basha, “Photocatalytic and electrochemical combined treatment of textile wash water,” J. Hazard. Mater., vol. 149, no. 2, pp. 371–378, Oct. 2007, doi: 10.1016/j.jhazmat.2007.04.025.

[13]	A. Akhundi and A. Habibi-Yangjeh, “Ternary g-C3N4/ZnO/AgCl nanocomposites: Synergistic collaboration on visible-light-driven activity in photodegradation of an organic pollutant,” Appl. Surf. Sci., vol. 358, pp. 261–269, Dec. 2015, doi: 10.1016/j.apsusc.2015.08.149.

[14]	Y. Anjaneyulu, N. Sreedhara Chary, and D. Samuel Suman Raj, “Decolourization of Industrial Effluents – Available Methods and Emerging Technologies – A Review,” Rev. Environ. Sci. Bio/Technology, vol. 4, no. 4, pp. 245–273, Nov. 2005, doi: 10.1007/s11157-005-1246-z.

[15]	Y. Chang, X. Liu, A. Cai, S. Xing, and Z. Ma, “Glycine-assisted synthesis of mesoporous TiO2 nanostructures with improved photocatalytic activity,” Ceram. Int., vol. 40, no. 9, pp. 14765–14768, Nov. 2014, doi: 10.1016/j.ceramint.2014.06.066.

[16]	L. S. Cavalcante, J. C. Sczancoski, N. C. Batista, E. Longo, J. A. Varela, and M. O. Orlandi, “Growth mechanism and photocatalytic properties of SrWO4 microcrystals synthesized by injection of ions into a hot aqueous solution,” Adv. Powder Technol., vol. 24, no. 1, pp. 344–353, Jan. 2013, doi: 10.1016/j.apt.2012.08.007.

[17]	K. N. Kumar, L. Vijayalakshmi, J. Lim, and J. Choi, “Dazzling green luminescent and biocompatible Tb3+ -activated lanthanum tungstate nanophosphors for group-III evaluation of latent fingerprints and anticancer applications,” J. Alloys Compd., vol. 959, p. 170415, Oct. 2023, doi: 10.1016/j.jallcom.2023.170415.

[18]	A. Elaouni, M. El Ouardi, A. BaQais, M. Arab, M. Saadi, and H. Ait Ahsaine, “Bismuth tungstate Bi 2 WO 6 : a review on structural, photophysical and photocatalytic properties,” RSC Adv., vol. 13, no. 26, pp. 17476–17494, 2023, doi: 10.1039/D3RA01987J.

[19]	V. Sasikala, P. Karthik, S. Ravichandran, N. Prakash, J. Rajesh, and A. Mukkannan, “Effective removal of organic dyes using novel MnWO4 incorporated CA/PCL nanocomposite membranes,” Surfaces and Interfaces, vol. 40, p. 103008, Aug. 2023, doi: 10.1016/j.surfin.2023.103008.

[20]	R. Surakasi et al., “Methylene Blue Dye Photodegradation during Synthesis and Characterization of WO3 Nanoparticles,” Adsorpt. Sci. Technol., vol. 2022, pp. 1–10, Jul. 2022, doi: 10.1155/2022/2882048.

[21]	M. Fang, X. Tan, Z. Liu, B. Hu, and X. Wang, “Recent Progress on Metal-Enhanced Photocatalysis: A Review on the Mechanism,” Research, vol. 2021, Jan. 2021, doi: 10.34133/2021/9794329.

[22]	J. Zhao, C. Chen, and W. Ma, “Photocatalytic Degradation of Organic Pollutants Under Visible Light Irradiation,” Top. Catal., vol. 35, no. 3–4, pp. 269–278, Jul. 2005, doi: 10.1007/s11244-005-3834-0.

[23]	C. Galindo, P. Jacques, and A. Kalt, “Photodegradation of the aminoazobenzene acid orange 52 by three advanced oxidation processes: UV/H2O2, UV/TiO2 and VIS/TiO2,” J. Photochem. Photobiol. A Chem., vol. 130, no. 1, pp. 35–47, Jan. 2000, doi: 10.1016/S1010-6030(99)00199-9.

[24]	K. B. Narayanan and N. Sakthivel, “Green synthesis of biogenic metal nanoparticles by terrestrial and aquatic phototrophic and heterotrophic eukaryotes and biocompatible agents,” Adv. Colloid Interface Sci., vol. 169, no. 2, pp. 59–79, Dec. 2011, doi: 10.1016/j.cis.2011.08.004.

[25]	B. Li et al., “Mesoporous cobalt tungstate nanoparticles for efficient and stable visible-light-driven photocatalytic CO2 reduction,” Mater. Today Energy, vol. 24, p. 100943, Mar. 2022, doi: 10.1016/j.mtener.2022.100943.

[26]	S. Ghazal, M. Mirzaee, and M. Darroudi, “Green synthesis of tungsten oxide (WO3) nanosheets and investigation of their photocatalytic and cytotoxicity effects,” Micro Nano Lett., vol. 17, no. 11, pp. 286–298, Sep. 2022, doi: 10.1049/mna2.12134.

[27]	Y. A. Asratemedhin B. Habtemariam, “Synthesis of WO3 Nanoparticles using Rhamnus Prinoides Leaf Extract and Evaluation of its Antibacterial Activities,” Biointerface Res. Appl. Chem., vol. 12, no. 1, pp. 529–536, Apr. 2021, doi: 10.33263/briac121.529536.

[28]	J. O. Tijani, O. Ugochukwu, L. A. Fadipe, M. T. Bankole, A. S. Abdulkareem, and W. D. Roos, “One-step green synthesis of WO 3 nanoparticles using Spondias mombin aqueous extract: effect of solution pH and calcination temperature,” Appl. Phys. A Mater. Sci. Process., vol. 125, no. 3, Mar. 2019, doi: 10.1007/s00339-019-2450-y.

[29]	H. V. S. B. Azevêdo et al., “Green synthesis of CoWO4 powders using agar-agar from red seaweed (Rhodophyta): Structure, magnetic properties and battery-like behavior,” Mater. Chem. Phys., vol. 242, Feb. 2020, doi: 10.1016/j.matchemphys.2019.122544.

[30]	A. Karthika, C. Sudhakar, A. Suganthi, and M. Rajarajan, “Eco-friendly synthesis of aloe vera plant extract decorated iron tungstate nanorods immobilized Nafion for selective and sensitive determination of theophylline in blood serum, black tea and urine samples,” J. Sci. Adv. Mater. Devices, vol. 4, no. 4, pp. 554–560, Dec. 2019, doi: 10.1016/j.jsamd.2019.09.004.

[31]	B. Fatima, S. I. Siddiqui, R. Ahmed, and S. A. Chaudhry, “Green synthesis of f-CdWO4 for photocatalytic degradation and adsorptive removal of Bismarck Brown R dye from water,” Water Resour. Ind., vol. 22, Dec. 2019, doi: 10.1016/j.wri.2019.100119.

[32]	R. Karthiga, B. Kavitha, M. Rajarajan, and A. Suganthi, “Photocatalytic and antimicrobial activity of NiWO4 nanoparticles stabilized by the plant extract,” Mater. Sci. Semicond. Process., vol. 40, pp. 123–129, Jul. 2015, doi: 10.1016/j.mssp.2015.05.037.

[33]	K. Buvaneswari and M. Ganagaraj, “GREEN SYNTHESIS OF NiWO 4 NANOPARTICLES USING PHYLLANTHUS AMARUS EXTRACT.”

[34]	K. Hkiri, H. E. A. Mohamed, C. B. Mtshali, N. Mongwaketsi, A. Gibaud, and M. Maaza, “Promising photocatalytic activity under visible light of ZnWO4 nanocrystals prepared via green synthesis approach,” Mater. Today Commun., vol. 35, p. 106355, Jun. 2023, doi: 10.1016/j.mtcomm.2023.106355.

[35]	B. Fatima et al., “Facile green synthesis of ZnO–CdWO4 nanoparticles and their potential as adsorbents to remove organic dye,” Environ. Pollut., vol. 271, Feb. 2021, doi: 10.1016/j.envpol.2020.116401.

[36]	L. Shiamala, K. Alamelu, V. Raja, and B. M. Jaffar Ali, “Synthesis, characterization and application of TiO2-Bi2WO6 nanocomposite photocatalyst for pretreatment of starch biomass and generation of biofuel precursors,” J. Environ. Chem. Eng., vol. 6, no. 2, pp. 3306–3321, Apr. 2018, doi: 10.1016/j.jece.2018.04.065.

[37]	S. Jha, S. Mehta, E. Chen, S. S. Sankar, S. Kundu, and H. Liang, “Bimetallic tungstate nanoparticle-decorated-lignin electrodes for flexible supercapacitors,” Mater. Adv., vol. 1, no. 6, pp. 2124–2135, 2020, doi: 10.1039/d0ma00494d.

[38]	U. Baig, M. A. Gondal, S. Rehman, and S. Akhtar, “Facile synthesis, characterization of nano-tungsten trioxide decorated with silver nanoparticles and their antibacterial activity against water-borne gram-negative pathogens,” Appl. Nanosci., vol. 10, no. 3, pp. 851–860, Mar. 2020, doi: 10.1007/s13204-019-01186-z.

[39]	G. Duan et al., “Robust Antibacterial Activity of Tungsten Oxide (WO 3-x ) Nanodots,” Chem. Res. Toxicol., vol. 32, no. 7, pp. 1357–1366, Jul. 2019, doi: 10.1021/acs.chemrestox.8b00399.

[40]	Z. Gu et al., “Large-scale synthesis of single-crystal hexagonal tungsten trioxide nanowires and electrochemical lithium intercalation into the nanocrystals,” J. Solid State Chem., vol. 180, no. 1, pp. 98–105, Jan. 2007, doi: 10.1016/j.jssc.2006.09.020.

[41]	N. S. Kavitha, K. S. Venkatesh, N. S. Palani, and R. Ilangovan, “Fungus mediated biosynthesis of WO3 nanoparticles using Fusarium solani extract,” 2017, p. 050130. doi: 10.1063/1.4980363.

[42]	Karthiga Rajendaran and Sudha Annamalai1, “Green Synthesis of ZnO Nanoparticles Using Sollanam Santhocarbom to Study Its Solarphotocatalytic Activity,” Int. J. Sci. Res., vol. 6, no. 6, pp. 2370–2376, Jun. 2015.

[43]	A. Mohamed Azharudeen, R. Karthiga, M. Rajarajan, and A. Suganthi, “Enhancement of electrochemical sensor for the determination of glucose based on mesoporous VO2/PVA nanocomposites,” Surfaces and Interfaces, vol. 16, pp. 164–173, Sep. 2019, doi: 10.1016/j.surfin.2019.05.005.

[44]	A. Mohamed Azharudeen, R. Karthiga, M. Rajarajan, and A. Suganthi, “Selective enhancement of non-enzymatic glucose sensor by used PVP modified on α-MoO3 nanomaterials,” Microchem. J., vol. 157, p. 105006, Sep. 2020, doi: 10.1016/j.microc.2020.105006.

[45]	A. M. Azharudeen et al., “Ultrasensitive and Selective Electrochemical Detection of Dopamine Based on CuO/PVA Nanocomposite-Modified GC Electrode,” Int. J. Photoenergy, vol. 2022, pp. 1–9, Feb. 2022, doi: 10.1155/2022/8755464.

[46]	R. Karthiga, B. Kavitha, M. Rajarajan, and A. Suganthi, “Synthesis of MoO3 microrods via phytoconsituents of Azadirachta indica leaf to study the cationic dye degradation and antimicrobial properties,” J. Alloys Compd., vol. 753, pp. 300–307, Jul. 2018, doi: 10.1016/j.jallcom.2018.04.230.

[47]	A. M. Azharudeen et al., “Solar Power Light-Driven Improved Photocatalytic Action of Mg-Doped CuO Nanomaterial Modified with Polyvinylalcohol,” J. Nanomater., vol. 2022, pp. 1–15, Mar. 2022, doi: 10.1155/2022/2430840.

[48]	B. Fatima et al., “Photocatalytic removal of organic dye using green synthesized zinc oxide coupled cadmium tungstate nanocomposite under natural solar light irradiation,” Environ. Res., vol. 216, p. 114534, Jan. 2023, doi: 10.1016/j.envres.2022.114534.

[49]	K. Hkiri, H. E. A. Mohamed, C. B. Mtshali, N. Mongwaketsi, A. Gibaud, and M. Maaza, “Promising photocatalytic activity under visible light of ZnWO4 nanocrystals prepared via green synthesis approach,” Mater. Today Commun., vol. 35, p. 106355, Jun. 2023, doi: 10.1016/j.mtcomm.2023.106355.

[50]	K. Buvaneswari, R. Karthiga, B. Kavitha, M. Rajarajan, and A. Suganthi, “Effect of FeWO 4 doping on the photocatalytic activity of ZnO under visible light irradiation,” Appl. Surf. Sci., vol. 356, pp. 333–340, Nov. 2015, doi: 10.1016/j.apsusc.2015.08.060.

[51]	A. Sarwar, A. Razzaq, M. Zafar, I. Idrees, F. Rehman, and W. Y. Kim, “Copper tungstate (CuWO4)/graphene quantum dots (GQDs) composite photocatalyst for enhanced degradation of phenol under visible light irradiation,” Results Phys., vol. 45, p. 106253, Feb. 2023, doi: 10.1016/j.rinp.2023.106253.

[52]	I. Arora, H. Chawla, A. Chandra, S. Sagadevan, and S. Garg, “Advances in the strategies for enhancing the photocatalytic activity of TiO2: Conversion from UV-light active to visible-light active photocatalyst,” Inorg. Chem. Commun., vol. 143, p. 109700, Sep. 2022, doi: 10.1016/j.inoche.2022.109700.

[53]	Y. M. Lee and C. H. Lai, “Preparation and characterization of solid n-TiO2/p-NiO hetrojunction electrodes for all-solid-state dye-sensitized solar cells,” Solid. State. Electron., vol. 53, no. 10, pp. 1116–1125, Oct. 2009, doi: 10.1016/j.sse.2009.07.004.

[54]	R. Arunadevi, B. Kavitha, P. P. Sudha, M. Rajarajan, and A. Suganthi, “Photocatalytic enhancing for tin oxide nanoparticles by codoping with nitrogen and bismuth,” Desalin. Water Treat., vol. 78, pp. 330–340, Jun. 2017, doi: 10.5004/dwt.2017.20773.