Piezo-and Magneto-Active Polymer Scaffolds in Tissue Engineering

Ogah Anselm Ogah*1, Friday Nwankwo Archibong2

1Department of Polymer & Textile Engineering, Nnamdi Azikiwe University, P.M.B. 5025, Awka, Nigeria

2Department of Mechanical Engineering, Alex-Ekwueme Federal University Ndufu-Alike Ikwo, P.M.B. 1010, Nigeria

*Corresponding Author Email Address: ao.ogah@unizik.edu.ng

Abstract

Biomedical engineering depends on scaffoldings for boosting cell diversification and development having rearmost precedence on incitement feedback platforms, sometimes nominated active structures. Amongst the elucidative in this substance order are piezoelectric structures, able of igniting positive or negative ions subject to insouciant excitation that generates substantial anticipation to exercising pulpits for safe treatment of whim-whams cell. Tissue engineering and recreating drug are growingly making good use of responsive accoutrements, enabling the force of determined signal to the organism. Specifically, the using electro-active substrates which conveys charged cue to the cells through involuntary excitations, unlock new chemical and high-tech windows which actually copy suggestions as well as issues which take place within natural systems, enabling elaboration at applicable terrain for restoration of organs.Therefore, an innovative approach was evolved that piezo-magneto-active polymer scaffolds are suitable for delivering those signals. This chapter focuses on the applications of piezo-magneto-active polymer scaffolds in tissue engineering.

Keywords: piezo-magneto-active, polymer scaffolds, tissue engineering, smart materials

Introduction

Smart accoutrements astronomically relate to substances that adjustably alter several of their active features, in agreement with forced outside incitement or to the changes within the immediate terrain [1]. An external persuading comprises light, temperature, and electromagnetic fields, pH, stress and strain. Piezoelectric pulpits can be contemplated as intelligent systems which convert mechanical cargo to electrical cues [2]. Pierre Curie and Jacques Curie in 1880 reported that the presence of a demitasse chassis and the absence of a center of harmonydetermine the piezoelectricity of a material [3]. “Piezo” is chased from the word “Piezein” meaning pressure which is of Greek origin [4].Piezoelectric products have a broad multifariousness of operations in electronics including transducers, selectors and detectors. Besides, notable area of operations of piezoelectric products is in biomedical engineering similar as electro-active platforms for organ reconstruct and restoration. Piezoelectric accoutrements convey changing charge activations in the absence of a source of external power [5]. The piezoelectric altar can induce electrical stimulation which can regenerate and repair napkin through defined routes [6]. The fine-tuned parcels of piezoelectric can make accurate bio-electro emigrations, identical with native matrisome, notable amid revamping situation in bone [7].

In biomedical engineering, electro-active support are veritably important in towel engineering using ionic excitation for the organ reconstruct or restoration, like neural organ reconstruct, bone reconstruct and restoration among others. [8]. Piezoelectricity has been observed in bone, cartilage, dentin, tendon and keratin [9]. A fiber-suchlike structure similar as collagen is anintroductory element in bone and cartilage responsible for the piezoelectric parcels [10]. The piezoelectric parcels of collagen cause electric cues in response to internal forces. The extracellular matrix (ECM) conveys the cues to the voltage-gated passages in the cell membrane. Largely, the osteoblasts are participators with mechano-transduction which village with bone-forming cells and bone-breaking cells. Boosting of these pathways conveys the extracellular cues to the origin guiding pungency of communicating avalanches, in control of the cellular conditioning including matrix manufacture, cell development and towel reconstruct [11]. Thus, electro-active structures imitating piezoelectric adjuvant of ingrain napkins could bean applicable procedure to reconstruct and restore bone and cartilage.

The objectification of cells, bioactive factors and pulpits for biomedical operations, similar as towel engineering, permits the advancement of natural reserves to restore and/or enhance towel functions [12]. Pulpits constitute a vital element in towel engineering approaches, allocating the structural bolster for cell growth in addition to the needed stimulantsfor factual towel regeneration [13, 14]. In this perspective, active intelligentaccoutrements are suitable to reversibly change one or further of their functional or structural features in a regulated and reproducible style when subordinated to outside stimulants, like temperature, stress, electric or glamorous fields, among others [15, 16]. The application of those smartaccoutrements is suitable to mimic the dynamic natural cell terrain by doling outhandyperson and/or electric stimulants identical to the bones available in the mortal organism [17]. Amid smart substances, electro-active accoutrements have depicted aptness for towel engineering operations owing to their implicit to transfigure a mechanical distortion into an electrical eventualityand contrarily, without taking an outside voltage origin [15, 18]. Thus, intelligent accoutrements are of enormous significance to refurbishing functional bio-mimetic microenvironments. This field is using merit of piezoelectric accoutrements to mimic electrical and mechanical signals living in the natural napkin and hence help in their ingrain rejuvenescence [19].

Bone diseases are an enlarging radix of solicitude as they produce important effect on humans, confining their standard of living, and on their families. They're veritably frequent, substantially amid aged people, and have high related prices. Between the colorful types of bone affections, osteoporosis is linked to greater costs [20, 21] and owing to increase in senior citizens, furtherindividualities are being touched. Persons impacted with osteoporosis have anadvanced trouble of fractures [22], creating impairment and confining their standard of living. Relating to remedy, present remedies are effective, although they've weak long-term compliance, being the mitigation of fractures typically the target of the treatment [23].With the growth of towel engineering ways, curatives have been advanced for bone-related affections [24]. Actually, towel engineering holds a high function for successful cure for bone complications and remarkable attempts are being conducted to develop current efficient restoration plans [25]. These rearmost plans bear refurbishing bone towel microhabitat, that covers mechanical, electromechanical and biochemical stimulating rudiments which are responsible for the modulation of osteogenic cell function [25].

Majority of accoutrements applied in bone towel engineering furnish external biochemical stimulants, like growth factors, yet there is a deficit of bioactivity in vivo, a hassle to manage overdose division and inaccurate prosecution, and as a result, clinical prospects of these accoutrements is confined [26]. Thus, current accoutrements and conduct are needed so as to surmount these lapses. One practicable way is creating biophysical stimulants, like mechanical and electrical, as they are available in the course of bone growth and function [26]. Natural bone towel is piezoelectric, which implies that when a mechanical incantation is done on the bone, an electric terrain is generated [27]. Actually, piezoelectric substances have been described to enhance osteoblasts proliferation and isolation [28, 29]. Amid the colorful physical stimulants, mechanical forces have been extensively studied as a catalyst to impel natural cellular response in a mechano-transduction process.

Nevertheless, rearmost types of physical stimulants like the employment of electrical and glamorous signals are getting prominent. Following the development of accoutrementswisdom, the concurrent application of similar stimulants is doable using intelligent accoutrements which via mechanical incantation concomitantly incite electrical or glamorous microenvironments on bone [29, 30]. Piezoelectric substances are one case of similar intelligent accoutrements. Regarding bone towel engineering, piezoelectric substances are contemplated new and the mix between biochemical factors and physical stimulants have been recently described [28, 29]. Either, modifying the face unevenness and face eventuality of the pulpits, it’s realizable to regulate the cell attachment [31] and mineralization procedure [32], independently. These kinds of accoutrements permit to modulate the function of the cells and ultimately make factual osteogenesis, boosting an electric eventuality to cells that revives osteoblasts in vitro, in a non-infectious manner. Colorful sizes and morphologies includingpervious membranes, nanofibers and flicks have been estimated for a befitting measure in bone towel engineering, utmost of the inquiries using these pulpits as a template for napkins and cells to gain [28–30, 33].

This chapter will be concentrated on the operations of piezo-and-magneto-active polymer scaffolds in tissue engineering.

Tissue Engineering

Tissue engineering is a treatment system that confronts towel injury or deterioration, which targets to make up new towel from individual samples, in likewise in-vitro or in-vivo conditions, avoiding the craving for contributors or waitlist [34]. But, it needs accoutrements with particular customized parcels, after attaining a height of bio-mimicry that permits advancement in flourishing and functional towel. Bulk muscle loss, owing to complaint or critical bruise, is especially serious problem of towel injury owing to the difficulty and low fixable of muscle towel. As a result, colorful treatments affect in reprehensible issues [35]. Towel engineering is an implicit remedy to this issue, still, the point and particular demands of the cadaverous muscle filaments engenders that norespectable towel engineering remedies have yet been advanced. A satisfactory result needs to be suitable to furnish the cells with either inert stimulants, like mechano-transduction by ways of accoutrements with particular stiffness and/or pulpits composed of acquainted filaments [36,37], and energetic stimulants, like dynamic electrical and mechanical, mimicking the natural growth surroundings of muscle towel [38]. Also, sundry of the accoutrements needed to be biocompatible and impeccably biodegradable, permitting the stimulants to be applied in a manageable way via rejuvenescence process.

Smart accoutrements are defined as accoutrements that are manipulated to respond in a controllable and reversible way, modifying some of their parcels as a result of external stimulants, similar as mechanical, chemical, electrical, or glamorous [39], have the eventuality to break these walls. Especially, polymer-grounded smart accoutrements can be reused into diverse morphologies, similar as flicks, filaments, and microspheres [40], and have been delved for towel engineering operations in bone [41], cardiac [42], and cadaverous muscle napkins, where it has been validated that energetic acquainted polymer fiber pulpits farther cell advancement and towel rejuvenescence [36,37]. One specific process, electrospinning, permits accurate mastery of micro- and nanofiber parcels, so that they can be modulated to particular purposes of end napkins and microenvironments, enhancing cell and towel rejuvenescence [37].

Certain of the constantly being biodegradable polymers applied in towel engineering designs are poly (α-hydroxy esters), such as poly (lactic acid) (PLA), poly (glycolic acid) (PGA), and the different poly (lactic-co-glycolide) (PLGA) copolymers [43]. Accepted for medical administration by both the US Food and Drug Administration (FDA) and the European Medicines Agency (EMA) [44], PLGA is a lot chosen rather than its homopolymers owing to excellent mastery of its degradability, permitting for use-specific revision. This polymer is either biocompatible and/or biodegradable, with its declination passing via a hydrolytic volume declination procedure, through arbitrary disunion medium, and its derivatives being lactic acid and glycolic acid, that are doused from natural organisms through the renal system [45]. PLGA has been reused in a different of morphologies, like micro and nanoparticles (NP), 3D pulpits and filaments [45], with biomedical uses in medicine delivery, diagnostics and towel engineering [46].Beneficial to modulate physical–chemical parcels of the polymers or to incite particular responses, like glamorous or electrical conductivity, polymer mixes are being fabricated for biomedical operations [46–48]. Amid the constantly employed paddings are glamorous bones, delved in spheres similar as hyperthermia, magneto-mechanical [49], and magneto-electric influences [41], among others, and conductive paddings delved in the field of electro-active stimulants [42]. As for glamorous spaddings for polymer blends, iron (II, III) oxide (Fe3O4) is a biocompatible emulsion that has been estimated for a variety of uses, from detectors and selectors to biomedicine and environmental requital [49,50]. Fe3O4 NPs present super-paramagnetic conduct at confines below 20 nm and is ferri-glamorous around 20 and 300 nm [51], making it fascinating for magnetically guiding the administration of stimulants in polymer-grounded pulpits.

The mature mortal heart is an active organ in control of blood pumping and rotation, in addition to oxygen and nutrients dispensation all over the body [52]. Cardiovascular diseases (CVDs) radiate from the irrecoverable detriment to cardiac cells caused by death of cells and death of body napkins, being the crucial originator of demise and fitness profitable rigors widely [53]. On damage or complaint, cardiac napkins have inadequate form capacity and are substituted by dysfunctional napkins, impacting the constrictive capability of the heart which can affect to disastrous failure [54, 55]. In these cases, transplantation is needed to recoup heart performance [56], but, it’s veritably confined by the availability of benefactors [56]. Cardiac towel engineering is a prospective strategy to substitute injured corridor of the heart with in vitro-finagled cardiac napkins that is a possible option to heart transplantation [56, 57]. Notwithstanding, developing fully grown cardiac napkins in vitro is still demanding [58], remarkable advance has been made over the last years concerning the advancement of useful biomaterials and biomimetic pulpits that can be employed to cardiac towel engineering [59–61]. In line with biomaterial's standpoint, intelligent piezoelectric accoutrements can produce redundant functionalities hence their character as under sub-caste and subscribe towards the advancement of cell-biomaterial exchange. Especially, piezoelectric accoutrementshave the prospective to mimic the mechano-electrical transduction structure available in cardiac napkins still they’ve been nearly fully delved in bone and cartilage towel engineering [62].

Beside the common biochemical signals furnished by bioactive factors, bioelectricity transmission, moderated by internal electrical fields and currents, plays a vital function as a biophysical signal [63–66]. In the deconstruction, different kinds of tissues bestow electrically conductive and/or responsive attributes similar as piezoelectricity and ferro-electricity, and hence numerous functions are controlled by electrical cues. As explained in Fig. 1, these types of towel comprises the nervous system, heart, bone, muscle, and skin, that are engaged in the affairs of neural rotation [67–74], twinkle functions [75–79], bone restoration80–83], muscle condensation[84–86], and trauma mending independently [87–89]. The nervous system, heart, and supplementary muscles are electro-active napkins organs in the mortal body. Amid them, the nervous system possesses the unrivaled electrical exertion, which transmits cues from neurons to the targeted corridor via synapses. Cardiomyocytes are the trendsetter cells of the heart and are responsible for dispatching out metrical stimulants. This metrical electrical encouragement runs via the whole heart and ultimately arrives at the ventricular myocytes, and next there is mechanical exertion, which is, heart pumping. Bone and skin also use electrical fields and also piezoelectricity to restore new tissues [64]. Internal bioelectrical cues are among the most apropos signals to decide towel function in electro-sensitive tissues and thereby play a significant function in the towel restoration process [63].

Fig.1: Electrical activity on the human body

Pulpits for Towel Restoration

Pulpits set up on electrospun electroactive nanofiber

Electrospinning is a type of high tech that is facile to handle and can be applied industrially. By using an electric field (EF) on the aeroplane of a thick and elastic fluid, ultra-fine filaments (having compasses varying between a few micrometers toknockouts of nanometers) are assembled by the proposition of electrostatic aversion [5, 65].Through altering the spinning variables and gathering processes, the arrangement and constitution of the deduced nanofibers can be regulated, to the extent that the nanofibers attain the asked mechanical stiffness and grasp the directional mastery of cell geste that can be employed for towel engineering [6, 10]. Synthetic polymers, like poly (ε-caprolactone) (PCL), poly (lactic acid) (PLA), and poly (lactic-co-glycolic-acid) (PLGA) and natural polymers, similar as collagen, gelatin, chitosan, and silk have been considerably manufactured by electrospun technology for towel reconstruct and restoration. When immingled with electrical stimulation, two typical kindof electrically active nanofibers are being estimated (i) electrically conductive nanofibers and (ii) piezoelectric nanofibers. Expiring from the conductive or piezoelectric nanofibers, biocompatible intelligent widgets like biosensors, medicine delivery bias, and nanogenerators have been advanced to foster the form of cardiac, whim-whams, bone, skin, and so forth.

Electrically conductive nanofiber pulpits can be developed embedded on different types of substrates varying from conductive polymers, like polyaniline (PANI), polypyrrole (PPy), and poly(3,4- ethylenedioxythiophene) corroborated with poly(styrene sulfonate) (PEDOT:PSS), to carbon-grounded nanomaterials, like graphene, graphene oxide (GO)and reduced graphene oxide (rGO), and carbon nanotubes (MWCNT), besides metallic nanoparticles. PANi is one of the loftiest favorable conductive polymers with quality biocompatibility in vitro at the same time not inspiring seditious responses in vivo [91–93].Carbon-grounded nanomaterials typically manifest exceptionally elevated conductivity, increased photothermal and mechanical properties, yet questionable biocompatibility. Conductive polymers can be directly electrospun to electrically conductive nanofibers by modulating the electrospinning variables, or a runner polymer can be blended with the conductive polymers to enhance the electrospinning eventuality. Once the rate of PANi to gelatin is 6:4, the conductivity of nanofibers made by electrospinning becomes 21mScm-1 [94]. A different procedure to make conductive nanofibers is to incorporate conductive nanomaterials into the polymer matrix via doping or face revision with conductive polymers, essence nanoparticles and carbon-grounded nanomaterials.

Piezoelectric biomaterials can attain electromechanical change, converting mechanical energy into electrical energy not having an external power source [95–97]. Alongside other piezoelectric accoutrements, upon the operation of a force through the direction of the piezoelectric measure of the nanofibers, deciduous charges are produced on the two facing shells of the accoutrement, wherein a face eventuality will be created. Responding to internal forces like muscle compression [98], cell traction force [99], or external stimulants similar as ultrasound, mechanical climate, and so on [100-104], piezoelectric nanofibers can convert electricity to natural network in situ, fused with the graces that it can induce biophysical and biochemical signals, fashioning them encouraging for towel rejuvenescence. Piezoelectric polymers that can be employed to fabricate nanofibers via electrospinning comprises polyvinylidene fluoride (PVDF) and its copolymers, similar as polyvinylidene fluoride-trifluoroethylene [P(VDF-TrFE)], Poly-L-lactic acid (PLLA), poly-β-hydroxybutyrate (PHB), poly-3-hydroxybutyrate-3-hydroxyvalerate (PHBV), and certain natural polymers, like collagen, silk, and chitin. Notwithstanding the fact that, piezoelectric polymers retain superior inflexibility and further respectable biocompatibility, their below par piezoelectric properties beget insensitivity to mechanical stimulants, that restricts their operations. The piezoelectricity of polymer substantially hinges on the crystallinity of the piezoelectric demitasse phase. Therefore, by answering the polymer result with nanomaterials like carbon nanotubes or graphene, stretching, or centralizing the nanofiber membrane, the crystallinity of the piezoelectric phase can be enhanced and, as a result, the general piezoelectricity of the membrane [105]. Nonetheless, this optimization is confined. The doping of lead-free piezoelectric ceramic nanomaterials can mainly enhance the piezoelectric properties of the membrane. Typical bones encompass barium titanate, lithium niobate, zinc oxide, gallium nitride, boron nitride, and so on.

Applications of Electro-active scaffolds in Tissue Engineering: Electrospun Nanofiber

Cardiac rejuvenescence

Myocardial necrosis can affect in weakened cardiac function, creating a significant waste of cardiomyocytes (CM). Waste CMs are restored by different stingy towel, and followed by irregular twinkle. The narrowing geste of CMs is modulated by the changing electromechanical terrain. Therefore, electroactive electrospun nanofiber pulpits (EENFs) are regarded as an over-and-coming volition in cardiac towel engineering. The single axis aligned fiber line-up can emulate the shape of natural myocardium, and the electroactive substrate can mimic the electrical-signal-transfer address of CMs to ameliorate the modernize compression. In a study, the rGO/silk fibroin electrospun nanofibers could bear the aligned stretching of CMs with a rod-suchlikeshape and acquainted sarcomere structures, permitting for the product of an aligned cardiac towel form with a fresh strong compression force [33]. By the operation of external EF to a nanofiber altar dressed with cardiac cells, a greater development towel form can be created with substantial proteins connected to muscle compression and electromechanical coupling. The exertion of a nanofiber altar for cardiac towel form is substantially influenced by its electrical conductivity. Invigorated rat CMs show the optimum wobbling performance on a fiber mat made of collagen (9.89%), hyaluronic acid (1.1%), and PANi (1.34%) [31]. The aligned magnetically PCL nanofiber altar enclosed with PVDF-TrFE can’t only ameliorate the cling of cardiac cells, but can also save some cell population rate and the pulsating of CMs, as well as accelerating the development [106].

Treatment of Nerve Wound

The suitable strength of electrical excitement can boost neurite expansion and neural isolation of neural stem cells (NSCs), and ameliorate the incarnation of whim-whams-linked proteins, that are probative for whim-wham rejuvenescence. Taking into account the electrophysiological features and frame of the nervous system, an applicable EENFS should have electrical attributes and particular morphological parcels to direct cell geste and ameliorate neuronal enterprise. The whim-whams pointer conduit (NPC) is applied as a viaduct to link the conterminous and side boundaries of injured jitters to repair girding whim-wham injury. Whim-wham channels bestowed with electrical exertion have a superior remedial result [106,107]. The migration, proliferation, myelination and incarnation of the myelin-definite gene of Schwann cells on poly (L-lactic acid-co-ε-caprolactone) (PLCL) nanofibers covered with rGO were remarkably bettered [108]. Electrical stimulation also fosters the neural isolation of PC12 cells on conductive pulpits. NGC embedded on EENFSs could boost the rejuvenescence of rat sciatic whim-whams crack, with issues similar to autologous transplantation. PPy was also applied as a covering of electrospun PLCL pulpits. Upon electrical stimulation (100 mV/cm), rejuvenescence of injured rat sciatic whim-whams was stimulated, whim-wham conduction haste and side emulsion muscle exertion prospects were also enhanced [108].

EENFSs have also been used for the repair of spinal cord crack by enhancing axonal stretching and neuron cell reconnection. When conductive PPy was invested in PLA nanofibers, varied to the separating order, the conductive nanofibers displayed a greater 21–point Basso, Beattie, and Bresnahan (BBB) open-field movement class and bettered electrophysiological affair in transected rat spinal cord model [109]. Whim-whams growth factors can also be added in micro-patterned conductive nanofiber pulpits as biochemical signals. During electrical stimulation, the topographical and electrical signals synergistically stimulate the proliferation, direct neuron isolation of NSCs, and enhance neurite stretching [54]. Piezoelectric polymers have been employed to modulate the direction of neurons and neurite projection devoid of the use of outside energy sources [110,111]. By altering the microstructural features of the electrospun piezoelectric fiber pulpits PVDF and PVDF-TrFE, it can give further broad mechanical transduction and electrical parcels for rearward root ganglions. Through modulating cell exertion, which influences cytoskeleton morphology and mechanical transduction signals [112], the stress filaments in whim-wham cells are produced and actuated yea-associated protein (YAP) nuclear localization, egging bettered neural isolation. An outside EF is applied as a non-invasive system to give electrical stimulation to remedy brain damage and neurodegenerative affections [113]. The power viscosity and period of the electrical stimulation as well as the growth ages of the hippocampal neurons, contribute to the variations in the neuronal feedback to the EFs [114]. Presently, the operation of combined electrical stimulation and EENFS for brain damage rectifiers is still scarce, but could be an implicit and intriguing exploration theme in the future.

Piezo–and Magneto-Active Biomaterials and Structures

Electroactive polymers like poly (vinylidene fluoride) (PVDF) and poly (L-Lactic acid) (PLLA) are being reused into pulpits with different shapes and sizes, similar as microspheres [115,116], membranes [117-119], filaments [120-122], and three dimensional (3D) pulpits by colorful ways [123] like electrospray, solvent casting and electrospinning procedures (Fig. 2). Recently, attempts are being concentrated on the elaboration of magneto-active biomaterials via the addition of glamorous patches for towel engineering [124]. Pulpits embedded on microspheres have gained surging cognizance for biomedical operations and boost for cell growth and isolation [115, 125]. Piezo- and magneto-active microspheres can be synthesized by various processes like phase separation or rush, conflation/solvent evaporation and electrospray [115].The difference in the processing parameters substantially permits the mastery of the flyspeck size and size distribution. PVDF microspheres with an unrough face and a mean periphery between 800 nm up to 7 μm have been achieved by electrospray process, where microspheres are made employing a polymer result in an adequately conductive solvent [115, 126]. In the electrospray procedure, counting on the result variables similar as result concentration, viscosity and surface pressure and the processing variables such as inflow rate, needle peiphery, distance of needle to collector, and applied voltage, a constant and charged spurt can be run down into driblets, proceeding in microspheres of colorful sizes [127]. This approach may master the lapses linked with traditional flyspeck-creating strategies like solvent casting, single and double conflation, spray-drying, pervious glass membrane emulsification, and coacervation [127]. Skimp studies have been described on PVDF and PLLA magneto-active microspheres.

Fig. 2: (a) neat (b) magnetic PLLA microspheres gotten by oil-in-water emulsion (c) random and (d) oriented PPLA fibers achieved via electrospinning; PVDF 3D scaffold gotten  by (e) solvent casting/NaCI particulate leaching, (f) solvent casting and nylon template and (g) freeze extraction.

Magneto-active PVDF microspheres gotten via this process implanted magnetostrictive patches like cobalt ferrites (CoFe2O4) nanoparticles into the PVDF sphere matrix are primarily in the β-phase (around 65% and 85%) [126]. It is noteworthy that electrospray does not permit a precise mastery of the sphere size [128]. From a conflation-solvent birth/evaporation process it is tenable to achieve biodegradable piezo- and CoFe2O4 compound PLLA-grounded microspheres with manageable size and compasses gauging from 0.16 to 3.9 μm for neat PLLA and between 0.8 and 2.2 μm for the compound microspheres [128]. Specifically for neural and muscle operation, towel engineering stringy pulpits have been fabricated to support and direct the lengthwise cells distention along their natural axis of development [129]. Aligned and irregular electrospun filaments with atomic severance size, density and large surface area can be achieved via electrospinning, identically to the electrospray process, when result viscosity is large enough (ranging from 650–2500cP) [130]. The electrospinning system makes for effectively achieving PVDF and PLLA irregular and aligned filaments employing a static and a rotating collector, independently, with a mean compasses gauging from ~500-900 nm [122, 131]. As stated by [123], PVDF irregular electrospun filaments show a β phase content about 50%. Raising the gyration speed of the collector from 500 to 2000 rpm, the bit of β phase surges and may gauge from 50 to 85 % owing to the larger stretching of the spurt in the electrospinning system. Also, the objectification of magnetostrictive nanoparticles into the polymeric PVDF result permits the processing of magnetoelectric filaments with a mean fiber periphery of ~325 nm [132]. As stated by [133], counting on solvent and electrospun processing variables, it′s likely to alter the current crystalline phase creating filaments primarily conforming of α or trans-state β or γ phases. The crystallization process of PVDF simply in the β phase can be achieved via high voltage or high stretching rate of the spurts and a rotating collector. Besides, the processing conditions and solvent employed affect the crystalline bit and other characteristics like fiber mean periphery, specific surface area, surface pressure and mechanical properties [122, 133].

3-dimensional pervious pulpits have been achieved via solvent casting/swab filtering, phase separation, gas raging, gel casting, rush and conflation snap–drying [123]. The principal advantages of these severance connected pulpits are connected with their capability to accelerate bettered commerce between cells and napkins, transport of metabolite and nutrients and a suitable vehicle of biochemical/mechanical and or electrical signals performing to the stimulation of both cells and napkins [123]. Electro-active β-PVDF 3D pulpits with colorful pervious sizes, infrastructures and severance interconnectivity have been gotten via solvent casting/particulate filtering (300 to 400 μm) and employing a nylon template (~60 μm or ~150 μm). Also, indurate birth processes with a PVA template boosts the elaboration of porous scaffolds with means compasses of ~300 and 500 μm, being the pervious mean compasses in the same span of the sacrificial material. Thus, the difference of the ratio of the swab into the result and the distance of the fibers of the template permits to regulate the severance size of the scaffold [123]. An identical process, similar as liquid-liquid phase separation with snap birth is applied to reuse PLLA pulpits with connected severance size gauging from 20 to 60 μm [134].

Towel Engineering Rooted on Piezo-and Magneto-Active Biomaterials

Smart polymers have been employed in several towel engineering operations like bone, neural and muscle napkins [135]. Specifically, piezoelectric and magneto-active polymers have been applied in colorful morphologies and with varying cell type. Still, preponderance of these studies is carried out in static conditions. The piezoelectric and magneto-active influence is only demonstrated when the dynamic conditions (either mechanical or electrical) are used (Table 1), or differently, just the appropriateness of the accoutrements and the significance of the face charge, when the material is paddled, are illustrated.

PVDF and its copolymers is the piezoelectric polymer majorly employed for towel engineering operations owing to their higher piezoelectric feedback. Especially, most of the inquiries reporting cell response in dynamic stimulation apply PVDF as a buttressing material for the cell proliferation and isolation. Rodrigues et al. presented that β-PVDF appreciatively charged flicks produce a favorable terrain for perfecting the elaboration and isolation of scapegoat gist cells into osteoblast in dynamic conditions, demonstrating a perfect buttress for the sowing and the development of undifferentiated cells towards a sought phenotype [136]. The compound of biochemical and physical stimulants can pilot to a promising approach of a biomimetic medium present in the mortal body. Ribeiro et al. demonstrated that PVDF negatively charged flicks [137] in dynamic conditions, further fitly mechanical stimulation, led to bettered osteogenic isolation of mortal adipose stem cells, which was established by advanced alkaline phosphatase exertion [138]. In the presence of PVDF flicks, MC3T3-E1 pre-osteoblast cells displayed different responses. In the presence of appreciatively charged β-PVDF flicks and in mechanical stimulants, a larger osteoblast adhesion and proliferation was noticed [139]. These results were established with in vivo studies where β-PVDF flicks were bedded in a bone fault, demonstrating remarkably further excrescence check and bone redoing. In this case, the mechanical conjurations are achieved via the rat migrations [140]. Farther piezoelectric polymers have also been employed similar as collagen type I where the inquiries demonstrated that the 3-D samples mechanically stretched boosted the proliferation and isolation of mortal osteoblastic precursor cells owing to the swell of genes expression connected to the early and late phases of osteoblastic isolation [141].

In relation to whim-whams rejuvenescence, it has also been revealed that PVDF and poly (vinylidene fluoride-trifluoroethylene) (PVDF-TrFe) in dynamic conditions accelerate cell proliferation and isolation. Antedating studies reported by [142] showed that paddled PVDF raises the chance of discerned neurons of mouse neuroblastoma cells and separate neurite lengths after 96 h of cell culture with both media conditions. These issues have been also substantiated with PVDF-TrFe [142]. Blends are also employed. Thus, whim-whams stem cells dressed on PLLA nanofibers with PANI brought about an enlarged neurite outgrowth when electrically stimulated at the same time compared to the cells grown on non-stimulated pulpits. Guo et al. noted that polyurethane/poly (vinylidene fluoride) (PU/PVDF) made by electrospinning have an effect on crack remedial. When the cells were excited by piezoelectric influence, the adhesion of the fibroblasts (NIH3T3) was bettered and as a consequence, advanced mRNA and protein expression degrees than the control pulpits were manifested [143].

A new strategy for towel engineering operations has been attained with biomaterials with magneto-active feedback. The inquiries were formed with MC3T3-E1 pre-osteoblast cells and magneto-active Terfenol-D/PVDF-TrFe blends. These biomaterials promote ≈25% of cell proliferation when the cells are dressed in mechanical and electrical stimulation a bit actuated by the operation of a different glamorous field. For muscle rejuvenescence, it was formerly demonstrated that the surface charged bettered the cell proliferation [144]. Nonetheless, to date, the study in dynamic conditions with piezoelectric biomaterials has not yet been conducted.

Table 1: Biomaterials, cell culture conditions and cells employed for various applications

| Biomaterial | Conditions | Cells | Applications | Ref. |
| --- | --- | --- | --- | --- |
| PVDF positively poled | -Mechanical stimulation -Mechanical stimulation in vertical vibration -Frequency = 1 Hz -Amplitude approx. 1mm | Goat marrow MC3T3- E1 pre-osteoblast | Bone | [136] [139] |
| PVDF Negatively poled | -Mechanical stimulation in vertical vibration -Frequency = 1 Hz -Maximum amplitude approx. 1mm | Human Adipose stem |  | [138] |
| Terfenol-D/P(VDF- TrFE) | -Magnetic stimulation; -Active time = 16 h (10 min of active time and 20 min of repose time); -Non-active time = 8 h; -Frequency = 0.3 Hz; -Displacement of permanent magnets ≈ 20 mm; -Maximum value = 230 Oe; -ME voltages = 0.115 mV. | MC3T3-E1 pre-osteoblast |  | [141] |
| Collagen Type 1 | -Stretched cyclically along the long axis -Frequency = 1 Hz -Magnitude = 10,000 μstrain (1%) -Number of cycles = 1800 -Time = every day for 30 min over a period of 3 weeks. | Human osteoblastic precursor |  | [141] |
| PVDF and PVDF-TrFe | -Sinusoidal output (vibrational forces); -Peak voltage ≈ 2.5mV; -Frequency = 1200Hz -Standard incubator shelves | Mouse neuroblastoma | Nerve | [142] |
| PLLA/PANI | -A silver electrode and a platinum electrode were inserted to opposite ends of the nanofibrous scaffold; -Constant voltage = 1.5 V; -Time = 60 min; -Electric field = 100 mV/mm. | Nerve stem cells |  |  |
| PU/PVDF | -Intermittent deformation of 8% -Frequency = 0,5 Hz | NIH3T3 | Wound therapeutic | [143] |

Stimulants Responsive scaffolds (Piezoelectric) vs. Passive

It is commonly discerned that the towel engineering pulpits should copy natural living extracellular matrix (ECM), enjoying similitude to a doable extent to the ingrain napkins they′re supposed to restore with regard to the chemical composition, morphology, physical and mechanical properties, in addition to biocompatibility and biodegradability. Completely, the introductory prerequisite, that bears to be considered in altar designing include altar biocompatibility, suitable declination time in the situation of biodegradable substances, the attending of interlinked pores in a suitable size range, altar consistence, mechanical properties, and comfort of operation during a surgical approach [145, 146].

It is prominent that extracellular matrix is a veritably active structure it′s continually being renewed, either enzymatically or non-enzymatically, and its molecular factors are put through multitudinous variations. Nevertheless, most of the latest artificial pulpits persists unresistant meaning non-stimuli responsive to the outside exchange of the terrain (static pulpits) [147]. Likewise, traditional static pulpits, still conductive, substantially undo the natural signaling channels, owing to their durability towards the signal transmission. Thus, there′s a dire demand for smart, stimulants responsive pulpits that can produce and convey the bioelectric signals analogous to the native napkins for applicable physiological roles. Piezoelectric substances can produce electrical signals in response to the administered force, which can be palmed indeed by attachment and migration of cells or body movements [148].Employing piezoelectric substances as towel engineering pulpits permits electrical activation in the absence of electrodes, an outside fount of electricity, or bedding batteries. Similar pulpits should have acceptable construction and mechanical properties as well in order to boost cell adhesion, proliferation, and isolation. The dimension of pores must be manageable and regulated so as to allow prolixity of the metabolite, likewise for material cell adhesion to the biomaterial. Ninety percent void bit and a severance size in the span of 10–100 µm appear to be respectable for neuron development. Pulpits designated by 85–90% void bit may be gotten via the electrospinning approach [149].Said porosity is described as boosting cellular migration and regulated prolixity of cells, metabolites, and medium, being essential for cells association, isolation, and durability[150,151].

Penetrating anal tar which is biocompatible, biodegradable, conducting, and vulnerable to infection so as to give neurite outgrowth is a legion undertaking [152]. Prosperous whim-whams rejuvenescence needs towelfinagledpulpits not only for mechanical buttress of  developing neurites and interference of the in-growth of stringy scar napkins, but also to dispatch natural suggestions to direct the axonal growth cone to the side trudge. Polymers are generally those accoutrements that have been mainly used for producing respectable pulpits for neural towel [153].

Application of Piezo-magneto-active Biomaterials in Neural Towel Engineering

Piezoceramics polymers

The first studied piezoelectric substance class is the piezoceramics. The foremost operations were told as far back as 1950, and later, they have been considerably used in the assiduity [154]. Wersing et al. [155] performed the settler exploration on pervious piezoceramics, in addition offered the fundamentals in the thesis and inchoate measures [156]. At present, there is a high demand for lead-free piezoelectric accoutrements, yet the major practical pottery is yet set up on lead zirconate titanate. Rat cortical neurons dressed on PZT slides carpeted with poly-L-lysine extend markedly longer axons, in malignancy of a reduction in cell number. Also, the frequence and breadth of the excitatory postsynaptic currents surged, inferring that piezoelectricity could have increased neuronal exertion [157]. It is important alluding that piezoceramics are employed for medical operations, particularly medical selectors, transducers, and detectors. Owing to antipathetic responses, piezoceramics are not applied in pure result for medical implants. The ingenious systems for medical exercises are complex grounded on polymer matrices, having ceramic paddings, in the form of filaments [158-160]. To gain bone sickness reconstruct, Lopes et al. [161] added barium titanate nanoparticles into polymer matrix, which touched off kindly high voluntary polarization. Likewise, this system is defined by lower weakness and can be employed as electroactive pulpits [162].

Barium Titanate

The foremost piezoelectric corollary in pottery were exhumed in poling of barium titanate (BT) and led to the expansive use of this material class, also as an addition in pulpits, specifically in medical operations [163,164]. Piezoceramics set up on barium titanate show reduced toxin juxtaposed to lead confirmed piezoelectric accoutrements. For their inordinate strain, they are included in the maturity of delved groups of piezoceramic.BT nanoparticles have displayed cytocompatibility, indeed at greater attention of 100 µg/mL [165]. Ciofani et al. [166] showed that PLGA matrix with the addition of BT nanoparticles reinforces the cell proliferation and attachment of osteocytes and osteoblasts. On top of that, the addition of barium titanate nanoparticles into the polymeric matrix enhances the mechanical properties of the combined altar [167] and stimulates cellular exertion in towel engineering operations [168].

Boron Nitride

Boron nitride (BN) embedded nanomaterials play a considerable part in nanotechnology due to their conductivity, mechanical strength, and high thermal stability [169, 170]. The popular boron nitride piezo-accoutrements are in the confines of nanotubes, and with greater cytocompatibility, they can be applied in towel engineering [171] and medicine delivery, owing to their large piezoelectric properties [172-176].It has been demonstrated that boron nitride nanotubes have a positive impact on the adhesion of cells [177].Among all the features of boron nitride nanotubes (BNNTs), their outstanding piezoelectricity is the most essential for applying them as nanovectors to transmitelectrical or mechanical suggestions within cells [178].

Zinc Oxide

Zinc oxide (ZnO) embedded piezoceramics are considerably used owing to their asymmetric hexagonal wurtzite structure and polar demitasse face. They've set up operation as piezoelectric nano generators, performing from the ease of fabrication [179]. ZnO in the shape of nanostructures is biocompatible [180]. It has been proffered that with ZnO dimension, its cytotoxicity expands, which has an effect on the degrees of reactive oxygen species, lowers the mitochondrial membrane eventuality, and causes the product of interleukin in mortal cells. Likewise, it has been shown that chemical revision can hamper toxin, swinging a means for application in biomedical operations [181, 182].

Piezopolymers

Piezoelectric polymers are a kindly current group of accoutrements permitting the conformation of electrical charges under mechanical activation in the absence of redundant energy sources or electrodes [183, 162].Similarly, which is veritably vital from the biomedical perspective, polymers are able to attain the conditions of biocompatibility and biodegradability, which is veritably critical for new types of implants in regenerative drug [184, 163]. Also, their huge merit is the veritably large processing flexibility, which distinguishes them from inorganic accoutrements [185].

Synthetic Polymers

Polyvinylidene Fluoride

In the midst of multitudinous piezoelectric polymers, PVDF is extensively delved, principally as a result of its large piezoelectricity, process capability, favorable chemical resistance, thermal stability, and bettered mechanical properties as juxtaposed to other piezoelectric polymers. PVDF may live no lower than five crystalline polymorphic phases, among which the β-phase exhibits the topmost piezoelectricity, which attains20 pC/N [186, 187]. PVDF macromolecules may assume different chain conformations and arrangement of CH2–CF2 molecular dipoles, giving rise to colorful net dipole moments [89-94]. An important electric moment in the PVDF monomer unit results from the buff electro-negativity of fluorine tittles as compared to hydrogen tittles. In the situation that polymer chains are arranged into chargers to form resemblant dipoles, the demitasse possesses a non-zero net dipole moment. Such a molecular arrangement is noticed in the β, γ, and δ phases, the initial one flaunting the strongest dipole moment, owing to the all-trans conformation. In the case of certain chain conformations: TGTG- and T3GT3G-, resemblant dipole moment arrangement, as in the δ and γ phases, independently, results to reduced opposition; in the situation of the identical conformations, anti-parallel chain dipole arrangement results to the zero net dipole moment as observed in the α and ε phases [188].

The piezoelectricity of PVDF is phase content reliant, which pivots on the processing parameters. Attaining a specific demitasse phase is doable using different tracks, containing melt or result crystallization, heat treatment at high pressure, mechanical delineation, or electrical poling. The actuality of polar phases is veritably necessary, specifically, owing to its bioelectrical impact of the stimulation of the nervous system, having eventuality for productive towel rejuvenescence [189, 190].  Regarding the most polar β-phase, it may be achieved, for case, by heat treatment at veritably high pressure from the α-phase, by oaring at a veritably high electrical field from the α-phase or δ-phase [191] or drawing from the γ-phase [192]. Concerning increase the content of polar phases, numerous procedures are described: melt-recrystallization [193], oaring in a high electric field [194], using of high pressure [195], mechanical stretching [196], and the objectification of nanoparticles, graphene, and nanowires [197].

The need to use PVDF in piezoelectric pulpits for towel engineering requires the operation of fabrication styles that permit having the correct morphology and high polar phase lading responsible for the high piezoelectricity [198]. Among the encouraging product styles to satisfy both hypotheticals is the electrospinning process. Multitudinous publications were committed to electrospinning of PVDF nanofibers from result [199], deciding the influence of processing conditions on the morphology and properties of nanofibers and the characteristics of nonwoven nanofiber [200]. The content of the β-phase in PVDF was estimated from the viewpoint of the applied voltage and revolution speed of the rotational collector. The collector revolution speed links to the mechanical deformation, which is studied to advance the conformation of the polar phase [201]. Liu et al. [202] formed nanofibers with colorful revolution spets of the collector 900, 1100, 1300, 1500, 1700 and 1900 rpm. XRD diffraction revealed a peak about 20.6–20.9 deg, which is combined to the β-phase, while the α-phase peaks dissolved. They attained piezoelectric PVDF filaments with anatomic periphery, indeed face morphology, and suitable β-phase at a haste of 1900 rpm. Current studies bolster the perspective that rising of the rotational speed of the collector prompts a greater content of the piezoelectric β-phase [203-205].

The hydrophobic character of PVDF is a complicated matter in neural towel engineering. In order to alleviate it, colorful studies have been performed. In order to ameliorate the hydrophilic in addition to the mechanical and electrical properties, PVDF has been changed by the addition of divergent nanostructures: nanoparticles [206-208], inorganic nanoparticles [209,210], nanotubes [211], and also by the objectification of colorful polymers like polyethylene glycol (PEG) [212] and polyvinyl alcohol (PVA) [213]. The addition of nanoparticles substantially metallic types enhances the chemical, physical, and optic properties [214], while diamond nanoparticles have no remarkable effect on neuroblastomacell morphology [215]. The addition of these nanostructures into a polymer piezoelectric altar can clearly impact the whim-whams towel. Also, revision of the face can enlarge the neuron length and number of synaptic associations [216, 217].

A study[218] estimated the piezoelectric pulpits’ prospective for stimulating in vitro neural isolation of mortal neural stem cells, thus displaying their felicitousnessin neural towel engineering. The authors in [218] prolonged the above examinations by applying mechanical vibration, while producing electric fields to impel the piezoelectric influence in piezo-polymers. The activation of the piezoelectric influence can be fulfilled by opting several sources of mechanical stimulation, similar as vibration plates, sound, and ultrasound (US) [219, 220]. Another study [221] estimated the effect of the piezoelectric PVDF substrate on buttressing neural isolation under dynamic stimulation. The issues demonstrated that the applied ultrasonic waves were acceptable to incite polarization in piezoelectric PVDF wastes and crowned in isolation of PC12 cells. Piezoelectric PVDF can control neuronal isolation and neurite bulge of mouse neuroblastoma cells [221].Electric fields have been proven to control the development and direction of neurons in vitro, since the electric field was produced through electrodes [222]. Certain examinations have been described favorable neural stimulation in multitudinous piezoelectric systems, substantially piezoelectric micro- and nano-filaments [223,224].

It was demonstrated that the long term operation of piezoelectric stimulation on neurons prompts the number, length, and branching of neural cells with regard to non-stimulation circumstances. No influences on neurite rejuvenescence were seen when vibrations were applied to non-piezoelectric accoutrements (e.g., mechanical stimulation of neurons) [225-227].

Poly-Vinylidene Fluoride-Trifluoroethylene

Amid the piezoelectric substances this copolymer displayed the topmost electroactive properties with a piezoelectric measure as high as 30 pC/N [228]. PVDF-TrFE forms the β-phase via copolymerization in the absence of mechanical extension or delineation [229]. In the case of fresh heat treatment, mechanical delineation, or electrical poling, it's doable to greater swell thecrystal clear natureand arrangement of the CF2 dipoles, therefore converting greater piezoelectricity in discrepancy to homopolymer PVDF, hinging on the TrFE content [230]. Electrospun PVDF-TrFE stringy pulpits demonstrated increased crystallinity and β-phase content in discrepancy to the forming grease paint material for neural and bone towel engineering [101-104]. PVDF-TrFE and barium titanate piezoelectric compound membrane has been described as a charge creator to stimulate bone rejuvenescence [106].

PVDF-TrFE piezoelectric stringy pulpits were employed to probe their effect on neural reconstruct. Several studies reported a positive effect of PVDF-TrFE pulpits on whim-whams cell development and isolation [231]. Lee et al., [114] produced a PVDF-TrFE piezoelectric electrospun altar with colorful exposures of the filaments, scattered and ordered. It was proved that the altar with ordered filaments gave the loftiest eventuality in neural towel engineering, substantially in neurite outgrowth of dorsal root ganglion neurons. It was noticed that PVDF-TrFE pulpits can stimulate the conformation of mature neural cells showing neuron-suchlike characteristics, while ordered filaments can support primary neuron extension and can guide the neurite outgrowth [232].

Whim-whams direct channels may be assembled using PVDF-TrFE for neural rejuvenescence [233]. In this exploration, paddled (negatively charged and appreciatively charged) and unpoled channels were employed. After the duration of four weeks, it was noticed that the appreciatively paddled channels spiked the number of regenerated jitters. In muscle rejuvenescence, the charge at the fringe of PVDF flicks controls the cell proliferation [234].Still, till date, studies with specific dynamic situations for piezoelectric PVDF-TrFE with mechanical or electrical stimulation have not been carried out.

Poly-3-Hydroxybutyrate-3-Hydroxyvalerate

Poly-3-hydroxybutyrate-3-hydroxyvalerate (PHBV) is a polyester with a reduced piezoelectric measuring 1.2 pC/N [235]. It is a thermoplastic made by colorful bacteria as an intracellular force of carbon and energy. PHBV is also biodegradable, biocompatible, and shows riotous mechanical properties, which permit using PHBV as an altar in biomedicine and as a biosensor [236, 237]. PHBV has an analogous piezoelectric eventuality to that of bone which can quicken bone growth and mending [238,239]; thus, it can be used in the form of a compound with the addition of hydroxyapatite for bone towel engineering. PHBV has been delved for neural towel engineering, as a supporter for neuronal cell growth and axon dendrite polarization [240]. In the form of electrospun ordered PHBV filaments, with the objectification of collagen, it can be applied as a substrate for whim-whams towel engineering [241-243].

Poly-L-Lactic Acid

Poly-L-lactic acid (PLLA) is a biodegradable and biocompatible polymer having a piezoelectric measuring -10 pC/N [223]. Fukada et al., illustrated that inculcation of PLLA can foster bone growth in the response of its piezoelectric polarization [93]. PLLA with a structure identical to native ECM may be employed as a biomaterial in multitudinous biomedical operations [245]. Ordered PLLA nanofibrous pulpits carpeted with graphene oxide stimulate neural cell growth [246]. Incipiently, the addition of iron oxide nanoparticles contributes to extending neurites besides electrospun PLLA microfibers [247, 248].

Natural Biopolymers

Natural polymers are receiving high attention in towel engineering due to their biodegradability and innocuous nature. Generally, various biological polymers show piezoelectricity. For instance, we illustrate certain polysaccharides and proteins having somewhat robust piezoelectricity.

Cellulose

Cellulose having a piezoelectric measuring 0.10 pC/N is extensively delved natural polymeric material. Cellulose is a direct homopolymer of glucose with great biocompatibility [249-255]. It is used in colorful shapes and forms similar as membrane bloodsuckers, microspheres, and non-woven, woven, or knitted fabrics. Cellulose has been studied in the towel engineering of bones [256,257],cartilage [258], for connective towel conformation [259], as a medicine delivery system [260], and as an altar for developing functional cardiac cell repairs in vitro [261]. One of the essential derivations of cellulose is methylcellulose (MC), showing in general respectable solubility in water, exceptionally at low temperatures, being reliant on the degree of methyl negotiation and the distribution of methoxy groups. As a whole, these data show that MC is accessible as a biocompatible injectable altar for the reconstruct of brain faults [262-264]. Gelatin carpeted nanoparticles held in cellulose acetate/PLA pulpits demonstrated advanced cell feasibility compared to uncoated pulpits, and they conducted as a whim-whams guidance channel for sciatic whim-whamsexcrescencies in vitro and in vivo [265], whereas a gelatin/chitosan/PEDOT mongrel altar bettered the neurite growth of PC12 cells and stimulated neuron-suchlike cell adhesion and proliferation [266].

Chitin and Chitosan

Chitin is a natural polysaccharide having a piezoelectric feature with a lowered piezoelectric measure gauging from 0.2-1.5 pC/N [267]. It is a natural element of the cuticles of crustaceans, insects, and mollusks. Thus it's hydrophilic and biocompatible chitin is used in biomedical operations, stimulating cell adhesion, proliferation, and isolation [268]. Chitosan is a biodegradable and biocompatible direct polysaccharide synthesized by partial deacetylation of chitin. It has been extensively studied for the product of pervious pulpits for cartilage towel engineering [269]. But, the poor mechanical properties of pulpits made from chitosan render its clinical operation delicate. A valid procedure to surmount chitosan’s limitations is to mix it with synthetic polymers [270-273]. Skop et al. designed biocompatible chitosan microspheres for the dispatch of neural stem cells and growth factors for CNS injuries [274]. Another platoon designed chitosan patches filled with the medicine piperine, recorded to have neuro protective prospect for Alzheimer’s complaint that explosively allocated peculiar spots of the brain [275]. Chitosan nanoparticles have also been produced for intranasal delivery of healing agents to the brain [276, 277]. Ordered PCL/chitosan filaments boost PC12 cells adhesion and development, perfecting neurite extension across the fiber direction [278]. PLGA/chitosan pulpits guided neuronal isolation for surface whim-whams rejuvenescence either in vitro or in vivo [279, 280].

Collagen

This is a natural piezoelectric material having a piezoelectric measure gauging from 0.2- 2.0 pC/N [281]. Study has been reported on the operation of collagen pulpits in bone remedial [282-285]. Also, collagen-calcium phosphate blends have been delved for cartilage towel engineering [286]. In the same tone, collagen-hydroxyapatite piezoelectric compound pulpits have been demonstrated to be applicable for cellular growth [287]. Collagen pulpits with the addition of chitosan have been anatomized in adipose towel rejuvenescence. Adipocytes were planted, and the in vitro cyto-compatibility and in vivo biocompatibility of pulpits was established experimentally [288]. An absorbing operation of collagen is entubulation, thus the use of magnetically ordered type I collagen gel, attained by exposing the forming collagen gel to a high strength glamorous field, as padding for collagen tubes. This approach was successful in small surface whim-whams lesions, enhancing whim-whams rejuvenescence remarkably in a 6 mm whim-whams band in mice [289] and directing neurite extension and Schwann cell irruption in vitro [290] and in vivo [291].

Conclusions and Future Perspectives

Currently, intelligent accoutrements have been of immense interest for scientists and croakers, due to the multitudinous openings to apply them as prospects for advancing the unborn generation of biomedical bias, flash implants, and medicine delivery medium. Taking into account smart pulpits for towel reconstruct and rejuvenescence, piezoelectric substances have recently been of specific interest as they can convey electrical encouragement in the absence of an outside power source. There is no gain saying that the bioelectric suggestions generated by piezoelectric pulpits can restore and reconstruct the napkins by established channels identical to the natural procedures passing within the native ECM. The combination of morphology in collaboration with the chemical, mechanical, and electrical properties of the pulpits is vital to the advance in towel rejuvenescence. Electrical charges are specifically consummate in neural towel engineering, in which electric pulses can promote neurite directional projection to enthrall gaps in nervous towel injuries. There is no fear that the point of view of the wider operation of piezo electric pulpits as smart accoutrements for neural towel rejuvenescence is of great significance, authorizing circumventing conventional (invasive) electrical stimulation. It was demonstrated not long ago in in-vitro situations that the distortion of the piezoelectric pulpits either through mechanical or ultrasound stimulation redounded to neurite extension and bettered cell adhesion and proliferation. Notwithstanding, one should be informed about that utmost of the ultramodern trials employing piezoelectric pulpits were carried out without similar stimulation, which doesn't affect to piezoelectricity and preceding electrical charges. In such a situation, the only charges that can be smart from the cellular point of view are supplemental charges owing to lasting polarization, as well as connected to temporary distortion created by the loss and outgrowth of the attached cells. Still, it is critical from the point of view of trials with piezoelectric pulpits to mimic the in vivo circumstances with internal macro- and micro-deformations through in vitro situations using mechanical (ultrasounds) anxiety, permitting achieving a real piezoelectric feedback. The coming issue in the field of piezoelectric pulpits is connected to the non-biodegradability of the polymers demonstrating the loftiest piezoelectric portions, which are PVDF and its copolymers. As a consequence, scrutiny should be concentrated on biodegradable piezoelectric polymers similar as PHB or PLLA. An immersing surrogate which should be delved in time to come is linked to the compound pulpits containing an electro-conductive polymer similar as PANi in addition to a piezoelectric polymer. It was demonstrated that the objectification of an electro-conductive polymer to the piezoelectric matrix crowned in an increase in piezoelectricity. This type of compound altar should be taken into consideration, when logic about biodegradable piezoelectric polymers with originally vastly moderate piezoelectricity.

References

[1] S.J. Lee, J.J. Yoo, and A. Atala. Biomaterials and tissue engineering. In: Clinical Regenerative Medicine in Urology. Singapore: Springer; 2018. p. 17–51.

[2] W.P. Mason. Piezoelectricity, its history and applications. The Journal of the Acoustical Society of America. 1981; 70(6):1561–6.

[3] R. Mindlin. Elasticity, piezoelectricity and crystal lattice dynamics. J Elast.1972; 2(4):217–82.

[4] R. Mould. Pierre Curie, 1859–1906. Curr Oncol. 2007; 14(2):74.

[5] T. Arinzeh, G. Collins, and Y.S. Lee. System and method for a piezoelectric scaffold for nerve growth and repair. In: Google Patents; 2016.

[6] M. Minary-Jolandan, and M.F. Yu. Nanoscale characterization of isolated individual type I collagen fibrils: polarization and piezoelectricity. Nanotechnology. 2009; 20(8):085706.

[7] T.L. Arinzeh, N. Weber, and M. Jaffe. Electrospun electroactive polymers for regenerative medicine applications. In: Google Patents; 2016.

[8] V.R. Shastri, C.E. Schmidt, R.S. Langer, and J.P. Vacanti. Neuronal stimulation using electrically conducting polymers. In: Google patents; 2000.

[9] C.A.L. Bassett. Biologic significance of piezoelectricity. Calcif Tissue Int. 1967; 1(1):252–72.

[10] C. Halperin, S. Mutchnik, A. Agronin, M. Molotskii, P. Urenski, M. Salai, and G. Rosenman. Piezoelectric effect in human bones studied in nanometer scale. Nano Lett. 2004:4(7):1253–6.

[11] B. Miara, E. Rohan, M. Zidi, and B. Labat. Piezomaterials for bone regeneration design-homogenization approach. Journal of the Mechanics and Physics of Solids. 2005; 53(11):2529-56.

[12] F.J. O’Brien. Biomaterials and scaffolds for tissue engineering. Mater. Today 2011, 14, 88–95.

[13] C. Ribeiro, D.M. Correia, S. Ribeiro, M.M. Fernandes, and S. Lanceros-Mendez. Piezo- and  magnetoelectric polymers as biomaterials for novel tissue engineering strategies. MRS Adv. 2018, 3, 1671–1676.

[14] S. Ribeiro, A.C. Gomes, I. Etxebarria, S. Lanceros-Mendez, and C. Ribeiro,  Electroactive biomaterial surface engineering effects on muscle cells differentiation. Mater.Sci. Eng. C Mater. Biol. Appl. 2018, 92, 868–874.

[15] J. Fraden. Handbook of Modern Sensors: Physics, Designs, and Applications; Springer Science & Business Media: Berlin/Heidelberg,Germany, 2004.

[16] C. Ribeiro, V. Sencadas, D.M. Correia, and S. Lanceros-Mendez. Piezoelectric polymers as biomaterials for tissue engineering applications. Colloids Surf. B Biointerfaces 2015, 136, 46–55.

[17] L.C. Fernandes, D.M. Correia, C. García-Astrain, N. Pereira, M. Tariq, J.M.S.S. Esperança, and S. Lanceros-Méndez. Ionic-liquid-based printable materials for thermochromic and thermoresistive applications. ACS Appl. Mater. Interfaces 2019, 11, 20316–20324.

[18] J. Jacob, N. More, K. Kalia, and G. Kapusetti. Piezoelectric smart biomaterials for bone and cartilage tissue engineering. Inflamm. Regen. 2018, 38, 2.

[19] C. Ribeiro, J. Pärssinen, V. Sencadas, V. Correia, S. Miettinen, V.P. Hytönen, and S. Lanceros-Méndez. Dynamic piezoelectric stimulation enhances osteogenic differentiation of human adipose stem cells. J. Biomed. Mater. Res.-Part A2015, 103, 2172–2175.

[20] S.W. Blume, and J.R. Curtis, Medical costs of osteoporosis in the elderly medicare population, Osteoporos. Int. 22 (2011) 1835–1844.

[21] E. Hernlund, A. Svedbom, M. Ivergård, J. Compston, C. Cooper, J. Stenmark, E.V. McCloskey, B. Jonsson, and J.A. Kanis, Osteoporosis in the European Union: medical management, Epidemiol. Econ.Burd. 8 (2013) 1–115.

[22] M.U.D.o.H. Office of the Surgeon General %J A Report of the Surgeon General.Rockville, O.o.t.S.G. Human Services, Bone health and osteoporosis, (2004) 68–87.

[23] T.D. Rachner, S. Khosla, and L.C. Hofbauer, Osteoporosis: now and the future, Lancet 377 (2011) 1276–1287.

[24] A.R. Amini, C.T. Laurencin, and S.P. Nukavarapu, Bone tissue engineering: recent advances and challenges, Crit. Rev. Biomed. Eng. 40 (2012) 363–408.

[25] G. Battafarano, M. Rossi, V. De Martino, F. Marampon, L. Borro, A. Secinaro, and A.D. Fattore, Strategies for bone regeneration: from graft to tissue engineering, Int. J. Mol. Sci. 22 (2021) 1–22.

[26] C. Ribeiro, V. Sencadas, D.M. Correia, and S. Lanceros-M´endez, Piezoelectric polymers as biomaterials for tissue engineering applications, Colloids Surf. B: Biointerfaces 136 (2015) 46–55.

[27] M.H. Shamos, L.S. Lavine, and M.I. Shamos, Piezoelectric effect in bone, Nature 197 (1963) 81.

[28] M.M. Fernandes, D.M. Correia, C. Ribeiro, N. Castro, V. Correia, and S. Lanceros-Mendez, Bioinspired three-dimensional magnetoactive scaffolds for bone tissue engineering, ACS Appl. Mater. Interfaces 11 (2019) 45265–45275.

[29] C. Ribeiro, J. Parssinen, V. Sencadas, V. Correia, S. Miettinen, V.P. Hytonen, and S. Lanceros-M´endez, Dynamic piezoelectric stimulation enhances osteogenic differentiation of human adipose stem cells, J. Biomed. Mater. Res. - Part A 103 (2015) 2172–2175.

[30] C. Ribeiro, V. Correia, P. Martins, F.M. Gama, and S. Lanceros-Mendez, Proving the suitability of magnetoelectric stimuli for tissue engineering applications, Colloids Surf. B: Biointerfaces 140 (2016) 430–436.

[31] P.K. Szewczyk, S. Metwally, Z.J. Krysiak, L. Kaniuk, J.E. Karbowniczek, and U. Stachewicz, Enhanced osteoblasts adhesion and collagen formation on biomimetic polyvinylidene fluoride (PVDF) films for bone regeneration, Biomed. Mater.14 (2019).

[32] P.K. Szewczyk, S. Metwally, J.E. Karbowniczek, M.M. Marzec, E. Stodolak-Zych, A. Gruszczynski, A. Bernasik, and U. Stachewicz, Surface-potential-controlled cell proliferation and collagen mineralization on electrospun polyvinylidene fluoride (PVDF) fiber scaffolds for bone regeneration, ACS Biomater. Sci. Eng. 5 (2019) 582–593.

[33] A. Reizabal, R. Brito-Pereira, M.M. Fernandes, N. Castro, V. Correia, C. Ribeiro, C.M. Costa, L. Perez, J.L. Vilas, and S. Lanceros-Mandendez, Silk fibroin magnetoactive nanocomposite films and membranes for dynamic bone tissue engineering strategies, Materialia 12 (2020), 100709.

[34] R. Langer, and J.P. Vacanti, Tissue Engineering, Science 260 (5110) (1993) 920–926, https://doi.org/10.1126/science.8493529.

[35] S.M. Greising, B.T. Corona, C. McGann, J.K. Frankum, and G.L. Warren, Therapeutic approaches for volumetric muscle loss injury: a systematic review and Meta- Analysis, Tissue Eng. Part B Rev. 25 (6) (2019) 510–525, https://doi.org/10.1089/ ten.TEB.2019.0207.

[36] S. Ribeiro, A.C. Gomes, I. Etxebarria, S. Lanceros-Mendez, and C. Ribeiro, Electroactive biomaterial surface engineering effects on muscle cells differentiation, Mater. Sci. Eng., C 92 (2018) 868–874, https://doi.org/10.1016/j.msec.2018.07.044.

[37] S. Jana, S.K.L. Levengood, and M. Zhang.  Anisotropic materials for skeletal-muscle-tissue engineering, Adv. Mater. (Deerfield Beach Fla.) 28 (48) (2016) 10588–10612, https://doi.org/10.1002/adma.201600240.

[38] S. Ribeiro, T. Ribeiro, C. Ribeiro, D.M. Correia, J.P.S. Farinha, A.C. Gomes, C. Baleizao, and S. Lanceros-Mendez, Multifunctional platform based on electroactive polymers and silica nanoparticles for tissue engineering applications, Nanomaterials (Basel, Switzerland) 8 (11) (2018) 933, https://doi.org/10.3390/ nano8110933.

[39] N. Shehata, M.A. Abdelkareem, E.T. Sayed, D.E. Egirani, and A.W. Opukumo, Smart Materials: The next generation, in: reference module in materials science and Materials Engineering, 2021, Elsevier. https://doi.org/10.1016/b978-0-12- 815732-9.00062-0.

[40] C. Ribeiro, C.M. Costa, D.M. Correia, J. Nunes-Pereira, J. Oliveira, P. Martins, R. Gonçalves, V.F. Cardoso, and S. Lanceros-Mendez, Electroactive poly(vinylidene fluoride)-based structures for advanced applications, Nat. Protoc. 13 (4) (2018) 681–704, https://doi.org/10.1038/nprot.2017.157.

[41] B. Hermenegildo, C. Ribeiro, L. Perez-´Alvarez, J.L. Vilas, D.A. Learmonth, R.A. Sousa, P. Martins, and S.  Lanceros-Mendez, Hydrogel-based magnetoelectric microenvironments for tissue stimulation, Colloids Surf., B 181 (2019) 1041–1047, https://doi.org/10.1016/j.colsurfb.2019.06.023.

[42] P. Hitscherich, A. Aphale, R. Gordan, R. Whitaker, P. Singh, L.H. Xie, P. Patra, and E. J. Lee, Electroactive graphene composite scaffolds for cardiac tissue engineering, J. Biomed. Mater. Res. Part A 106 (11) (2018) 2923–2933, https://doi.org/ 10.1002/jbm.a.36481.

[43] P. Gentile, V. Chiono, I. Carmagnola, and P.V. Hatton, An overview of poly(lactic-co-glycolic) acid (PLGA)-based biomaterials for bone tissue engineering, Int. J. Mol. Sci. 15 (3) (2014) 3640–3659, https://doi.org/10.3390/ijms15033640.

[44] K.K. Chereddy, G. Vandermeulen, and V. Preat, PLGA based drug delivery systems: Promising carriers for wound healing activity, Wound Repair Regen. 24 (2) (2016) 223–236, https://doi.org/10.1111/wrr.12404.

[45] C. Martins, F. Sousa, F. Araújo, and B. Sarmento, Functionalizing PLGA and PLGA derivatives for drug delivery and tissue gegeneration applications, Adv. Healthcare Mater. 7 (1) (2017) 1701035, https://doi.org/10.1002/ adhm.201701035.

[46] J.M. Lü, X. Wang, C. Marin-Muller, H. Wang, P.H. Lin, Q. Yao, and C. Chen, Current advances in research and clinical applications of PLGA-based nanotechnology, Expert Rev. Mole. Diagn.9 (4) (2009) 325–341, https://doi.org/10.1586/ erm.09.15.

[47] Z. He, F. Rault, M. Lewandowski, E. Mohsenzadeh, and F. Salaün, Electrospun PVDF nanofibers for piezoelectric applications: a review of the influence of electrospinning parameters on the β-Phase and crystallinity enhancement, Polymers 13 (2) (2021) 174, https://doi.org/10.3390/polym13020174.

[48] J.C. Middleton, and A.J. Tipton, Synthetic biodegradable polymers as orthopedic devices, Biomaterials 21 (23) (2000) 2335–2346, https://doi.org/10.1016/s0142- 9612(00)00101-0.

[49] Y. Wang, Y. Miao, G. Li, M. Su, X. Chen, H. Zhang, Y. Zhang, W. Jiao, Y. He, J. Yi, X. Liu, and H. Fan, Engineering ferrite nanoparticles with enhanced magnetic response for advanced biomedical applications, Mater. Today Adv. 8 (2020) 100119, https://doi.org/10.1016/j.mtadv.2020.100119.

[50] Y. Shen, B.O. Jiang, and Y.I. Xing, Recent advances in the application of magnetic Fe3O4 nanomaterials for the removal of emerging contaminants, Environ. Sci. Pollut. Res. 28 (7) (2021) 7599–7620.

[51] Q. Li, C.W. Kartikowati, S. Horie, T. Ogi, T. Iwaki, and K. Okuyama, Correlation between particle size/domain structure and magnetic properties of highly crystalline Fe(3)O(4) nanoparticles, Sci. Rep. 7 (1) (2017) 9894, https://doi.org/ 10.1038/s41598-017-09897-5.

[52] T.A. Quinn, Cardiac mechano-electric coupling: a role in regulating normal function of the heart? Cardiovasc.Res. 108 (1) (2015) 1–3, https://doi.org/ 10.1093/cvr/cvv203.

[53] World Health Organization, Cardiovascular diseases. https://www.who.int/west ernpacific/health-topics/cardiovascular-diseases, 2022.

[54] M. Mazzola, and E.D. Pasquale, toward cardiac regeneration: combination of pluripotent stem cell-based therapies and bioengineering strategies, Front. Bioeng.Biotechnol. 8 (2020) 455, https://doi.org/10.3389/fbioe.2020.00455.

[55] Y. Huang, T. Wang, M.E.U. Lopez, M. Hirano, A. Hasan, and S.R. Shin, Recent advancements of human iPSC derived cardiomyocytes in drug screening and tissue regeneration, Microphysiol. Syst. 4 (2020), https://doi.org/10.21037/mps- 20-3.

[56] T.C. Suh, A.Y. Amanah, and J.M. Gluck, Electrospun scaffolds and induced pluripotent stem cell-derived cardiomyocytes for cardiac tissue engineering applications, Bioengineering 7 (3) (2020), https://doi.org/10.3390/ bioengineering7030105.

[57] A. Mathew, R. Augustine, N. Kalarikal, and S. Thomas, in: Tissue engineering: principles, recent trends and the future: state of the art and recent trends, 2016, pp. 31–82, https://doi.org/10.1201/b19867-3.

[58] N.F. Huang, Big bottlenecks in cardiovascular tissue engineering, Commun. Biol. 1 (1) (2018), https://doi.org/10.1038/s42003-018-0202-8.

[59] A. Khademhosseini, and R. Langer, A decade of progress in tissue engineering, Nat. Protoc. 11 (10) (2016) 1775–1781, https://doi.org/10.1038/nprot.2016.123.

[60] P.S. Alberte, J. Vaithilingam, J.C. Moore, R.D. Wildman, C.J. Tuck, M. R. Alexander, R.J.M. Hague, and F.J. Rawson, Development of conductive gelatine-methacrylate inks for two-photon polymerisation, Polymers 13 (7) (2021), https://doi.org/10.3390/polym13071038.

[61] J. Vaithilingam, P.S. Alberte, S. Campora, G.A. Rance, L. Jiang, J. Thorpe, L. Burroughs, C.J. Tuck, C. Denning, R.D. Wildman, R.J.M. Hague, M. R. Alexander, and F.J. Rawson, Multifunctional bioinstructive 3D architectures to modulate cellular behavior, Adv. Funct. Mater.29 (38) (2019), https://doi.org/ 10.1002/adfm.201902016.

[62] K. Kapat, Q.T.H. Shubhra, M. Zhou, and S. Leeuwenburgh, Piezoelectric nano-biomaterials for biomedicine and tissue regeneration, Adv. Funct.Mater.30 (44) (2020), https://doi.org/10.1002/adfm.201909045.

[63]K. Kapat, Q.T.H. Shubhra, M. Zhou, and S. Leeuwenburgh, Piezoelectric nanobiomaterials for biomedicine and tissue regeneration, Adv. Funct. Mater.30 (2020) 1909045.

[64]R.A. Surmenev, T. Orlova, R.V. Chernozem, A.A. Ivanova, A. Bartasyte, S. Mathur, and M.A. Surmeneva, Hybrid lead-free polymer-based nanocomposites with improved piezoelectric response for biomedical energy-harvesting applications: a review, Nano Energy 62 (2019) 475–506.

[65]B.W. Walker, R.P. Lara, C.H. Yu, E.S. Sani, W. Kimball, S. Joyce, and N. Annabi, Engineering a naturally-derived adhesive and conductive cardiopatch, Biomaterials 207 (2019) 89–101.

[66]Q. Wang, M. Wu, X. Xu, C. Ding, J. Luo, and J. Li, Direct current stimulation for improved osteogenesis of MC3T3 cells using mineralized conductive polyaniline, ACS Biomater. Sci. Eng. 7 (2021) 852–861.

[67]B. Katz, and R. Miledi, Release of acetylcholine from a nerve terminal by electric pulses of variable strength and duration, Nature 207 (1965) 1097–1098.

[68]S. Ribeiro, C. Puckert, C. Ribeiro, A.C. Gomes, M.J. Higgins, and S. Lanceros-Mendez, Surface charge-mediated cell-surface interaction on piezoelectric materials, ACS Appl. Mater. Interfaces 12 (2020) 191–199.

[69]S. Farzamfar, M. Salehi, S.M. Tavangar, J. Verdi, K. Mansouri, A. Ai, Z.V. Malekshahi, and J. Ai, A novel polycaprolactone/carbon nanofiber composite as a conductive neural guidance channel: an in vitro and in vivo study, Prog. Biomater. 8 (2019) 239–248.

[70]F. Gisbert Roca, J. Mas Estelles, M. Monleon Pradas, and C. Martinez-Ramos, Axonal extension from dorsal root ganglia on fibrillar and highly aligned poly(lactic acid)-polypyrrole substrates obtained by two different techniques: electrospun nanofibres and extruded microfibres, Int. J. Biol. Macromol. 163 (2020) 1959–1969.

[71]A. Wang, Z. Liu, M. Hu, C. Wang, X. Zhang, B. Shi, Y. Fan, Y. Cui, Z. Li, and K. Ren, Piezoelectric nanofibrous scaffolds as in vivo energy harvesters for modifying fibroblast alignment and proliferation in wound healing, Nano Energy 43 (2018) 63–71.

[72]D. Kim, S.A. Han, J.H. Kim, J.H. Lee, S.W. Kim, and S.W. Lee, Biomolecular piezoelectric materials: from amino acids to living tissues, Adv. Mater. 32 (2020) 1906989.

[73]M. Seiti, P. Ginestra, R.M. Ferraro, E. Ceretti, and E. Ferraris, Nebulized jet-based printing of bio-electrical scaffolds for neural tissue engineering: a feasibility study, Biofabrication 12 (2020) 025024.

[74]L. Wang, Y. Wu, T. Hu, P.X. Ma, and B. Guo, Aligned conductive core-shell biomimetic scaffolds based on nanofiber yarns/hydrogel for enhanced 3D neurite outgrowth alignment and elongation, Acta Biomater. 96 (2019) 175–187.

[75]J. Ren, Q. Xu, X. Chen, W. Li, K. Guo, Y. Zhao, Q. Wang, Z. Zhang, H. Peng, Y.G. Li, Adv. Mater. 29 (2017).

[76]N. Adadi, M. Yadid, I. Gal, M. Asulin, R. Feiner, R. Edri, and T. Dvir, Electrospun fibrous PVDF-TrFe scaffolds for cardiac tissue engineering, differentiation, and maturation, Adv. Mater. Technol. 5 (2020) 1900820.

[77]K. Roshanbinfar, L. Vogt, F. Ruther, J.A. Roether, A.R. Boccaccini, F.B. Engel, Adv. Funct. Mater. 30 (2019).

[78]H. Stone, S. Lin, and K. Mequanint, Preparation and characterization of electrospun rGO-poly (ester amide) conductive scaffolds, Mater. Sci. Eng. C Mater. Biol. Appl. 98 (2019) 324–332.

[79]G. Zhao, X. Zhang, B. Li, G. Huang, F. Xu, and X. Zhang, Solvent-free fabrication of carbon nanotube/silk fibroin electrospun matrices for enhancing cardiomyocyte functionalities, ACS Biomater. Sci. Eng. 6 (2020) 1630–1640.

[80]A.A. Marino, and R.O. Becker, Piezoelectricity in hydrated frozen bone and tendon, Nature 253 (1975) 627–628.

[81]H. Cui, Y. Liu, M. Deng, X. Pang, P. Zhang, X. Wang, X. Chen, and Y. Wei, Synthesis of biodegradable and electroactive tetraaniline grafted poly (ester amide) copolymers for bone tissue engineering, Biomacromolecules 13 (2012) 2881–2889.

[82]B. Maharjan, V.K. Kaliannagounder, S.R. Jang, G.P. Awasthi, D.P. Bhattarai, G. Choukrani, C.H. Park, and C.S. Kim, In-situ polymerized polypyrrole nanoparticles immobilized poly (ε-caprolactone) electrospun conductive scaffolds for bone tissue engineering, Mater. Sci. Eng. C Mater.Biol. Appl. 114 (2020) 111056.

[83]H. Nekounam, Z. Allahyari, S. Gholizadeh, E. Mirzaei, M.A. Shokrgozar, and R. Faridi-Majidi, Simple and robust fabrication and characterization of conductive carbonized nanofibers loaded with gold nanoparticles for bone tissue engineering applications, Mater. Sci. Eng. C Mater.Biol. Appl. 117 (2020) 111226.

[84]T. Fu, L. Jiang, Y. Peng, Z. Li, S. Liu, J. Lu, and F. Zhang, Electrical muscle stimulation accelerates functional recovery after nerve injury, Neuroscience 426 (2020) 179–188.

[85]H.Y. Gong, J. Park, W. Kim, J. Kim, J.Y. Lee, and W.G. Koh, A novel conductive and micropatterned PEG-based hydrogel enabling the topographical and electrical stimulation of myoblasts, ACS Appl. Mater. Interfaces 11 (2019) 47695–47706.

[86]K.H. Nakayama, M. Shayan, and N.F. Huang, Engineering biomimetic materials for skeletal muscle repair and regeneration, Adv. Healthc.Mater.8 (2019) 1801168.

[87]M.J. Mulroy, D.W. Altmann, T.F. Weiss, and W.T. Peake, Intracellular electric responses to sound in a vertebrate cochlea, Nature 249 (1974) 482–485.

[88]S. Du, N. Zhou, Y. Gao, G. Xie, H. Du, H. Jiang, L. Zhang, J. Tao, and J. Zhu, Bioinspired hybrid patches with self-adhesive hydrogel and piezoelectric nanogenerator for promoting skin wound healing, Nano Res. 13 (2020) 2525–2533.

[89]P. Moutsatsou, K. Coopman, and S. Georgiadou, Biocompatibility assessment of conducting PANI/chitosan nanofibers for wound healing applications, Polymers 9 (2017).

[90]J. Xue, J. Xie, W. Liu, and Y. Xia, Electrospun nanofibers: new concepts, materials, and applications, Acc. Chem. Res. 50 (2017) 1976–1987.

[91]L. Mohammadi Amirabad, M. Massumi, M. Shamsara, I. Shabani, A. Amari, M. Mossahebi Mohammadi, S. Hosseinzadeh, S. Vakilian, S.K. Steinbach, M.R. Khorramizadeh, M. Soleimani, and J. Barzin, Enhanced cardiac differentiation of human cardiovascular disease patient-specific induced pluripotent stem cells by applying unidirectional electrical pulses using aligned electroactive nanofibrous scaffolds, ACS Appl. Mater. Interfaces 9 (2017) 6849–6864.

[92]C. Zhang, M.H. Hsieh, S.Y. Wu, S.H. Li, J. Wu, S.M. Liu, H.J. Wei, R.D. Weisel, H.W. Sung, and R.K. Li, A self-doping conductive polymer hydrogel that can restore electrical impulse propagation at myocardial infarct to prevent cardiac arrhythmia and preserve ventricular function, Biomaterials 231 (2020) 119672.

[93]G. Thrivikraman, P.S. Lee, R. Hess, V. Haenchen, B. Basu, and D. Scharnweber, Interplay of substrate conductivity, cellular microenvironment, and pulsatile electrical stimulation toward osteogenesis of human mesenchymal stem cells in vitro, ACS Appl. Mater. Interfaces 7 (2015) 23015–23028.

[94]S. Ostrovidov, M. Ebrahimi, H. Bae, H.K. Nguyen, S. Salehi, S.B. Kim, A. Kumatani, T. Matsue, X. Shi, K. Nakajima, S. Hidema, M. Osanai, and A. Khademhosseini, Gelatin-polyaniline composite nanofibers enhanced excitation-contraction coupling system maturation in myotubes, ACS Appl. Mater. Interfaces 9 (2017) 42444–42458.

[95]S. Xu, Y. Qin, C. Xu, Y. Wei, R. Yang, and Z.L. Wang, Self-powered nanowire devices, Nat. Nanotechnol. 5 (2010) 366–373.

[96]Z.L. Wang, towards self-powered nanosystems: from nanogenerators to nanopiezotronics, Adv. Funct. Mater. 18 (2008) 3553–3567.

[97]X. Wang, J. Song, L. Jin, and L.W. Zhong, Direct-current nanogenerator driven by ultrasonic waves, Science 316 (2007) 102–105.

[98]Y. Zhang, Z. Zheng, M. Yu, C. Hsu, E.A. Berthiaume, H. Pan, X. Zhang, A.Z. Stieg, B. Wu, H. Wang, K. Ting, and C. Soo, Using an engineered galvanic redox system to generate positive surface potentials that promote osteogenic functions, ACS Appl. Mater. Interfaces 10 (2018) 15449–15460.

[99]X. Zhang, X. Cui, D. Wang, S. Wang, Z. Liu, G. Zhao, Y. Zhang, Z. Li, Z.L. Wang, and L. Li, Soft acoustic metamaterials: bubble architectures for locally resonant acoustic metamaterials (Adv. Funct. Mater.51/2019), Adv. Funct.Mater.29 (2019) 1970346.

[100]R.V. Chernozem, M.A. Surmeneva, S.N. Shkarina, K. Loza, M. Epple, M. Ulbricht, A. Cecilia, B. Krause, T. Baumbach, A.A. Abalymov, B.V. Parakhonskiy, A.G. Skirtach, and R.A. Surmenev, Piezoelectric 3-D fibrous poly(3-hydroxybutyrate)-based scaffolds ultrasound-mineralized with calcium carbonate for bone tissue engineering: inorganic phase formation, osteoblast cell adhesion, and proliferation, ACS Appl. Mater. Interfaces 11 (2019) 19522–19533.

[101]A. Marino, G.G. Genchi, V. Mattoli, and G. Ciofani, Piezoelectric nanotransducers: the future of neural stimulation, Nano Today 14 (2017) 9–12.

[102]A. Marino, J. Barsotti, G. de Vito, C. Filippeschi, B. Mazzolai, V. Piazza, M. Labardi, V. Mattoli, and G. Ciofani, Two-photon lithography of 3D nanocomposite piezoelectric scaffolds for cell stimulation, ACS Appl. Mater. Interfaces 7 (2015) 25574–25579.

[103]L. Jiang, Y. Yang, R. Chen, G. Lu, R. Li, J. Xing, K.K. Shung, M.S. Humayun, J. Zhu, Y. Chen, Q. Zhou, Adv. Funct. Mater.29 (2019).

[104]D.K. Piech, B.C. Johnson, K. Shen, M.M. Ghanbari, K.Y. Li, R.M. Neely, J.E. Kay, J.M. Carmena, M.M. Maharbiz, and R. Muller, A wireless millimetre-scale implantable neural stimulator with ultrasonically powered bidirectional communication, Nat. Biomed. Eng. 4 (2020) 207–222.

[105]A.C. Wang, M. Hu, L.W. Zhou, and X.Y. Qiang, Phenanthroline-derivative functionalized carbon dots for highly selective and sensitive detection of Cu2+ and S2− and imaging inside live cells, Nanomaterials 8 (2018) 1071.

[106]P.J. Gouveia, S. Rosa, L. Ricotti, B. Abecasis, H.V. Almeida, L. Monteiro, J. Nunes, F.S. Carvalho, M. Serra, S. Luchkin, A.L. Kholkin, P.M. Alves, P.J. Oliveira, R. Carvalho, A. Menciassi, R.P. das Neves, and L.S. Ferreira, Flexible nanofilms coated with aligned piezoelectric microfibers preserve the contractility of cardiomyocytes, Biomaterials 139 (2017) 213–228.

[107]Y. Zou, J. Qin, Z. Huang, G. Yin, X. Pu, and D. He, Fabrication of aligned conducting PPy-PLLA fiber films and their electrically controlled guidance and orientation for neurites, ACS Appl. Mater. Interfaces 8 (2016) 12576–12582.

[108]J. Wang, Y. Cheng, L. Chen, T. Zhu, K. Ye, C. Jia, H. Wang, M. Zhu, C. Fan, and X. Mo, In vitro and in vivo studies of electroactive reduced graphene oxide-modified nanofiber scaffolds for peripheral nerve regeneration, Acta Biomater. 84 (2019) 98–113.

[109]R.F. Valentini, T.G. Vargo, J.A. Gardella, and P. Aebischer, Electrically charged polymeric substrates enhance nerve fibre outgrowth in vitro, Biomaterials 13 (1992) 183–190.

[110]E.G. Fine, R.F. Valentini, R. Bellamkonda, and P. Aebischer, Improved nerve regeneration through piezoelectric vinylidenefluoride-trifluoroethylene copolymer guidance channels, Biomaterials 12 (1991) 775–780.

[111]J.I. Kim, T.I. Hwang, J.C. Lee, C.H. Park,and  C.S. Kim, Springer Proceedings in Physics: Proceedings of the International Conference on “Physics and Mechanics of New Materials and Their Applications”, PHENMA 2018, Adv. Funct. Mater.30 (2019).

[112]Raynald, B. Shu, X.B. Liu, J.F. Zhou, H. Huang, J.Y. Wang, X.D. Sun, C. Qin, and Y.H. An, Polypyrrole/polylactic acid nanofibrous scaffold cotransplanted with bone marrow stromal cells promotes the functional recovery of spinal cord injury in rats, CNS Neurosci. Ther. 25 (2019) 951–964.

[113]N. Grossman, D. Bono, N. Dedic, S.B. Kodandaramaiah, A. Rudenko, H.J. Suk, A.M. Cassara, E. Neufeld, N. Kuster, L.H. Tsai, A. Pascual-Leone, and E.S. Boyden, Noninvasive deep brain stimulation via temporally interfering electric fields, Cell 169 (2017) 1029–1041 e1016.

[114]K.M. Kim, S.Y. Kim, and G.T. Palmore, Axon outgrowth of rat embryonic hippocampal neurons in the presence of an electric field, ACS Chem. Neurosci. 7 (2016) 1325–1330.

[115] D. M. Correia, R. Golcalves, C. Ribeiro, V. Sencadas, G. L. Botelho, J. L. Gomez-Ribelles and s.lanceros-mendez, RSC Adv 4 , 33013-33021 (2014).

[116] D. M. Correia, V. Sencadas, C. Ribeiro, P. M. Martins, P. Martins, F. M. Gama, G. Botelho and S.Lanceros-Méndez, J Colloid Interf Sci 476, 79-86 (2016).

[117] V. Sencadas, R. Gregorio and S. Lanceros-Méndez, J Macromolec Sci B 48 (3), 514-525 (2009).

[118] S. J. Hong, H. S. Yu and H. W. Kim, Acta Biomaterialia 5 (5), 1725-1731 (2009).

[119] V. Sencadas, S. Lanceros-Méndez and J. F. Mano, Thermochimica Acta 424 (1–2), 201-207 (2004).

[120] Z. H. Liu, C. T. Pan, L. W. Lin and H. W. Lai, Sens Actuat A 193 (0), 13-24 (2013).

[121] H. Na, X. Liu, J. Li, Y. Zhao, C. Zhao and X. Yuan, Polymer 50 (26), 6340-6349 (2009).

[122] C. Ribeiro, V. Sencadas, J. L. G. Ribelles and S. Lanceros-Méndez, Soft Mater 8 (3), 274-287 (2010).

[123] D. M. Correia, C. Ribeiro, V. Sencadas, L. Vikingsson, M. Oliver Gasch, J. L. Gómez Ribelles, G.Botelho and S. Lanceros-Méndez, Mater Design 92, 674-681 (2016).

[124] C. Ribeiro, V. Correia, P. Martins, F. M. Gama and S. Lanceros-Mendez, Colloids Surf B 140, 430-436 (2016).

[125] M. N. T.-M. R. Sobreiro-Almeida, E. O. Carvalho, L. Cordón, S. Doria, L. Senent, D. M. Correia, C.Ribeiro, S. Lanceros-Méndez, R. Sabater i Serra, J. L. Gomez Ribelles and A. Sempere, Intern J Molec Sci 18 (11), 2391 (2017).

[126] R. Gonçalves, P. Martins, D. M. Correia, V. Sencadas, J. L. Vilas, L. M. León, G. Botelho and S.Lanceros-Méndez, RSC Adv 5 (45), 35852-35857 (2015).

[127] M. Zamani, M. P. Prabhakaran and S. Ramakrishna, Int J Nanomedicine 8, 2997-3017 (2013).

[128] D. M. Correia, V. Sencadas, C. Ribeiro, P. M. Martins, P. Martins, F. M. Gama, G. Botelho and S.Lanceros-Méndez, J Colloid Interf Sci 476 (Supplement C), 79-86 (2016).

[129] M. P. Prabhakaran, L. Ghasemi-Mobarakeh, G. R. Jin and S. Ramakrishna, J. Biosci.Bioeng.112 (5), 501-507 (2011).

[130] C. Ribeiro, D. M. Correia, S. Ribeiro, V. Sencadas, G. Botelho and S. Lanceros-Méndez, Eng LifeSci 15 (4), 351-356 (2015).

[131] C. Ribeiro, V. Sencadas, C. M. Costa, J. L. Gómez Ribelles and S. Lanceros-Méndez, Sci TechnolAdv Mater 12 (1) (2011).

[132] R. Gonçalves, P. Martins, X. Moya, M. Ghidini, V. Sencadas, G. Botelho, N. D. Mathur and S. Lanceros-Mendez, Nanoscale 7 (17), 8058-8061 (2015).

[133] J. Zheng, A.He, J. Li and C. C. Han, Macromolecular Rapid Commun 28 (22), 2159-2162 (2007).

[134] L. Budyanto, Y. Q. Goh and C. P. Ooi, J Mater Sci: Mater Medicine 20 (1), 105-111 (2009).

[135] A. H. Rajabi, M. Jaffe and T. L. Arinzeh, Acta Biomater.24, 12-23 (2015).

[136] M. T. Rodrigues, M. E. Gomes, J. F. Mano and R. L. Reis, in Advanced Materials Forum Iv, edited by A. T. Marques, A. F. Silva, A. P. M. Baptista, C. Sa, F. Alves, L. F. Malheiros and M. Vieira (Trans Tech Publications Ltd, Stafa-Zurich, 2008), Vol. 587-588, pp. 72-76.

[137]J. Parssinen, H. Hammaren, R. Rahikainen, V. Sencadas, C. Ribeiro, S. Vanhatupa, S. Miettinen, S. Lanceros-Mendez and V. P. Hytonen, J. Biomed. Mater.Res.A 103 (3), 919-928 (2015).

[138] C. Ribeiro, J. Parssinen, V. Sencadas, V. Correia, S. Miettinen, V. P. Hytonen and S. Lanceros-Mendez, J. Biomed. Mater.Res.A 103 (6), 2172-2175 (2015).

[139] C. Ribeiro, S. Moreira, V. Correia, V. Sencadas, J. G. Rocha, F. M. Gama, J. L. G. Ribelles and S.Lanceros-Mendez, RSC Adv. 2 (30), 11504-11509 (2012).

[140] C. Ribeiro, D. M. Correia, I. Rodrigues, L. Guardao, S. Guimaraes, R. Soares and S. Lanceros-Mendez, Mater Letters 209, 118-121 (2017).

[141] A. Ignatius, H. Blessing, A. Liedert, C. Schmidt, C. Neidlinger-Wilke, D. Kaspar, B. Friemert and L.Claes, Biomaterials 26 (3), 311-318 (2005).

[142] R. F. Valentini, T. G. Vargo, J. A. Gardella and P. Aebischer, Biomaterials 13 (3), 183-190 (1992).

[143] H. F. Guo, Z. S. Li, S. W. Dong, W. J. Chen, L. Deng, Y. F. Wang and D. J. Ying, Colloids Surf B96, 29-36 (2012).

[144] P. M. Martins, S. Ribeiro, C. Ribeiro, V. Sencadas, A. C. Gomes, F. M. Gama and S. Lanceros-Méndez, RSC Adv 3 (39), 17938-17944 (2013).

[145] Y. Zhong, and R.V. Bellamkonda, Biomaterials for the central nervous system. J. R. Soc. Interface 2008, 5, 957–975.

[146] O. Jeznach, D. Kołbuk, and P. Sajkiewicz. Injectable hydrogels and nanocomposite hydrogels for cartilage regeneration. J. Biomed. Mater.Res. A 2018, 106, 2762–2776.

[147] B.N. Brown, and S.F. Badylak. Extracellular matrix as an inductive scaffold for functional tissue reconstruction.Transl. Res. 2014, 163, 268–285.

[148] R. Ravichandran, C. Astrand, H.K. Patra, A.P. Turner, V. Chotteau, and J. Phopase. Intelligent ECM mimetic injectable scaffolds based on functional collagen building blocks for tissue engineering and biomedicalapplications. RSC Adv. 2017, 7, 21068–21078.

[149] S.P. Miguel, R.S. Sequeira, A.F. Moreira, C.C. Cabral, A.G. Mendonça,  P. Ferreira,  and I.J. Correia. An overview of electrospun membranes loaded with bioactive molecules for improving the wound healing process. Eur. J. Pharm. Biopharm. 2019, 139, 1–22.

[150] M. Okamoto. The role of scaffolds in tissue engineering. In Handbook of Tissue Engineering Sca_olds; Elsevier:Amsterdam, The Netherlands, 2019; Vo1, pp. 23–49.

[151] P.I. Morgado, A. Aguiar-Ricardo, and I.J. Correia. Asymmetric membranes as ideal wound dressings: An overview on production methods, structure, properties and performance relationship. J. Membr. Sci. 2015,490, 139–151.

[152] A. Subramanian, U.M. Krishnan, and S.  Sethuraman. Development of biomaterial scaffold for nerve tissue engineering: Biomaterial mediated neural regeneration. J. Biomed. Sci. 2009, 16, 108.

[153] F. Shapiro. Overview of Deformities. In Pediatric Orthopedic Deformities; Springer: Cham, Switzerland, 2016, Vol. 1, pp. 159–254.

[154] E. Mercadelli, A. Sanson, and C. Galassi. Porous Piezoelectric Ceramics. In Piezoelectric Ceramics;Suaste-Gomez, E., Ed.; InTech: Rijeka, Croatia, 2010; pp. 111–129.

[155] W. Wersing, W. Lubitz, and J. Mohaupt. Dielectric, elastic and piezoelectric properties of porous PZT ceramics.Ferroelectrics 1986, 68, 77–97.

[156] E. Ringgaard, F. Lautzenhiser, L. Bierregaard, T. Zawada, and E. Molz. Development of porous piezoceramics for medical and sensor applications. Materials 2015, 8, 8877–8889.

[157] C. Xue, N. Hu, Y Gu,  Y. Yang,  Y Liu,  J. Liu, F. Ding,  and X. Gu. Joint use of a chitosan/PLGA scaffold and MSCs to bridge an extra large gap in dog sciatic nerve. Neurorehabil. Neural Repair 2012, 26, 96–106.

[158] N.C. Carville, L. Collins, M. Manzo, K. Gallo, B.I. Lukasz, K.K. McKayed, and B.J. Rodriguez. Biocompatibilityof ferroelectric lithium niobate and the influence of polarization charge on osteoblast proliferation andfunction. J. Biomed. Mater.Res. A 2015, 103, 2540–2548.

[159] K. Furuya, Y. Morita, K. Tanaka, T. Katayama, and E. Nakamachi. Acceleration of osteogenesis by using barium titanate piezoelectric ceramic as an implant material. In Proceedings of the International Society for Opticsand Photonics, San Diego, CA, USA, 3–7 May 2011; Vol. 7975, p. 79750U.

[160] J.P. Ball, B.A. Mound, J.C. Nino, and J.B. Allen. Biocompatible evaluation of barium titanate foamed ceramic structures for orthopedic applications. J. Biomed. Mater. Res. A 2014, 102, 2089–2095.

[161] H.B. Lopes, T.D.S. Santos, F.S. De Oliveira, G.P. Freitas, A.L. De Almeida, R. Gimenes, and M.M. Beloti. Poly (vinylidene-trifluoroethylene)/barium titanate composite for in vivo support of bone formation. J. Biomater. Appl. 2014, 29, 104–112.

[162] X. Zhang, C.  Zhang, Y. Lin, P. Hu, Y. Shen, K. Wang, and Y. Liu. Nanocomposite membranes enhance bone regeneration through restoring physiological electric microenvironment. ACS Nano 2016, 10, 7279–7286.

[163] S. Roberts. Dielectric and piezoelectric properties of barium titanate. Phys. Rev. 1947, 71, 890.

[164] F.R. Baxter, C.R. Bowen, I.G. Turner, and A.C. Dent. Electrically active bioceramics: A review of interfacialresponses. Ann. Biomed. Eng. 2010, 38, 2079–2092.

[165] G. Ciofani, L. Ricotti, C. Canale, D. D’Alessandro, S. Berrettini, B. Mazzolai, and V. Mattoli. Effects of barium titanate nanoparticles on proliferation and differentiation of rat mesenchymal stem cells. Colloids Surf.B Biointerfaces 2013, 102, 312–320.

[166] G. Ciofani, L.  Ricotti, and V. Mattoli. Preparation, characterization and in vitro testing of poly (lactic-co-glycolic)acid/barium titanate nanoparticle composites for enhanced cellular proliferation. Biomed. Microdevices 2011,13, 255–266.

[167] O. Ivanova, C. Williams, and T. Campbell. Additive manufacturing (AM) and nanotechnology: Promises and challenges. Rapid Prototyp. J. 2013, 19, 353–364.

[168] J. Jacob, N. More, K. Kalia, and G. Kapusetti. Piezoelectric smart biomaterials for bone and cartilage tissueengineering.Inflamm. Regen. 2018, 38, 2.

[169] F. Matassi, L. Nistri, D.C. Paez, and M. Innocenti. New biomaterials for bone regeneration. Clin.Cases Miner.Bone Metab. 2011, 8, 21.

[170] P. Ahmad, M.U. Khandaker, Z.R. Khan, and Y.M. Amin. Synthesis of boron nitride nanotubes via chemical vapour deposition: A comprehensive review. Mater. Sci. Eng. R. 2010, 70, 92–111.

[171] D. Lahiri, F. Rouzaud, T. Richard, A.K. Keshri, S.R. Bakshi, L. Kos, and A. Agarwal. Boron nitride nanotube reinforced polylactide–polycaprolactone copolymer composite: Mechanical properties and cytocompatibility with osteoblasts and macrophages in vitro. Acta Biomater.2010, 6, 3524–3533.

[172] D. Lahiri, V. Singh, A.P. Benaduce, S. Seal, L. Kos, and A. Agarwal. Boron nitride nanotube reinforced hydroxyapatite composite: Mechanical and tribological performance and in-vitro biocompatibility toosteoblasts. J. Mech. Behav. Biomed.2011, 4, 44–56.

[173] X. Li, C. Zhi, N. Hanagata, M. Yamaguchi, Y. Bando, and D. Golberg. Boron nitride nanotubes functionalized with mesoporous silica for intracellular delivery of chemotherapy drugs. Chem. Commun. 2013, 49, 7337–7339.

[174] G. Ciofani, S. Danti, G.G. Genchi, B. Mazzolai, and V. Mattoli. Boron nitride nanotubes: Biocompatibility and potential spill-over in nanomedicine. Small 2013, 9, 1672–1685.

[175]  X. Li, N. Hanagata, X. Wang, M. Yamaguchi, W. Yi, Y. Bando, and D. Golberg. Multimodal luminescent-magnetic boron nitride nanotubes@ NaGdF 4: Eu structures for cancer therapy. Chem. Commun.2014, 50, 4371–4374.

[176] Q. Weng, B. Wang, X. Wang, N. Hanagata, X. Li, D. Liu, and D. Golberg. Highly water-soluble, porous, and biocompatible boron nitrides for anticancer drug delivery. ACS Nano 2014, 8, 6123–6130. X

[177] J. Wang, C.H. Lee, and Y.K. Yap. Recent advancements in boron nitride nanotubes. Nanoscale 2010, 2, 2028–2034.

[178] G. Ciofani, V.  Raa, A.  Menciassi, and A. Cuschieri. Boron nitride nanotubes: An innovative tool for nanomedicine. Nano Today 2009, 4, 8–10.

[179] J.W. Rasmussen, E.  Martinez, P. Louka, and D.G. Wingett.  Zinc oxide nanoparticles for selective destruction of tumor cells and potential for drug delivery applications. Expert Opin.Drug Deliv.2010, 7, 1063–1077.

[180] S. Goel, and B. Kumar. A review on piezo-/ferro-electric properties of morphologically diverse ZnO nanostructures. J. Alloys Compd. 2019, 816, 152491.

[181] Y. Yin, Q.  Lin, H. Sun, D. Chen, Q. Wu, X. Chen, and S. Li. Cytotoxic ejects of ZnO hierarchical architectures on RSC96 Schwann cells. Res. Lett. 2012, 7, 439.

[182] M. Safaei, H.A. Sodano, and S.R. Anton. A review of energy harvesting using piezoelectric materials: State-of-the-art a decade later (2008–2018). Smart Mater. Struct.2019, 28, 113001.

[183] C. Ribeiro, D.M. Correia, S. Ribeiro, V. Sencadas, G. Botelho, and S. Lanceros-Méndez. Piezoelectric poly (vinylidene fluoride) microstructure and poling state in active tissue engineering. Eng. Life Sci. 2015, 15, 351–356.

[184] M.R. Aguilar, and J. San Román. Introduction to smart polymers and their applications. in smart polymers and their applications; Woodhead Publishing: Sawston, UK, 2019; pp. 1–11.

[185] E. Piskin. Biodegradable polymers as biomaterials. J. Biomater. Sci. Polym. Ed. 1995, 6, 775–795.

[186] P. Sajkiewicz. Crystallization behavior of poly (vinylidene fluoride). Eur. Polym. J. 1999, 35, 1581–1590.

[187] A. Gradys, P. Sajkiewicz, S. Adamovsky, A.A. Minakov, and C. Schick. Crystallization of poly (vinylidenefluoride) during ultra-fast cooling. Thermochim. Acta 2007, 461, 153–157.

[188] D.M. Esterly, and B.J. Love. Phase transformation to β-poly (vinylidene fluoride) by milling. J. Polym. Sci. BPolym. Phys. 2004, 42, 91–97.

[189] E.S. Cozza,o.  Monticelli, E. Marsano, and S. Cebe. On the Electrospinning of PVDF: Influence of the experimental conditions on the nanofiber properties. Polym. Int. 2013, 62, 41–48.

[190] L. Yu, and P. Cebe. Crystal polymorphism in electrospun composite nanofibers of poly (vinylidene fluoride) with nanoclay. Polymer 2009, 50, 2133–2141. stop

[191] B.E. El Mohajir, and N. Heymans. Changes in structural and mechanical behavior of PVDF with processing and thermomechanical treatments. 1. Change in structure. Polymer 2001, 42, 5661–5667.

[192] R. Imamura, A.B. Silva, and R. Gregorio, Jr. γ→β Phase transformation induced in poly (vinylidene fluoride)by stretching. J. Appl. Polym. Sci. 2008, 110, 3242–3246.

[193] J. Wang, H. Li, J. Liu, Y. Duan, S. Jiang, and Y. Yan. On the α→β Transition of carbon coated highly oriented PVDF ultrathin film induced by melt recrystallization. J. Am. Chem. Soc. 2003, 125, 1496–1497.

[194] T. Kaura, R. Nath, and M.M. Perlman. Simultaneous stretching and corona poling of PVDF films. J. Phys. D: Appl. Phys. 1991, 24, 1848.

[195] A.K. Ramanathan, L.M. Headings, and M.J. Dapino. Design optimization of flexible piezoelectric PVD funimorphs for surface pressure transducer applications. In smart structures and NDE for energy systems and industry 4.0; International Society for Optics and Photonics: Bellingham, WA, USA, 2019; Vol. 10973, p. 1097307.

[196] C. Ellingford, H. Smith, X. Yan, C.  Bowen, L. Figiel, T. McNally, and C. Wan. Electrical dual-percolation in MWCNTs/SBS/PVDF based thermoplastic elastomer (TPE) composites and the effect of mechanical stretching. Eur. Polym. J. 2019, 112, 504–514.

[197] S. Zhang, Z. Jia, T. Liu, G. Wei, and Z. Su. Electrospinning nanoparticles-based materials interface for sensor applications. Sensors 2019, 19, 3977.

[198] Y. Li, C. Liao, and S.C. Tjong. Electrospun polyvinylidene fluoride-based fibrous scaffolds with piezoelectric characteristics for bone and neural eissue Engineering. Nanomaterials 2019, 9, 952.

[199] L. Yu, P. Zhou, D. Wu, L. Wang, L. Lin, and D. Sun. Shoepad nanogenerator based on electrospun PVDF nanofibers. Microsyst. Technol. 2019, 25, 3151–3156.

[200] C. Ribeiro, C.M. Costa, D.M. Correia, J. Nunes-Pereira, J. Oliveira, P. Martins, and S. Lanceros-Méndez. Electroactive poly (vinylidene fluoride)-based structures for advanced applications. Nat. Protoc. 2018, 13, 681.

[201] M. Fortunato, D. Cavallini, G. De Bellis, F. Marra, A. Tamburrano, F. Sarto, and M.S. Sarto. Phase inversion in PVDF films with enhanced piezoresponse through spin-coating and quenching. Polymers 2019, 11, 1096.

[202] Z.H. Liu, C.T. Pan, L.W. Lin, J.C. Huang, and Z.Y. Ou. Direct-write PVDF nonwoven fiber fabric energy harvesters via the hollow cylindrical near-field electrospinning process. Smart Mater.Struct. 2013, 23, 025003.

[203] B. Zaarour, L. Zhu, and X. Jin. Controlling the surface structure, mechanical properties, crystallinity, and piezoelectric properties of electrospun PVDF nanofibers by maneuvering molecular weight. Soft Mater.2019, 17, 181–189.

[204] R.K. Singh, S.W. Lye, and J. Miao. PVDF nanofiber sensor for vibration measurement in a string. Sensors 2019, 19, 3739.

[205] M. Khalifa, S. Janakiraman, S. Ghosh, A. Venimadhav, and S. Anandhan. PVDF/halloysite nanocomposite-basednon-wovens as gel polymer electrolyte for high safety lithium ion battery. Polym.Compos.2019, 40, 2320–2334.

[206] S. Liang, Y. Kang, A. Tiraferri, E.P. Giannelis, X. Huang, and M. Elimelech. Highly hydrophilic polyvinylidenefluoride (PVDF) ultrafiltration membranes via post-fabrication grafting of surface-tailored silica nanoparticles.ACS Appl. Mater. Interfaces 2013, 5, 6694–6703.

[207] D. Mandal, K. Henkel, and D. Schmeißer. The electroactive β-phase formation in poly (vinylidene fluoride) by gold nanoparticles doping. Materials Lett.2012, 73, 123–125.

[208] J.H. Li, X.S. Shao, Q. Zhou, M.Z. Li, and Q.Q. Zhang. The double ejects of silver nanoparticles on the PVDF membrane: Surface hydrophilicity and antifouling performance. App. Surf. Sci. 2013, 265, 663–670.

[209] S. Liang, K. Xiao, Y. Mo, and X. Huang. A novel ZnO nanoparticle blended polyvinylidene fluoride membrane for anti-irreversible fouling. J. Membr. Sci. 2012, 394, 184–192.

[210] Y.H. Teow, A.L. Ahmad, J.K. Lim, and B.S. Ooi. Preparation and characterization of PVDF/TiO2 mixed matrix membrane via in situ colloidal precipitation method. Desalination 2012, 295, 61–69.

[211] J. Zhang, Z. Xu, W. Mai, C. Min, B. Zhou, M. Shan, and  X. Qian. Improved hydrophilicity, permeability, antifouling and mechanical performance of PVDF composite ultrafiltration membranes tailored by oxidizedlow-dimensional carbon nanomaterials. J. Mater. Chem. A 2013, 1, 3101–3111.

[212] H. Song, J. Shao, Y. He, B. Liu, and X. Zhong. Natural organic matter removal and flux decline with PEG–TiO2-doped PVDF membranes by integration of ultrafiltration with photocatalysis. J. Membr. Sci. 2012,405, 48–56.

[213] N. Li, C. Xiao, S. An, and X. Hu. Preparation and properties of PVDF/PVA hollow fiber membranes. Desalination 2010, 250, 530–537.

[214] A.L. Gayen, D. Mondal, D. Roy, P. Bandyopadhyay, S. Manna, R. Basu, and P. Nandy. Improvisation of electrical properties of PVDF-HFP: Use of novel metallic nanoparticles. J. Mater. Sci.: Mater. 2017, 28, 14798–14808.

[215] B. Jaleh, S. Sodagar, A. Momeni, and A. Jabbari. Nanodiamond particles/PVDF nanocomposite flexible films: Thermal, mechanical and physical properties. Mater.Res. Express 2016, 3, 085028.

[216] A. Fraczek-Szczypta. Carbon nanomaterials for nerve tissue stimulation and regeneration. Mater. Sci. Eng. C2014, 34, 35–49.

[217] C. Tsonos, C. Pandis, N. Soin, D. Sakellari, E. Myrovali, S. Kripotou, and E Siores. Multifunctional nanocomposites of poly (vinylidene fluoride) reinforced by carbon nanotubes and magnetite nanoparticles. Express Polym. Lett.2015, 9.

[218] B. Lorber, W.K. Hsiao, I.M. Hutchings, and K.R. Martin. Adult rat retinal ganglion cells and glia can be printed by piezoelectric inkjet printing. Biofabrication 2013, 6, 015001.

[219] T. Inaoka, H. Shintaku, T. Nakagawa, S. Kawano, H. Ogita, T. Sakamoto, and J. Ito. Piezoelectric materials mimic the function of the cochlear sensory epithelium. Proc. Natl. Acad. Sci. USA 2011, 108, 18390–18395.

[220] Y. Gao, and Z.L. Wang. Electrostatic potential in a bent piezoelectric nanowire. The fundamental theory of nanogenerator and nanopiezotronics. Nano Lett. 2007, 7, 2499–2505.

[221] J.F. Walsh, M.E. Manwaring, and P.A. Tresco. Directional neurite outgrowth is enhanced by engineered meningeal cell-coated substrates. Tissue Eng. 2005, 11, 1085–1094.

[222] T. Asano, T. Kubo, and Y. Nishikitani. Electrochemical properties of dye-sensitized solar cells fabricated with PVDF-type polymeric solid electrolytes. J. Photochem. Photobiol.2004, 164, 111–115.

[223] A. Marino, S. Arai, Y. Hou, E. Sinibaldi, M. Pellegrino, B. Chang, V. Mazzolai, M. Mattoli Suzuki, and G. Ciofani. Piezoelectric nanoparticle-assisted wireless neuronal stimulation. ACS Nano 2015, 9, 7678–7689.

[224] G.G. Genchi, L. Ceseracciu, A. Marino, M. Labardi, S. Marras, F. Pignatelli, L. Bruschini, V. Mattoli, and G. Ciofani. P(VDF-TrFE)/BaTiO3 nanoparticle composite films mediate piezoelectric stimulation and promote differentiation of SH-SY5Y neuroblastoma cells. Adv. Healthc. Mater.2016, 5, 1808–1820.

[225] N. Weber, Y.S. Lee, S. Shanmugasundaram, M. Jae, and T.L. Arinzeh. Characterization and in vitrocytocompatibility of piezoelectric electrospun scaffolds.Acta Biomater.2010, 6, 3550–3556.

[226] G.C. De Ruiter, M.J. Malessy, M.J. Yaszemski, A.J. Windebank, and R.J. Spinner. Designing ideal conduits for peripheral nerve repair. Neurosurg. Focus. 2009, 26, E5.

[227] S. Ichihara, Y.  Inada, and T. Nakamura. Artificial nerve tubes and their application for repair of peripheral nerve injury: An update of current concepts. Injury 2008, 39, 29–39.

[228] Y. Ji, R. Jin, X. Zhang, R. Bouchilaoun, J. Fan, R. Zhao, and H. Yang. Electric polarizations in PVDF-TrFE nanorods under lateral nanoshaping. Int. J. Appl. 2019, 126, 174108.

[229] C. Wan, and C.R. Bowen. Multiscale-structuring of polyvinylidene fluoride for energy harvesting: The impact of molecular-, micro- and macro-structure. J. Mater. Chem. A 2017, 5, 3091–3128.

[230] F.C. Sun, A.M. Dongare, A.D. Asandei, S.P. Alpay, and S. Nakhmanson. Temperature dependent structural, elastic, and polar properties of ferroelectric polyvinylidene fluoride (PVDF) and trifluoroethylene (TrFE)copolymers. J. Mater. Chem. C 2015, 3, 8389–8396.

[231] J.S. Belkas, M.S. Shoichet, and R. Midha. Peripheral nerve regeneration through guidance tubes. Neurol. Res.2004, 26, 151–160.

[232] R. Boni, A. Ali, A. Shavandi, and A.N. Clarkson. Current and novel polymeric biomaterials for neural tissue engineering. J Biomed.Sci. 2018, 25, 90.

[233] E.G. Fine, R.F. Valentini, R. Bellamkonda, and P. Aebischer. Influence of surface texture of polymeric sheetsthrought piezoelectric vinylidenefluoride-trifluoroethylene copolymer guidance channels. Biomaterials 1991, 12, 259–263.

[234] P.M. Martins, S. Ribeiro, C. Ribeiro, V. Sencadas, A.C. Gomes, F.M. Gama, and S. Lanceros-Méndez. Effect of poling state and morphology of piezoelectric poly (vinylidene fluoride) membranes for skeletal muscle tissue engineering. RSC Adv. 2013, 3, 17938–17944.

[235] S. Ke, H. Huang, L. Ren, and Y. Wan. Nearly constant dielectric loss behavior in poly (3-hydroxybutyrate-co-3-hydroxyvalerate) biodegradable polyester. J. Appl. Phys. 2009.

[236] K. Numata, H. Abe, and Y. Doi. Enzymatic processes for biodegradation of poly (hydroxyalkanoate) s crystals.Can. J. Chem. 2008, 86, 471–483.

[237] S.M. Willerth, and S.E. Sakiyama-Elbert. Approaches to neural tissue engineering using scaffolds for drug delivery.Adv. Drug Deliv. Rev. 2007, 59, 325–338.

[238] Q. Wu, Y. Wang, and G.O. Chen. Medical application of microbial biopolyesters polyhydroxyalkanoates.Artif.Cells Blood Substit.Immobil.Biotechnol.2009, 37, 1–12.

[239] S.K. Misra, S.P. Valappil, I. Roy, and A.R. Boccaccini. Polyhydroxyalkanoate (PHA)/inorganic phase composites for tissue engineering applications. Biomacromolecules 2006, 7, 2249–2258.

[240] M.P. Prabhakaran, E. Vatankhah, and S. Ramakrishna. Electrospun aligned PHBV/collagen nanofibers assubstrates for nerve tissue engineering. Biotechnol Bioeng. 2013, 110, 2775–2784.

[241] M.S. Rahman, and T. Tsuchiya. Enhancement of chondrogenic differentiation of human articular chondrocytesby biodegradable polymers. Tissue Eng. 2001, 7, 781–790.

[242] W. Chen, and Y.W. Tong. PHBV microspheres as neural tissue engineering scaffold support neuronal cell growth and axon–dendrite polarization. Acta Biomater.2012, 8, 540–548.

[243] A.L. Rivera-Briso, and A. Serrano. Poly (3-Hydroxybutyrate-co-3-Hydroxyvalerate): Enhancement strategies for advanced applications. Polymers 2018, 10, 732.

[244] V. Sencadas, C. Ribeiro, A. Heredia, I.K. Bdikin, A. L. Kholkin, and S. Lanceros-Méndez. Local piezoelectric activity of single poly (L-lactic acid)(PLLA) microfibers. Appl. Phys. A 2012, 109, 51–55.

[245] L. Jin, Z.Q. Feng, M.L. Zhu, T. Wang, M.K. Leach, and Q. Jiang. A novel fluffy conductive polypyrrolenano-layer coated PLLA fibrous sca_old for nerve tissue engineering. J. Biomed. Nanotechnol.2012, 8, 779–785.

[246] K. Zhang, H. Zheng, S. Liang, and C. Gao. Aligned PLLA nanofibrous scaffolds coated with graphene oxide for promoting neural cell growth. Acta Biomater.2016, 37, 131–142.

[247] J.M. Zuidema, C. Provenza, T. Caliendo, S. Dutz, and R.J. Gilbert. Magnetic NGF-releasing PLLA/ironoxide nanoparticles direct extending neurites and preferentially guide neurites along aligned electrospunmicrofibers. ACS Chem. Neurosci. 2015, 6, 1781–1788.

[248] J. Venugopal, Y.Z.  Zhang, and S. Ramakrishna. Electrospun nanofibres: Biomedical applications. Proceedings of the institution of mechanical engineers.N J. Nanoeng.Nanosyst. 2004, 218, 35–45.

[249] B. Philipp, W. Bock, and F. Schierbaum. Application of polysaccharides and their derivatives as supportingmaterials and auxiliary substances in medicine and nutrition. J. Polym. Sci. Polym. Symp.1979, 66, 83–100.

[250] G. Franz. Polysaccharides in pharmacy. Adv. Polym. Sci. 1986, 76, 1–30.

[251] T. Miyamoto, S.I. Takahashi, H. Ito, H. Inagaki, and Y. Noishiki. Tissue biocompatibility of cellulose and its derivatives. J. Biomed. Mater. Res. 1989, 23, 125–133.

[252] Y. Ikada. Biomedical applications of cellulose membranes. in cellulose: structural and functional aspects; Kennedy, J.F., Phillips, G.O.,Williams, P.A., Eds.; Ellis Horwood: Chichester, UK, 1989; pp. 447–455.

[253] C. Barbié, D. Chauveaux, X. Barthe, C. Baquey, and J. Poustis. Biological behavior of cellulosic materials after bone implantation: Preliminary results. Clin.Mater.1990, 5, 251–258.

[254] U. Gross, C. Muller-Mai, and C. Voigt. The tissue response on cellulose cylinders after implantation in the distal femur of rabbits. In Proceedings of the Fourth World Biomaterials Congress, Berlin, Germany,19–24 May 1992; p. 192.

[255] M. Märtson, J. Viljanto, T. Hurme, and P. Saukko. Biocompatibility of cellulose sponge with bone. Eur. Surg. Res.1998, 30, 426–432.

[256] A. Bhatnagar, and M. Sain. Processing of cellulose nanofiber-reinforced composites. J. Reinf. Plast. Comp. 2005, 24, 1259–1268.

[257] J.C. Fricain, P.L. Granja, M.A. Barbosa, B. De Jéso, N. Barthe, and C. Baquey. Cellulose phosphates as biomaterials. In vivo biocompatibility studies. Biomaterials 2002, 23, 971–980.

[258] A. Svensson, E. Nicklasson, T. Harrah, B. Panilaitis, D.L. Kaplan, M. Brittberg, and P. Gatenholm. Bacterial cellulose as a potential sca_old for tissue engineering of cartilage. Biomaterials 2005, 26, 419–431.

[259] M. Märtson, J. Viljanto, P. Laippala, and P. Saukko. Connective tissue formation in subcutaneous cellulose sponge implants in the rat. Eur. Surg. Res. 1998, 30, 419–425.

[260] G. Fundueanu, M. Constantin, E. Esposito, R. Cortesi, C. Nastruzzi, and E. Menegatti. Cellulose acetate butyrate microcapsules containing dextran ion-exchange resins as self-propelled drug release system. Biomaterials2005, 26, 4337–4347.

[261] E. Entcheva, H. Bien, L. Yin, C.Y. Chung, M. Farrell, and Y. Kosto. Functional cardiac cell constructs on cellulose-based scaffolding. Biomaterials 2004, 25, 5753–5762.

[262] M.C. Tate, D.A. Shear, S.W. Hoffman, D.G. Stein, and M.C. LaPlaca. Biocompatibility of methylcellulose-based constructs designed for intracerebral gelation following experimental traumatic brain injury. Biomaterials2001, 22, 1113–1123.

[263] S.M. Hoseini, K. Khosravi-Darani, and M.R. Mozafari. Nutritional and medical applications of spirulina microalgae. Mini Rev. Med. Chem. 2013, 13, 1231–1237.

[264] P.L. Granja, M.A. Barbosa, L. Pouységu, B. De Jéso, F. Rouais, and C. Baquey. Cellulose phosphates as biomaterials. Mineralization of chemically modified regenerated cellulose hydrogels. J. Mater. Sci. 2001,36, 2163–2172.

[265] M. Naseri-Nosar, M. Salehi, and S. Hojjati-Emami. Cellulose acetate/poly lactic acid coaxial wet-electrospun scaffold containing citalopram-loaded gelatin nanocarriers for neural tissue engineering applications. Int. J.Biol. Macromol. 2017, 103, 701–708.

[266] S. Wang, C. Sun, S. Guan, W. Li, J. Xu, D. Ge, and X. Ma. Chitosan/gelatin porous scaffolds assembled with conductive poly (3, 4-ethylenedioxythiophene) nanoparticles for neural tissue engineering. J. Mat. Chem. B2017, 5, 4774–4788.

[267] S.S. Koide. Chitin-chitosan: Properties, benefits and risks. Nutr. Res. 1998, 18, 1091–1101.

[268] M. Rinaudo. Chitin and chitosan: Properties and applications. Prog. Polym. Sci. 2006, 31, 603–632.

[269] S.V. Madihally, and H.W. Matthew. Porous chitosan scaffolds for tissue engineering. Biomaterials 1999, 20, 1133–1142.

[270] K. Ohkawa, D. Cha, H. Kim, A. Nishida, and H. Yamamoto. Electrospinning of chitosan. Macromol.Rapid Commun.2004, 25, 1600–1605.

[271] D. Izzo, B. Palazzo, F. Scalera, F. Gullotta, V. Lapesa, S. Scialla, and F. Gervaso. Chitosan scaffolds for cartilage regeneration: Influence of di_erent ionic crosslinkers on biomaterial properties. Int. J. Polym. Mater.2019, 68, 936–945.

[272] A. Maged, A.A. Abdelkhalek, A.A. Mahmoud, S. Salah, M.M. Ammar, and M.M. Ghorab. Mesenchymalstem cells associated with chitosan sca_olds loaded with rosuvastatin to improve wound healing. Eur. J.Pharm. Sci. 2019, 127, 185–198.

[273] Y. Xue, M. Wu, Z. Liu, J. Song, S. Luo, H. Li, and F. Chen. In vitro and in vivo evaluation of chitosan scaffolds combined with simvastatin-loaded nanoparticles for guided bone regeneration. J. Mater. Sci. Mater. Med. 2019, 30, 47.

[274] N.B. Skop, F. Calderon, S.W. Levison, C.D. Gandhi, and C.H. Cho. Heparin crosslinked chitosan microspheres for the delivery of neural stem cells and growth factors for central nervous system repair. Acta Biomater.2013, 9, 6834–6843.

[275] Y.S.R. Elnaggar, S.M. Etman, and D.A. Abdelmonsif. Intranasal piperine-loaded chitosan nanoparticles as brain-targeted therapy in alzheimer’s disease: optimization, biological efficacy, and potential toxicity. J. Pharm. Sci. 2015, 104, 3544–3556.

[276] R. Raj, S. Wairkar, V. Sridhar, and R. Gaud. Pramipexole dihydrochloride loaded chitosan nanoparticles for noseto brain delivery: Development, characterization and in vivo anti-Parkinson activity. Int. J. Biol. Macromol.2018, 109, 27–35.

[277] S.H. Liu, and P.C. Ho. Intranasal administration of brain-targeted HP-β-CD/chitosan nanoparticles for delivery ofscutellarin, a compound with protective effect in cerebral ischaemia. J. Pharm. Pharmacol. 2017, 69, 1495–1501.

[278] A. Cooper, N. Bhattarai, and M. Zhang. Fabrication and cellular compatibility of aligned chitosan–PCL fibersfor nerve tissue regeneration.Carbohydr.Polym.2011, 85, 149–156.

[279] Y.C. Kuo, C.F. Yeh, and J.T. Yang. Differentiation of bone marrow stromal cells in poly (lactide-co-glycolide)/chitosan scaffolds. Biomaterials 2009, 30, 6604–6613.

[280] V. Marchesano, O. Gennari, L. Mecozzi, S. Grilli, and P. Ferraro. Effects of lithium niobate polarization on cell adhesion and morphology. ACS Appl. Mater. Interfaces.2015, 7, 18113–18119.

[281] A. Tiffany, and B.A. Harley. Sequestration of biomolecules for controlled delivery in mineralized collagen scaffolds. In 42nd society for biomaterials annual meeting and exposition 2019: The pinnacle of biomaterials innovation and excellence. Soc. Biomater. 2019, 40, 1526–7547.

[282] I. Sallent, H. Capella-Monsonís, and D.I. Zeugolis. Production and characterization of chemically cross-linked collagen scaffolds. in collagen; Humana Press: New York, NY, USA, 2019; pp. 23–38.

[283] L. Mohee, G.S. Offeddu, A. Husmann, M. L. Oyen, and R.E. Cameron. Investigation of the intrinsic permeability of ice-templated collagen scaffolds as a function of their structural and mechanical properties. Acta Biomater.2019, 83, 189–198.

[284] Y. Liu, T. Nelson, J. Chakro, B. Cromeens, J. Johnson, J. Lannutti, and G.E. Besner. Comparison of polyglycolic acid, polycaprolactone, and collagen as scaffolds for the production of tissue engineered intestine. J. Biomed.Mater. Res. B 2019, 107, 750–760.

[285] X. Lei, J. Gao, F. Xing, Y. Zhang, Y. Ma, and G. Zhang. Comparative evaluation of the physicochemical properties of nano-hydroxyapatite/collagen and natural bone ceramic/collagen scaffolds and their osteogenesis-promoting effect on MC3T3-E1 cells. Regen. Biomater.2019, 6, 361–371.

[286] S. Radhakrishnan, S. Nagarajan, M. Bechelany, and S.N. Kalkura. Collagen based biomaterials for tissue engineering applications: a review. in processes and phenomena on the boundary between biogenic and abiogenic; Nature; Springer: Cham, Switzerland, 2020; pp. 3-22.

[287] A. Eltom, G. Zhong, and A. Muhammad. Scaffold Techniques and Designs in Tissue Engineering Functions and Purposes: A Review. Adv. Mater. Sci. Eng. 2019.

[288] M. Mohseni, N.J. Castro, H.P. Dang, T.D. Nguyen, H.M. Ho, M.P.N. Tran, and P.A. Tran. Adipose tissue regeneration: scaffold-biomaterial strategies and translational perspectives. in biomaterials in translational medicine; Academic Press: Cambridge, MA, USA, 2019; pp. 291–330.

[289] D. Ceballos, X. Navarro, N. Dubey, G. Wendelschafer-Crabb, W.R. Kennedy, and R.T. Tranquillo. Magnetically Aligned Collagen Gel Filling a Collagen Nerve Guide Improves Peripheral Nerve Regeneration. Exp. Neurol.1999, 158, 290–300.

[290] N. Dubey, P.C. Letourneau, and R.T. Tranquillo. Guided neurite elongation and schwann cell invasion into magnetically aligned collagen in simulated peripheral nerve regeneration. Exp. Neurol. 1999, 158, 338–350.

[291] Y. Eguchi, M. Ogiue-Ikeda, and S. Ueno. Control of orientation of rat schwann cells using an 8-T static magnetic field. Neurosci.Lett.2003, 351, 130–132.