Piezo-and Magneto-Active Polymer Scaffolds in Tissue Engineering

Ogah Anselm Ogah*1, Friday Nwankwo Archibong2

1Department of Polymer & Textile Engineering, Nnamdi Azikiwe University, P.M.B. 5025, Awka, Nigeria

2Department of Mechanical Engineering, Alex-Ekwueme Federal University Ndufu-Alike Ikwo, P.M.B. 1010, Nigeria

*Corresponding Author Email Address: ao.ogah@unizik.edu.ng

Abstract

Biomedical engineering depends on scaffoldings for boosting cell diversification and development having rearmost precedence on incitement feedback platforms, sometimes nominated active structures. Amongst the elucidative in this substance order are piezoelectric structures, able of igniting positive or negative ions subject to insouciant excitation that generates substantial anticipation to exercising pulpits for safe treatment of whim-whams cell. Tissue engineering and recreating drug are growingly making good use of responsive accoutrements, enabling the force of determined signal to the organism. Specifically, the using electro-active substrates which conveys charged cue to the cells through involuntary excitations, unlock new chemical and high-tech windows which actually copy suggestions as well as issues which take place within natural systems, enabling elaboration at applicable terrain for restoration of organs.Therefore, an innovative approach was evolved that piezo-magneto-active polymer platforms are ideal for dispatching those cue. Hence the applications of piezo-magneto-active polymer scaffolds in tissue engineering will be discussed.

Keywords: piezo-magneto-active, polymer scaffolds, tissue engineering, smart materials

Introduction

Smart accoutrements astronomically relate to substances that adjustably alter several of their active features, in agreement with forced outside incitement or to the changes within the immediate terrain [1]. An external persuading comprises light, temperature, and electromagnetic fields, pH, stress and strain. Piezoelectric pulpits can be contemplated as intelligent systems which convert mechanical cargo to electrical cues [2]. Pierre Curie and Jacques Curie in 1880 reported that the presence of a demitasse chassis and the absence of a center of harmonydetermine the piezoelectricity of a material [3]. The term “Piezo” chased from the Greek word “Piezein” connoting constrain [4].Piezoelectric products have a broad multifariousness of operations in electronics including transducers, selectors and detectors. Besides, notable area of operations of piezoelectric products is in biomedical engineering similar as electro-active platforms for organ reconstruct and restoration. Piezoelectric accoutrements convey changing charge activations in the absence of a source of external power [5]. The piezoelectric altar can induce electrical stimulation which can regenerate and repair napkin through defined routes [6]. The fine-tuned parcels of piezoelectric can make accurate bio-electro emigrations, identical with native matrisome, notable amid revamping situation in bone [7].

In biomedical engineering, electro-active support are veritably important in towel engineering using ionic excitation for the organ reconstruct or restoration, like neural organ reconstruct, bone reconstruct and restoration among others. [8]. Piezoelectricity has been observed in skeleton, gristle, tusk, sinew and scleroproteins [9]. A fiber-suchlike structure similar as collagen is anintroductory element in skeleton and gristle accountable for the magnetostrictive parcels [10]. The magnetostrictive parcels of gelatin cause electrifying cues in reaction to intra constrain. The extracellular matrix (ECM) conveys the cues to the voltage-controlled channels of the cytomembrane. Largely, osteoblasts is participators with mechano-transduction which village with bone-forming cells and bone-breaking cells. Boosting of these pathways conveys the extracellular cues to the origin guiding pungency of communicating avalanches, in control of the cellular conditioning including matrix manufacture, cell development and towel reconstruct [11]. Thus, electro-active structures imitating piezoelectric adjuvant of ingrain napkins could bean applicable procedure to reconstruct and restore bone and cartilage.

The objectification of cells, bioactive factors and pulpits for biomedical operations, similar as towel engineering, permits the advancement of natural reserves to restore and/or enhance towel functions [12]. Pulpits constitute a vital element in towel engineering approaches, allocating anatomical bolster for corpuscle development in addition to needed stimulants for factual towel regeneration [13, 14]. In this perspective, active intelligent accoutrements are suitable to adjustably change sole or further of their operative or anatomical features in a regulated or reproducible style being subordinated by outside stimulants, like heat, tension, galvanic or glamorous spheres, etc [15, 16]. Application of these smart accoutrements is suitable to copy the changing innate cell terrain through doling out handy person or charged stimulants identical with bones available in mortal organism [17]. Amid smart substances, electro-active accoutrements have depicted aptness for towel engineering operations owing to their implicit to transfigure a mechanical distortion into an electrical eventualityand contrarily, without taking an outside voltage origin [15, 18]. Thus, intelligent accoutrements are of enormous significance to refurbishing functional bio-mimetic milieu. The subject is uses merit in magnetostrictive accoutrements to imitate electronic and automatic signals living in natural napkin and hence help for ingrain rejuvenescence [19].

Bone diseases are an enlarging radix of solicitude as they produce important effect on humans, confining their standard of living, and on their families; that are veritably frequent, substantially amid aged people, and have high related prices. Between the colorful categories of skeletal affections, bone weakening is linked with greater expenses [20, 21] resulting to increase in senior citizens, further individualities are being touched. Persons impacted with osteoporosis have anadvanced trouble of fractures [22], creating impairment and diminishing their standard of living. Relating to remedy, present remedies are effective, although they've weak prolonged compliance, due to mitigation of wound typically is target for treatment [23].Due to the growth in towel manufacturing ways, curatives have advanced for skeletal affections [24]. Actually, towel engineering holds a high function for successful cure for bone complications and remarkable attempts are being conducted to develop recent efficient restoration plans [25]. These rearmost plans bear refurbishing bone towel micro-habitat that covers automatic, mechanoelectric and chemical processes arousing rudiments which are in-charge of modulating osteogenic cellular activity [25].

Majority of accoutrements applied in skeletal towel engineering furnish external biochemical stimulants, like cytokine, yet it is deficit in biological response taking place in living organism, hassle in managing excessive division or inaccurate prosecution, as a result, therapeutic prospects of the accoutrements are confined [26]. Therefore, current accoutrements conduct is needed so as to surmount these lapses. One practicable way is creating biophysical stimulants, like mechanical and electrical, as they are available in the course of bone growth and activity [26]. Native skeletal towel is piezoelectrifying implying that once an automatic incantation is performed on the skeleton, a charged terrain is generated [27]. Actually, piezoelectric substances have are described to enhance osteoblasts proliferation and isolation [28, 29]. Amid the colorful physical stimulants, automatic effects are extensively studied as catalyst to impel natural kinesis to mechano-transduction action.

Nevertheless, a rearmost genre of material stimulants like employment of charges and glamorous signals is getting prominent. Following the development of accoutrements wisdom, the concurrent application of similar stimulants is doable using intelligent accoutrements which via mechanical incantation concomitantly incite electronic and glamorous milieu in skeleton [29, 30]. A magnetostrictive substance is a case in similar intelligent accoutrements. Regarding bone towel engineering, piezoelectric substances are contemplated a new mix among organic elements and somatic stimulants described recently [28, 29]. Either, modifying the face unevenness and face eventuality of the pulpits, it’s realizable to regulate the corpuscle attachment [31] and mineralization procedure [32], independently. These kinds of accoutrements permit the modulation of the activities of the cells and eventually make factual osteogenesis, boosting an electric eventuality to cells that revives cells that form new bones outside the living organism, in non-contagious manner. Colorful sizes and morphologies including pervious membranes, nanofibers and flicks are estimated in a befitting measure for skeleton towel manufacturing, utmost inquiries utilizing pulpits template as napkins and cells to gain [28–30, 33].

This chapter will be concentrated on the operations of piezo-and-magneto-active polymer scaffolds in towel manufacturing.

Towel manufacturing

Towel manufacturing refers to a treatment system confronting towel injury or deterioration, which targets to make up new towel from individual cases, including inside or outside conditions, avoiding craving for contributors [34]. But, it needs accoutrements with particular customized parcels, after attaining a height of bio-mimicry that permits advancement in flourishing and functional towel. Bulk muscle loss, owing to complaint or critical bruise, is especially serious problem of towel injury owing to the difficulty and low fixable of muscle towel. As a result, colorful treatments affect in reprehensible issues [35]. Towel engineering is an implicit remedy to this issue, still, the point and particular demands of the cadaverous muscle filaments engenders that norespectable towel engineering remedies have yet been advanced. A satisfactory result needs to be suitable to furnish the cells with either inert stimulants, like mechano-transduction by ways of accoutrements in particular stiffness and/or pulpits composed of acquainted filaments [36,37], and energetic stimulants, like changing electronic and automatic, imitation of the traditional development surroundings of tendon towel [38]. Also, sundry of the accoutrements needed to be nontoxic, impeccably degradable, permitting stimulants applicability through manageable way via rejuvenescence process.

Smart accoutrements are defined as accoutrements that are manipulated to respond in a controllable and reversible way, modifying some of their parcels as a result of external stimulants, similar as automated, chemistry, electronic, or glamorous [39], have eventually broken the walls. Especially, macromolecules-grounded intelligent accoutrements recycled by diverse shapes, similar as flicks, filaments, and microspheres [40], already delved in towel engineering operations in skeleton [41], heart [42], as well as cadaverous tendon napkins, having been validated in energetic acquainted plastic fiber pulpits farther corpuscle advancement in towel rejuvenescence [36,37]. One specific process, electrospinning, permits accurate mastery of very small- and tiny fiber parcels, being modulated for particular purposes end napkins and milieus, enhancing corpuscle and towel rejuvenescence [37].

Certain of the constantly being biodegradable polymers applied in towel engineering designs include poly (lactic acid), poly (glycolic acid) and different poly (lactic-co-glycolide) blend of polymers [43]. Accepted for therapeutic administration by the United States Food and Drug Administration and the European Medicines Agency [44], poly (lactic-co-glycolide) is a lot chosen rather than its homopolymers owing to excellent mastery decomposability, permitting its use-defined revision. The polymer is either nontoxic or degradable, having declination passing via a hydrolysis volume declination procedure, through arbitrary disunion medium, with derivatives such as lactic and glycolic acid that is doused using natural organisms through the kidney structure [45]. Poly (lactic-co-glycolide) is reused in different dimensions such as very small and tiny particles, 3-dimensional pulpits filaments [45], having bioengineering uses for medical and symptomatic rescue and towel engineering [46]. Beneficial to modulate physicochemical parcels in plastics to incite particular reactions, like glamorous or electronic admittance, poly mixes fabricated for bioengineering operations [46–48]. Amid the constantly employed paddings are glamorous bones, delved in spheres similar as hyperthermia, magneto-mechanical [49], and magneto-electric influences [41], among others, and conductive paddings delved in the field of electro-active stimulants [42]. As for glamorous spaddings for plastic blends, ferric oxides is a nontoxic emulsion estimated for a diverse applications, such as detectors, selectors, bioengineering and ecological requital [49,50]. Ferric oxide nano-particles exhibit super-paramagnetic conduct in confines ˂ 20 nanometer is ferri-glamorous around 20 and 300 nanometers respectively [51], with fascinating magnetically guiding administration stimulants for plastic-grounded pulpits.

The mature mortal heart is an active organ in control of blood pumping and rotation, in addition to oxygen and nutrients dispensation all over the anatomy [52]. Heart diseases radiate by irrecoverable detriment to heart cells caused through death of cells, death of body napkins, being the crucial originator of demise and fitness profitable rigors widely [53]. On damage or complaint, cardiac napkins possess inadequate form capacity and are substituted by dysfunctional napkins, impacting the constrictive capability of the cardiac which could result in disastrous collapse [54, 55]. Consequently, surgical operation is needed to recoup cardiac performance [56], but, they are veritably confined by the handiness of benefactors [56]. Heart towel manufacturing is a prospective approach to substitute injured corridor of the viscus with artificial-finagled heart napkins with a possible option to cardiac surgical procedure [56, 57]. Notwithstanding, developing fully grown cardiac napkins in vitro is still demanding [58], remarkable advance has been made over the last years concerning the advancement of useful biological materials and bioinspiration pulpits  employed for heart towel engineering [59–61]. In line with biomaterial's standpoint, intelligent piezoelectric accoutrements can produce redundant functionalities hence their character as under sub-caste and subscribe towards the advancement of cell-biomaterial exchange. Especially, piezoelectric accoutrementshave the prospective to mimic the mechano-electrical transduction structure available in cardiac napkins still they’ve been nearly fully delved in bone and cartilage towel engineering [62].

Beside the common biochemical signals furnished by growth factors, electrophysiology transmission, moderated internal circuit fields and flows, perform a vital function in biological and physical signal [63–66]. Different kinds of towels bestow electronically transmittance and responsive attributes in deconstruction similar as piezoelectricity and ferro-electricity, and hence numerous activities are controlled by charged cues. Figure 1, shows the different types of towel comprising of the neurotic system, cardiac, skeleton, tendon, and rind involved in regulating the nervous rotation [67–74], twinkle functions [75–79], bone restoration [80–83], muscle condensation[84–86], and trauma mending independently [87–89]. The neurotic system, cardiac, and supplementary tendons are electro-active napkins organs of mortal anatomy. In this line, the neurotic system possesses unrivaled charged exertion that transmits cues through nerve cells to targeted corridor via neuronal junction. Myocardial cells are trendsetter corpuscles of the cardiac which function to dispatch metrical stimulants. The metrical ions encouragement spread via the whole cardiac system ultimately arrives at the alveolar muscle tissue, next is automatic exertion, which pumps the heart. Skeleton and skin utilize electrical fields as well as magnetostrictive to restore fresh tissues [64]. Internal biomagnetic cue is among most apropos signals deciding towel activity in electro-sensitive towels thereby perform significant function in towel restoration operation [63].

Figure1: Electronic movement in the human anatomy

Pulpits for Towel Restoration

Pulpits manufactured by electrospinning

The manufacture of ultrafine (nanometer) fibers by charging and ejecting a polymer melt or solution through a spinneret under a high-voltage electric field is an advanced technology. Using electric field on aeroplane thick and elastic liquid, superfine filaments (having compasses varying between few very small to knockouts of very tiny dimensions) assembled by proposition stationary electric charges aversion [5, 65]. Through altering the twisting variables, gathering processes, arrangement, constitution of deduced tiny fibers are regulated, to the extent that the tiny fibers attain the asked automatic stiffness grasping orientation mastery of corpuscle geste that are employed in towel manufacturing [6, 10]. Man-made polymers, like poly (caprolactone), poly (lactic acid), and poly (lactic-co-glycolic-acid) and innate plastics, similar as fibrous protein, pectin, chitin, and silk are considerably manufactured by electrospinned innovation for towel reconstruct or restoration. Whilst immingled with charged pique, dual typical kind of charged smart tiny fibers are estimated (a) electrically transmitting tiny fibers and (b) magnetostrictive tiny fibers. Expiring from the conveying or magnetostrictive tiny fibers, harmless intelligent widgets like biosensors, medicine delivery bias, very tiny generators are advanced to foster form of heart, whim-whams, skeleton, and rind, among others.

Electrically transmissive tiny fiber pulpits are developed embedded in different types of substrates varying from transmitting plastics, like polyaniline, polypyrrole, and poly-3,4-ethylenedioxythiophene corroborated in poly (styrene sulfonate) with carbon-grounded  tiny materials, like graphene, oxide of graphene, reduced graphene oxide, and carbon nanotubes, besides mineral nanoparticles. Polyaniline is among the loftiest favorable transmitting plastics having quality non-toxicity externally at the same time not inspiring seditious responses internally [91–93].Carbon-grounded nanomaterials typically manifest exceptionally elevated conductivity, increased light-heat and mechanical charactristics, yet questionable non-toxicity. Transmitting plastics can be straightforward electro-twisted to electrically transmitting tiny fibers by modulating the electro-twisting variables, a runner plastic are blended with the transmissive plastics to enhance the electro-twisting eventuality. Once the rate of polyalinine to pectin is 6:4, the transmissibility of tiny fibers made by electro-twisting becomes 21mScm-1 [94]. Different procedures to make transmitting tiny fibers are to incorporate transmitting nanomaterials into the plastic template via doctoring or face revision with transmitting plastics, essence tiny particles and carbon-grounded tiny materials.

Piezoelectric biological materials could attain electroautomatic change, converting auto energy into electro energy not having any outside energy source [95–97]. Alongside other piezoelectric accoutrements, upon the operation of a force through the orientation of the piezoelectric measure of the tiny fibers, deciduous excitations are produced by two facing shells of accoutrement, wherein face eventuality is created. Responding to intra stress like tendon compression [98], corpuscle adhesion pressure [99], and surface stimulants similar as sonography, automatic climate, and so on [100-104], magnetostrictive nanofibers convert electronic to natural network unchanged, fused with graces that can induce biophysico- and biochemical signals, fashioning and encouraging in towel rejuvenescence. Piezoelectric plastics employed in fabrication of tiny fibers via electro-twisting comprise poly (vinylidene fluoride) and its triblock, similar to poly (vinylidene fluoride-trifluoroethylene), Poly (l-lactic acid), poly (β-hydroxybutyrate), poly (3-hydroxybutyrate-3-hydroxyvalerate), certain innate plastics, like fibrous protein, silk, and chitosan. Notwithstanding the fact that, piezoelectric polymers retain superior inflexibility and further respectable biocompatibility, their below par piezoelectric properties beget insensitivity to mechanical stimulants, that restricts their operations. The magnetostrictivity of plastic substantially hinges on the structural order of the magnetostrictive demitasse stage. Thus, through answering the plastic result with tiny materials like carbon nanotubes and graphene, elongating, or centralizing the tiny fiber layer, the ordered region of the magnetostrictive phase can be enhanced as a result the general magnetostrictivity of the layer [105]. Nonetheless, the improvement is confined. The doctoring of non-lead piezoelectric brittle tiny materials mainly enhances the magnetostrictive features of the layer. Barium titanate, lithium niobate, zinc oxide, gallium nitride, and boron nitride are examples of typical bone composites materilas.

Applications of Electroactive scaffolds (Electrotwisted Nanofiber) in Towel Manufacturing

Cardiac rejuvenescence

Myocardial necrosis can affect in weakened cardiac function, creating a significant waste of cardiomyocytes. Waste cardiomyocytes are restored by different stingy towel, and followed by irregular twinkle. The narrowing geste of cardiomyocytes is modulated by the changing electromechanical terrain. Therefore, electroactive electrospun nanofiber pulpits are regarded as an over-and-coming volition in heart towel manufacturing. The single axis oriented fiber line-up emulates shape of innate muscular tissue of the heart, and the electrical stimuli layer can follow the electronic-cue-cede address of cardiomyocytes to ameliorate the modernized compression. The reduced graphene-oxide/silk fibroin electrotwisted nanofibers could bear the aligned stretching of cardiomyocytes having rod-like shape and acquainted myofibril arrangement, permitting product of aligned heart towel form having fresh strong compression pressure [33]. By the operation of external EF to a tiny fiber altar dressed in heart corpuscles, a greater development towel form can be created with substantial proteins connected to tendon compression and electro-automatic pairing.  Exertion of a tiny fiber altar the heart towel form substantially influenced by the electronic transmittance. Invigorated rodent cardiomyocytes show optimum wobbling accomplishment on a fiber covering made with fibrous protein 9.89%, hyaluronic acid 1.1%, and polyaniline 1.34% [31]. Aligned polycaprolactone arresting nanofiber altar enclosed in poly (vinylidene fluoride-trifluoroethylene) does only ameliorate a cling of heart corpuscles, but save some corpuscle growth rate, the pulsating of cardiomyocytes and accelerating their development [106].

Curing Nervous Injury

A suitable strength of electronic excitement could boost neural expansion and nervous isolation of somatic stem cells ameliorates incarnation in whim-whams-linked polypeptides that probate whim-wham rejuvenescence. Taking into account the electrical properties of biological cells and tissues frame of the neurons, an applicable electroactive electrospun nanofiber pulpit should possess charged attributes with particular structural parcels directing corpuscular geste while ameliorating nervous enterprise. A whim-whams pointer pipe applied viaduct links conterminous side boundaries injured jitters mending girding whim-wham injury. Whim-wham channels bestowed with electrical exertion have a superior remedial result [106,107]. The movement, increase, medullated incarnation of the sheath-definite gene of neurilemma cells on poly (L-lactic acid-co-epsilon-caprolactone) tiny fibers covered by reduced graphene oxide are remarkably bettered [108]. Electronic agitation also fosters the nervous isolation of catecholamine cells on propagating pulpits. Non-graphene carbon embedded on electroactive electrospun nanofibers can boost rejuvenescence of rodent numbness whim-whams crack in issues similar to self surgical procedure. Poly (pyrolidone) applied as covering on electrotwisted poly (lactide-co-epsilon-caprolactone) pulpits. Upon current agitation with 100 mV/cm rejuvenescence in injured rodent numbness whim-whams were stimulated; whim-wham propagation haste with side emulsion tendons exertion prospects was enhanced [108].

Electroactive electrospun nanofibers are used to restore vertebral column crack through enhancing nerve fiber stretching and neural cell reopening. As propagating poly (pyrolidone) is invested with poly (lactic acid) tiny fibers, varied to separating order, the propagating tiny fibers displayed greater twenty-one-point Basso, Beattie, and Bresnahan bare-field movement class bettered electrical properties of biological cells affair in bisected rodent vertebral column facsimile [109]. Whim-whams cytokine are added to micro-patterned propagating nanofiber pulpits as biogenic signals. During electronic perturbation, arrangement and charged signals interactively stimulate the increment, straight nervous isolation of non somatic cells enhancing neural stretching [54]. Magnetostrictive plastics are employed in modulating direction of nervous and neural projection devoid of outside power roots [110,111]. Altering microstructural features of the electrotwisted piezoelectric filament pulpits poly (vinylidene fluoride) and poly (vinylidene fluoride-tetrafluoroethylene), give further broad automatic transformation and electronic parcels rearward origin controls. By modulating corpuscle exertion, that influences structure, shape and automatic transformation prompts [112], pressure filaments whim-wham corpuscles is produced actuated serine protease inhibitor E1 (SERPINE 1) fissile restriction, egging bettered nervous isolation. Outside electro-fiber applied harmless system give electronic excitation as remedy for cerebrum damage and brain degeneration affections [113]. The control viscosity period for electronic excitation and growth ages of brain neurons, furnish variations in the nervous feedback to the eletrofibers [114]. Presently, the operations for blended charged excitation in cerebrum injury rectifiers are scarce, are implicit or intriguing exploration theme in time to come.

Piezo–and Magneto-Active Biomaterials and Structures

Electroactive plastics like poly (vinylidene fluoride)  and poly (L-Lactic acid) are being reused into pulpits with different shapes and sizes, similar as microspheres [115,116], membranes [117-119], filaments [120-122], and three dimensional (3D) pulpits by colorful ways [123] like electronic spray, chemical casting and electrotwisting procedures (Fig. 2).Lately, attempts are concentrated on elaborating magneto-active biomaterials via the addition of glamorous patches for towel engineering [124]. Pulpits embedded on microspheres have gained surging cognizance for biomedical operations and boost for cell growth isolation [115, 125]. Piezo- and magneto-active microspheres can be synthesized by various processes like phase detachment or rush, conflation/chemical dissipation and electronic spray [115]. Difference in manufacturing parameters substantially permits mastery of flyspeck area and volume dispensation. Poly (vinylidene fluoride) small spheres with an unrough face a mean periphery ranging 800 nanometer up to 7 micrometer are achieved via electronic spray process, wherein small spheres made employing plastic result to an adequately transmitting liquid [115, 126]. In electronic spray procedure, counting result variables similar as result engrossment, viscidity, exterior pressure the manufacturing variables including inflow frequency, syringe periphery, gap of syringe to stockpiler, and enforced potential difference, constant charged spurt run down to driblets, proceeding small spheres of colorful sizes [127]. The approach master lapses linked to traditional flyspeck-creating strategies like liquid casting, sole and dual conflation, spray-wilting, pervious glass layer commingling, and agglomeration [127]. Skimp researches describing poly (vinylidene fluoride) and poly (l-lactic acid) magneto-active microspheres.

Fig. 2: (a) pristine (b) hypnotic poly (l-lactic acid) tiny spheres gotten from oil-in-water dispersion (c) arbitrary and (d) directed poly (l-lactic acid) filaments achieved via electrotwisting; 3-dimesional poly (vinylidene fluoride)  scaffold gotten  via (e) liquid casting/Sodium chloride particle seeping, (f) liquid casting and polyamide scaffold and (g)ice evocation.

Magneto-active poly (vinylidene fluoride) PVDF microspheres gotten via this process implanted magnetostrictive patches like cobalt ferrites (CoFe2O4) nanoparticles into the poly (vinylidene fluoride) circular mold primarily in the beta-phase (around 65-85 percent) [126]. It is noteworthy that electronic spray disallows a precise mastery of the circular dimension [128]. In a conflation-liquid birth/disappearance process tenable to achieve biodegradable piezo- and CoFe2O4 compound PLLA-grounded microspheres with manageable size and compasses gauging from 0.16 to 3.9 micrometer for pristine poly (l-lactic acid) PLLA and between 0.8 and 2.2 micrometer for compound microspheres [128]. Specifically for nervous and tendon operation, towel engineering stringy pulpits are fabricated for reinforcement, direct lengthwise corpuscles distention via the raw arbor in development [129]. Aligned and regular electronic twisted filaments having atomic severance dimension, compactness and large volume coverage are achieved via electronic twisting, identically with electronic spray process, where result viscidity is extensive (ranging from 650–2500cP) [130]. The electrospinning system makes for effectively achieving PVDF and PLLA irregular and aligned filaments employing a static and a rotating collector, independently, with a mean compasses gauging from ~500-900 nm [122, 131]. As stated by [123], PVDF irregular electronic spun filaments depict a beta state volume about fifty percent. Raising gyration rate of gatherer from 500-2000 revolutions per minute bit of beta state surges gauge from 50-85 percent owing to larger distending spurt in the electronic twisting system. Also, an objectification magnetostrictive tiny particle into the plastic PVDF result permits the manufacturing of magnetoelectric filaments with a mean fiber periphery of ~325 nm [132]. As stated by [133], counting by liquid and electronic spun production variables, likely alter current ordered state creating filaments primarily conforming of alpha or trans-state beta or gamma states. The techniques in crystallization of PVDF simply in the beta state are achieved via great potential difference or high extension rate spurts revolving gatherer. Besides, the manufacturing environments and liquid employed affect the regular bit and certain features like filament mean periphery, definite surface volume, surface forces and automatic attributes [122, 133].

3-dimensional pervious pulpits have been achieved via solvent casting/swab filtering, state uncoupling, fume raging, solid film, rush or conflation snap–desiccating [123]. Principal edge of the severance connected pulpits is connected to capability in accelerating bettered commerce of corpuscles and napkins, movement of biogenic substances, aliments and a suitable vehicle of biochemical/mechanical and or robotic signals performing to the perturbation of both corpuscles and napkins [123]. Electro-active beta-PVDF 3-dimensional pulpits having colorful pervious shapes, infrastructures severance interwoven are gotten via liquid casting/particle filtering of 300-400 micrometer and employing polyamide pattern approx 60-150 micrometer. Besides, indurate birth processes using a polyvinyl alcohol model boost elaboration of spongy platforms with means compasses of approx 300-500 micrometer, which is the pervious mean compasses similar span in oblational substance. Therefore, difference in ratio of swab in result to distance in fibers patterns permit to regulate the severance dimension of the template [123]. An identical process, similar as solvent-solvent state separation in snap birth applied to reuse of poly (l-lactic acid) pulpits connected severance size gauging range 20-60 micrometer [134].

Towel Manufacturing Rooted in Piezo-Magneto-Active Biosensors

Smart plastics are employed in diverse towel engineering operations like bone, neural and muscle napkins [135]. Specifically, piezoelectric and magneto-active plastics are applied for colorful shapes in varying corpuscle category. Still, preponderance investigations are carried out for stable atmosphere. The piezoelectronic-magneto-active influence is demonstrated in potent environments (any of automatic or electrical) is used as shown in Table 1, or differently, the appropriateness of accoutrements and importance in face barge, as the substrate is paddled.

Poly (vinylidene fluoride) PVDF and its combinations is a synthetic plastic majorly employed in towel engineering operations owing to their higher piezoelectric feedback. Especially, in inquiries reporting corpuscle feedback in changing excitations apply PVDF as buttressing material for cell increase and isolation. Rodrigues and coworkers presented beta-PVDF appreciatively ionized flicks produce a favorable terrain for perfecting the elaboration and isolation of scapegoat gist corpuscles osteoblast in changing environments, demonstrating a perfect buttress for sowing and growth in allied cells in the direction of a sought expression [136]. A compound of biological, chemical and ordinary stimulants pilot promising procedures in biognosis media residing in corporeal anatomy. Ribeiro and coworkers demonstrated PVDF excess electron flicks [137] in changing environments, further fitly automatic excitations, led bettered osteoprogenitor cells isolation in mortal mesenchymal stem cells, established for advanced salty enzyme exertion [138]. Before poly (vinylidene fluoride) flicks, precursors of bone-forming cells displayed various reactions. Before appreciatively ionic beta-poly (vinylidene fluoride) flicks in automatic stimuli, larger bone-forming coupling and increment were noticed [139]. Results are established with internal studies of beta-poly (vinylidene fluoride) flicks are bedded in a skeleton fault, exhibiting remarkably further excrescence check on skeleton redoing. Then, automatic conjurations achieved via rodent migrations [140]. Farther magnetostrictive plastics are employed similar to native protein whereby inquiries showed three-dimensional specimens automatically extended boosted increase and isolation in mortal bone-forming precursor cells owing to swell in protein expression connected with prior and tardy phases in bone-forming isolation [141].

In relation to whim-whams rejuvenescence revealed poly (vinylidene fluoride) and poly (vinylidene fluoride-trifluoroethylene) in changing environments accelerate cell increase and isolation. Antedating investigations [142] showed paddled poly (vinylidene fluoride) raises chance in discerned nerves of rodent neuroblastoma corpuscles in dissociate nervous dimensions ensuing 96 hours of cell growth in both substrate environments. The issues were substantiated using poly (vinylidene fluoride-trifluoroethylene) [142] in addition to blends. Consequently, whim-whams progenitor cell dressed in poly (l-lactic acid) nanofibers with polyaniline brought about enlarged neural protrusion upon electronic excited at same time analogous to cells cultured in non-excited pulpits. Guo and coworkers noted polyurethane and poly (vinylidene fluoride) made via electronic spinning had effect in crack remedial. Upon stimulation of cells using piezoelectric influence, the bonding of the macrophages was bettered as a consequence, advanced protein expression degrees rather than guide pulpits was manifested [143].

New strategies for towel engineering operations are attained in biological materials with magneto-active feedback. An inquiry was formed in precursor bone-forming cells and magneto-active Terfenol-poly (vinylidene fluoride-trifluoroethylene) blends. The biological materials enhanced approximately 25% of cell increase upon the cells dressed in automatic and electronic stimulation a bit actuated via operation in different glamorous area. In tendon rejuvenescence formerly demonstrated the superficial current bettered cell production [144]. Nonetheless, to date, research in changing environments with piezoelectric biosensors is scanty.

Table 1: Biomaterials, cell growth conditions, cells employed in various utilizations

| Biosensor | Environments | Cells | Applications | References |
| --- | --- | --- | --- | --- |
| Polyvinylidene fluoride cationic poled | -Automatic excitation -Automatic excitation in vertical vibration -Frequency = 1 Hz -Amplitude approx. 1mm | Cow marrow MC3T3- E1 Precursor bone-forming cells | Bone | [136] [139] |
| Polyvinylidene fluoride Anionic poled | -Automatic excitation in vertical vibration -Frequency = 1 Hz -Peak amplitude approx. 1milimeter | Human Adipose stem |  | [138] |
| Terfenol-D/P(VDF- TrFE) | -Magnetic stimulation; -Active time = 16 h (10 min of active time and 20 min of repose time); -Non-active time = 8 h; -Frequency = 0.3 Hz; -Displacement of permanent magnets ≈ 20 mm; -Peak value = 230 Oe; -ME voltages = 0.115 mV. | MC3T3-E1 pre-osteoblast |  | [141] |
| Collagen Type 1 | -Stretched cyclically along the long axis -Frequency = 1 Hz -Magnitude = 10,000 μstrain (1%) -Number of cycles = 1800 -Time = every day for 30 min over a period of 3 weeks. | Human osteoblastic precursor |  | [141] |
| PVDF and PVDF-TrFe | -Sinusoidal output (vibrational forces); -Maximum voltage ≈ 2.5mV; -Frequency = 1200Hz -Standard incubator shelves | Mouse neuroblastoma | Nerve | [142] |
| PLLA/PANI | -A silver electrode and a platinum electrode were inserted to opposite ends of the nanofibrous scaffold; -Constant voltage = 1.5 V; -Time = 60 min; -Electric field = 100 mV/mm. | Nerve stem cells |  |  |
| PU/PVDF | -Intermittent deformation of 8% -Frequency = 0,5 Hz | NIH3T3 | Wound therapeutic | [143] |

Stimulants Responsive scaffolds

A general discernment is that towel manufacturing pulpits would copy native living intercellular matrix, enjoying similitude to a doable extent to the ingrain napkins they′re supposed to restore with regard to chemical constitution, shape, material and mechanical features, in addition to bioabsorbability and environmentally-friendly. Completely, introductory prerequisite, bears to be considered in altar designing include altar biocompatibility, suitable declination period in situation of environmentally-safe substances, attending of interlinked vents in a suitable proportions, altar consistence, automatic features, and comfort in operation in a clinical approach [145, 146].

A prominent extracellular matrix is a veritably active structure that is continually renewed through enzymatic or non-enzymatic approaches, with molecular factors put through multitudinous variations. Nevertheless, most of the latest artificial pulpits persists non-resistant meaning non-incitement reactions to outside exchange of terrain (fixed pulpits) [147]. Likewise, traditional static pulpits, still conductive, substantially undo the traditional prompting channels, owing to the durability for prompt transmission. Therefore, a dire demand for intelligent, stimulants reactive pulpits which could produce and convey the bioelectronic cues analogous to traditional napkins for applications in physiological roles is needed. Magnetostrictive substances can produce electronic prompts in reaction to the administered force, palmed indeed through adhesion and movement of cells or anatomical displacements [148]. Employing magnetostrictive substances in towel manufacturing pulpits permits electronic activation devoid of electrodes outside fount of current and bedding batteries. Similar pulpits should have acceptable construction and automatic features to boost cell adherence, production, and isolation. Dimension of holes must be manageable and regulated so as to allow prolixity of the metabolite, likewise material cell adherence to the biosensor. A void bit of 90% with severance dimension of 10–100 micrometer appears to be respectable for neural development. Pulpits designated for 85–90% void bit are gotten via electronic spinning approach [149]. Said opening described is boosting cellular movement and regulated prolixity of corpuscles, metabolites, and substrate are essential to cells association, isolation and durability [150,151].

Penetrating anal tar which is bioabsorbable, environmentally-safe, transmitting, and vulnerable to disease are giving neural protrusion legion undertaking [152]. Prosperous whim-whams rejuvenescence needs towel finagled pulpits for automatic buttress in developing nerves interference in-growth in stringy blister napkins, as well as to dispatch natural suggestions to direct nerve fiber sprouting cone to the side trudge. Generally, plastics are those accoutrements mainly employed in producing respectable pulpits for nervous towel [153].

Application of Piezo-magneto-active Biosensors in Nervous Towel Manufacturing

Ferroelectric polymers

Ferroelectric materials such as piezoceramics were the dominant class of polycrystalline structures to be investigated. Foremost operations told as far back as 1950, and later, were considerably implemented in assiduity [154]. Wersing and coworkers [155] performed settler exploration of pervious ferroelectrics, in addition offered the fundamentals in the thesis and inchoate measures [156]. At present, high demand for non-lead ferroelectric accoutrements, yet a major experimental pottery is yet to be set up for lead zirconate titanate. Rodent cortical nerves dressed in Lead Zirconate Titanate presentations carpeted in poly-L-lysine extend markedly lengthier nerve fibers, in malignancy of reduction in cell quantity. Also, the frequence and breadth of the stimulative nerve impulse drifts surged, inferring that piezoelectric effect could have increased nervous exertion [157].  Importance alludes that piezoceramics is employed for clinical operations, particularly therapeutic selectors, converters, and pointers. Owing to antipathetic responses, ferroelectrics are not applied with perfect result in therapeutic devices. An ingenious structure for curative exercises is complex grounded in plastic substrates, having earthenware paddings, in form of filaments [158-160]. Achieving skeleton sickness reconstruct, Lopes et al. [161] added barium titanate nanoparticles into plastic substrate that touched off kindly tall voluntary emission. Likewise, the structure is defined by lower weakness employed as electro active pulpits [162].

Barium Titanate

A foremost ferroelectric corollary pottery exhumed in purification of barium titanate resulting in expansive application of the compound type in pulpits specifically in curative operations [163,164]. Piezoceramics set up using barium titanate show reduced toxin juxtaposed against lead confirmed ferroelectric accoutrements. The inordinate strain properties included maturity of delved class of piezoceramic. Barium titanate nanoparticles displayed the property of not being harmful to a cell with higher concentration 100 microgram per milliliter [165]. Ciofani et al. [166] showed poly (lactic-co-glycolic acid) pattern combined barium titanate nanoparticles reinforces the cell production and appendage of bone cells and bone formation. Besides, the addition of barium titanate nanoparticles into the plastic pattern enhances the automatic features combined altar [167] and stimulates biotic exertion in towel manufacturing operations [168].

Boron Nitride

Boron nitride embedded nanoscale particles constitute a considerable part of molecular manufacturing caused by conductance, automatic strength, and large heat stability [169, 170].  Popular boron nitride ferro-accoutrements in the confines of nanotubes are higher cell-friendly can be applied in towel manufacturing [171] and healing execution, owing to cumbersome ferroelectric features [172-176]. Research demonstrated that boron nitride nanotubes showed promising impact on cells fixation [177]. Of all the features boron nitride nanotubes the ferroelectricity is the most outstanding in applications as nanovectors to convey electrical and automatic suggestions inside tissues [178].

Zinc Oxide

Zinc white embedded ferroelectric is considerably utilized owing to the lopsided six-sided wurtzite shape and charge demitasse face, set up operation as piezoelectric nano generators, performing from the ease of fabrication [179]. Zinc white with a nanostructured morphology is bioabsorbable [180]. It is proffered that with zinc white shape the degree of toxicity to tissues expands affecting the degrees of oxidations lowers the chondriosome eventuality, causing production of cytokines in human cells. Likewise, it is shown that actinic revision could hamper toxin swinging a means for application in bioengineeering operations [181, 182].

Piezoplastics

A ferroelectric plastic is a kindly current group of accoutrements permitting conformation in electronic dissipations upon automatic activation without redundant power supply or electrodes [183, 162]. Similarly, is veritably vital in bioengineering perspective, plastics attain conditions of bioabsorbability and environmental-friendliness veritably critical for novel class of devices for renewing drug [184, 163]. Also, their huge merit is the veritably large manufacturing pliability distinguishing it from other man-made accoutrements [185].

Synthetic Polymers

Polyvinylidene Fluoride

In the midst of multitudinous piezoelectric polymers, PVDF is extensively delved, principally as a result of its large piezoelectricity, process capability, favorable actinic impedance, heat unchangeability, and bettered automatic features juxtaposed to certain ferroelectric plastics. Poly (vinylidne fluoride) lives no lower than 5 lucid multitudinal phases the beta-phase exhibits topmost ferroelectricity attaining 20 pC/N [186, 187]. Poly (vinylidene fluoride) plastics might assume different chain configurations and distributions of trifluoroethylene molecular polarity, giving rise to colorful net dipole moments [89-94]. An important electric moment in the poly (vinylidene fluoride) monomer unit results in the buff tendency to attract electrons toward fluorine tittles compared to hydrogen tittles. In a situation where plastic repeat units are arranged as chargers forming resemblant polarity, demitasse possesses an integer resultant dipole moment. Such atomic positioning is typifies beta, gamma, and delta phases, the initial flaunting the highest dipole moment, owing to the opposite arrangement. In certain chain arrangements: TGTG- and T3GT3G-, resemblant polarity moment configurations, delta and gamma phases, independently, results in reduced opposition; situation identical arrangements, anti-parallel chain polar configurations results in zero resultant polar moment observed in alpha and epsilon phases [188].stop

The piezoelectric effect of poly (vinylidene fluoride) is state motif reliant pivoting on the manufacturing parameters. Attaining specific demitasse state is doable via different tracks, containing viscous result ossification, heat treatment at elevated strain, mechanical trace, or electrical purifying.  Actuality of polar state is veritably necessary, specifically, owing to biomagnetism effect of the excitation of the neurotic organization, having eventuality to productive towel rejuvenescence [189, 190].  Regarding the maximum polar beta-state is achieved in this case, by heat treatment in veritably elevated strain from the alpha-state, by soaring at a veritably towering electrical field from the alpha- or delta-state [191] by stretching from the gamma-state [192]. Concerning increase in concentration of polar states, numerous procedures are described: melt-resolidification [193], soaring in a towering electric field [194], using elevated strain [195], automatic drawing [196], objectification of minute particles, graphene, and minute wires [197].

Need for poly (vinylidene fluoride) in piezoelectric pulpits for towel manufacturing necessitates operation in production styles ensuring correct shape and towering polar state lading accountable for elevated piezoelectric effect [198]. Among encouraging product styles satisfy hypotheticals inthe electrotwisting process. Multitudinous reporting are committed to electrotwisting of poly (vinylidene fluoride) nanofibers result [199], deciding the influence of manufacturing conditions on shape and features of nanofibers and the attributes of knitting nanofiber [200].  Content of the beta-state in poly (vinyliedene fluoride) is estimated in the viewpoint of adapted potential and revolution rate of the rotational gatherer. The gatherer revolution rate links to the automatic change in shape studied to advance conformation of the polar state [201]. Liu et al. [202] developed nanofibers having colorful revolution spets in gatherer of 900, 1100, 1300, 1500, 1700 and 1900 revolutions per minute. X-ray diffraction revealed a maximum at 20.6–20.9oC combined with the beta-state whereas the alpha-state peaks dissolved; attained piezoelectric poly (vinylidene fluoride) filaments anatomic periphery, indeed face structure, suitable beta-state haste of 1900 revolutions per minute. Current studies bolster perspective rising to the circular speed of the gatherer prompts at greater volume of the piezoelectric beta-state [203-205].

The water repelling character of poly (vinylidene fluoride) is a complicated matter in nervous towel production. As a way to alleviate this, colorful studies were performed. As a means to ameliorate the insolubility in addition to the automatic and electronic properties, poly (vinlyidene fluoride) was changed by mixing of divergent nanomaterials: nanoparticles [206-208], inorganic nanoparticles [209,210], nanotubes [211], by objectification of colorful plastics including polyethylene glycol [212] and polyvinyl alcohol [213]. Inclusion of nanoparticles substantially mineral types enhances actinic, material, and optical attributes [214], although diamond nanoparticles show remarkable effect in cancer cell structure [215].  Addition of nanostructures into plastic piezoelectric altar clearly impact whim-whams towel. Also, revision of face enlarges the nervous dimension and amount of coupling associations [216, 217].

A study [218] estimated the piezoelectric pulpits’ prospective for stimulating artificial nervous isolation in mortal nervous progenitor cells, hence displaying felicitousnessin nervous towel manufacturing. The authors [218] prolonged the examinations by using automatic fluctuations, during producing electronic fields impelling piezoelectric effect in ferro-polymers. The mobilization of the magnetosrictive influence is fulfilled via opting for several means of automatic activation, similar as oscillating plates, vibration, and sonography [219, 220]. Another study [221] estimated the effect of the magnetostrictive poly (vinylidene fluoride) matrix in buttressing nervous isolation in changing activation. Issues demonstrated applying unhearable waves are acceptable in inciting division of magnetostrictive poly (vinylidene fluoride) wastes crowned isolation catecholamine cells. Magnetostrictive poly (vinylidene fluoride) controls nervous isolation and neural bulge in rat cancer cells [221]. Electric fields are proven in controlling development and orientation of nerves artificially, since the electronic field is produced through terminals [222]. Certain examinations are described favorable nervous activation for multitudinous magnetostrictive structure, substantially magnetostrictive micro- and nano-filaments [223,224].

The demonstration of the prolonged period operation of magnetostrictive activation on nerves prompts the amount, dimension, and branching of nervous cells regarding non-activation circumstances.  Influences on neural rejuvenescence are not seen in oscillations applied to non-magnetostrictive accoutrements such as automatic pique of nerves [225-227].

Poly (vinylidene fluoride-trifluoroethylene)

Amid the magnetostrictive substances poly (vinylidenefluoride trifluoroethylene) displayed topmost depolarizer attributes having piezoelectric measure of 30 pC/N [228]. Poly (vinylidenefluoride trifluoroethylene) pattern the beta-state via copolymerization in the absence of automatic extension or delineation [229]. In case of fresh heat treatment, automatic delineation, or electronic poling, it's doable to greater swell the crystal clear natureand arrangement of the CF2 dipoles, therefore converting greater piezoelectricity in discrepancy to homopolymer poly (vinylidenefluoride), hinging on trifluoroethylene concentration [230]. Electrotwisted poly (vinylidenefluoride trifluoroethylene) stringy pulpits demonstrated increased pellucid and beta-state concentration in discrepancy to forming grease paint substance for nervous and skeleton towel manufacturing [101-104]. Poly (vinylidenefluoride trifluoroethylene) and barium titanate piezoelectric compound layer are described as charge creator to stimulate skeleton rejuvenescence [106].

Poly (vinylidenefluoride trifluoroethylene) piezoelectric stringy pulpits are employed in probing effect on nervous reconstruct. Several studies described favorable effect in poly (vinylidenefluoride trifluoroethylene) pulpits in whim-whams cell development and isolation [231]. Lee et al., [114] produced a poly (vinylidenefluoride trifluoroethylene) piezoelectric electrotwisted altar in colorful exposures of filaments, scattered and ordered. It is proved that the altar in ordered filaments gave a loftiest eventuality in nervous towel manufacturing, substantially in neural protrusion of rear source ganglion neurons. It is noticed that poly (vinylidenefluoride trifluoroethylene) pulpits stimulate conformation of mature nervous corpuscles showing neural-suchlike features as ordered filaments support primary nervous elongation guiding the nervous protrusion [232].

Whim-whams direct channels are assembled using poly (vinylidenefluoride trifluoroethylene) for nervous rejuvenescence [233]. In this exploration, paddled (negatively charged and appreciatively charged) and unpoled channels were employed. After the duration of four weeks, it was noticed that the appreciatively paddled channels spiked the number of regenerated jitters. In tendon rejuvenescence, the charge at the fringe of poly (vinylidenefluoride) flicks controls the corpuscle increase [234]. Still, till date, investigations with specific changing situations for piezoelectric poly (vinylidenefluoride trifluoroethylene) with automatic or electronic activation are yet to be carried out.

Poly (3-hydroxybutyrate-3-hydroxyvalerate)

Poly (3-hydroxybutyrate-3-hydroxyvalerate) is a hydroxyalkanoate having reduced piezoelectric effect measuring 1.2 pC/N [235]. It is a thermoplastic made by colorful bacteria as an intracellular force of carbon and energy. Poly (3-hydroxybutyrate-3-hydroxyvalerate) is also environmental-safe, bioabsorbable, and shows riotous automatic attributes, permitting application of poly (3-hydroxybutyrate-3-hydroxyvalerate) as an altar in bioengineering and as a bioelectronics [236, 237]. Poly (3-hydroxybutyrate-3-hydroxyvalerate) has an analogous piezoelectric eventuality to that of skeleton which can quicken skeleton development and mending [238,239]; hence, it can be used in the form of a compound with the incorporation of hydroxyapatite for skeleton towel manufacturing.  Poly (3-hydroxybutyrate-3-hydroxyvalerate) has delved in nervous towel fabrication, as a supporter for nervous cell development and axon dendrite polarization [240]. In the form of electrospun ordered poly (3-hydroxybutyrate-3-hydroxyvalerate) filaments, with objectification of collagen, it can be applied as a substrate for whim-whams towel production [241-24].

Poly (L-Lactic Acid)

Poly (L-lactic acid) is an environmentally-friendly and bioabsorbable plastic having a piezoelectric measuring -10 pC/N [223]. Fukada et al., illustrated that inculcation of poly (L-lactic acid) foster skeleton development in reaction to piezoelectric polarization [93]. Poly (L-lactic acid) has a configuration identical to native intracellular matrix employed as a biosensor in multitudinous bioengineering operations [245]. Ordered poly (L-lactic acid) nanofibrous pulpits carpeted with graphene oxide stimulate nervous corpuscle development [246]. Incipiently, addition of iron oxide nanoparticles contributes to extending neural besides electrotwisted poly (L-lactic acid) microfibers [247, 248].

Natural Bioplastics

Natural plastics are receiving high attention in towel manufacturing due to their environmental-safe and innocuous nature. Generally, various biological polymers show piezoelectricity. For instance, we illustrate certain polysaccharides and proteins having somewhat robust piezoelectric effect.

Polysaccharide

Carbohydrate having a piezoelectric measuring 0.10 pC/N is extensively delved traditional plastic substance. Polysaccharide is a direct homopolymer of glucose having lofty bioabsorbability [249-255]. It is used in colorful dimensions and shapes similar as layer bloodsuckers, microspheres, and unwoven, interlaced, or crocheted fabrics. Cellulose is studied in towel fabricating of skeleton [256,257], gristle [258], for network towel conformation [259], in medicine consignment system [260], as altar for developing usable heart cell repairs outside the body [261]. One of the essential derivations of cellulose is methylcellulose, showing in general respectable solubility in water, exceptionally at low temperatures, being reliant on the degree of methyl negotiation and the distribution of methoxy groups. As a whole, these data show that methylcellulose is accessible as a bioabsorbable injectable altar for reconstruct in cerebral faults [262-264]. Gelatin carpeted nanoparticles held in cellulose acetate/poly(lactic acid) pulpits demonstrated advanced cell feasibility compared to uncoated pulpits, and they conducted as whim-whams direction channel for ischias whim-whams excrescencies external and internal [265], whereas a gelatin/chitosan/PEDOT mongrel altar bettered the nervous development of immobilized cells and stimulated neural-suchlike cell bonding and production [266].

Chitin and Chitosan

Chitin is a natural polysaccharide having a piezoelectric feature with a lowered piezoelectric measure gauging from 0.2-1.5 pC/N [267]. It is a natural element of the cuticles of crustaceans, insects, and mollusks. Thus the soluble and bioabsorbable chitin is used in bioengineering operations, stimulating cell bonding, increse, and isolation [268]. Chitosan is a benign and bioabsorbable direct polysaccharide synthesized by partial deacetylation of chitin. It has been extensively studied for the product of pervious pulpits for cartilage towel manufacturing [269]. But, poor automatic attributes of pulpits made from chitosan render its clinical operation delicate. A valid procedure to surmount chitosan’s limitations is to mix it with synthetic polymers [270-273]. Skop et al. designed biocompatible chitosan microspheres for the dispatch of neural stem cells and growth factors for central nervous system damages [274]. Another platoon designed chitosan patches filled with the medicine piperine, recorded to have neuro protective prospect for Alzheimer’s complaint that explosively allocated peculiar spots of the cerebrum [275]. Chitosan nanoparticles have also been produced for intranasal consignment of healing agents to the brain [276, 277]. Ordered PCL/chitosan filaments boost PC12 cells adhesion and development, perfecting nervous extension across the fiber direction [278]. PLGA/chitosan pulpits guided neuronal isolation for surface whim-whams rejuvenescence either in vitro or in vivo [279, 280].

Scleroprotein

Scleroprotein is an organic magnetostrictive substance having a piezoelectric measure gauging from 0.2- 2.0 pC/N [281]. Study reported the operation of scleroprotein pulpits for skeleton remedial [282-285]. Also, scleroprotein-calcium phosphate blends are delved for gristle towel manufacturing [286]. In the same tone, scleroprotein-hydroxyapatite piezoelectric compound pulpits have demonstrated application in corpuscular development [287]. Scleroprotein pulpits mixed with chitosan are anatomized for fat towel rejuvenescence. Lipocytes are planted external cyto-compatibility and internal bioabsorbable pulpits is established analytically [288]. The absorbing operation in scleroprotein is surgery thus using magnetism ordered collagen gel type 1, attained through flaunting the forming collagen gel to elevated strength glamorous sphere, as padding for scleroprotein pipes. The approach is successful in miniature surface whim-whams bruises, enhancing whim-whams rejuvenescence remarkably at 6 mm whim-whams band in rodents [289] directing neural extension and neurilemma cell irruption external [290] and internal [291].

Summary and Forthcoming Outlook

Currently, intelligent accoutrements are of immense attraction to researchers and croakers, due to multitudinous openings in their applications to advancing unborn era of bioengineering bias, flash devices, and medicine shipment medium. Taking into account smart pulpits for towel reconstruct and rejuvenescence, piezoelectric substances lately are of specific concern because it convey electronic encouragement in the absence of an outside energy route. It is well known that electrophysiology suggestions generated by magnetostrictive pulpits could restore and reconstruct napkins through established channels identical to crude procedures passing through native intracellular matrix. The mixing of structure in collaboration with actinic, automatic, and electronic attributes of pulpits is vital to advance towel rejuvenescence. Electronic dipoles are specifically consummate in nervous towel manufacturing, whereby electrical vibrations could promote neural orientational projection in enthralling voids in neural towel damages. There is assurance from the viewpoint of wider operation in piezo electric pulpits as intelligent accoutrements in nervous towel rejuvenescence are of immense significance, authorizing circumventing conventional (invasive) electrical stimulation. It was demonstrated not long ago in artificial situations that distortion of the magnetostrictive pulpits through automatic or sonography activation redounded in neural elongation bettered cell attraction and production. Notwithstanding, one is informed about utmost ultramodern trials employing piezoelectric pulpits were carried out without similar stimulation, which doesn't affect piezoelectric effect preceding electronic dipoles. In such cases, smart electrons in cellular viewpoint are supplemental electrons owing lasting division connected to temporary distortion created by loss and outgrowth of connected cells. Still critical from the view point of trials using magnetostrictive pulpits copying internal circumstances in inner large-and small-contortions through external situations applying automatic (ultrasounds) anxiety permitting achieving actual piezoelectric reactions. Emerging issues in the field of piezoelectric pulpits are connected with imperishability of the plastics demonstrating the loftiest piezoelectric portions, which are poly (vinylidene fluoride) and its blends. As a consequence, scrutiny is concentrated in environmentally-friendly piezoelectric plastic similar as poly hydroxybutyrate or poly (l-lactic acid). An immersing surrogate which can be delved into with time to come is linked with compound pulpits having electro-transmitting plastic similar as poyaniline as well as piezoelectric plastic. It is demonstrated that objectification of an electro-transmitting plastic to the piezoelectric web crowned with upsurge in piezoelectric effect. This type of compound altar can be considered as logic in environment-safe piezoelectric plastic having initially vastly moderate piezoelectric effect.

References

[1] S.J. Lee, J.J. Yoo, and A. Atala. Biomaterials and tissue engineering. In: Clinical Regenerative Medicine in Urology. Singapore: Springer; 2018. p. 17–51.

[2] W.P. Mason. Piezoelectricity, its history and applications. The Journal of the Acoustical Society of America. 1981; 70(6):1561–6.

[3] R. Mindlin. Elasticity, piezoelectricity and crystal lattice dynamics. J Elast.1972; 2(4):217–82.

[4] R. Mould. Pierre Curie, 1859–1906. Curr Oncol. 2007; 14(2):74.

[5] T. Arinzeh, G. Collins, and Y.S. Lee. System and method for a piezoelectric scaffold for nerve growth and repair. In: Google Patents; 2016.

[6] M. Minary-Jolandan, and M.F. Yu. Nanoscale characterization of isolated individual type I collagen fibrils: polarization and piezoelectricity. Nanotechnology. 2009; 20(8):085706.

[7] T.L. Arinzeh, N. Weber, and M. Jaffe. Electrospun electroactive polymers for regenerative medicine applications. In: Google Patents; 2016.

[8] V.R. Shastri, C.E. Schmidt, R.S. Langer, and J.P. Vacanti. Neuronal stimulation using electrically conducting polymers. In: Google patents; 2000.

[9] C.A.L. Bassett. Biologic significance of piezoelectricity. Calcif Tissue Int. 1967; 1(1):252–72.

[10] C. Halperin, S. Mutchnik, A. Agronin, M. Molotskii, P. Urenski, M. Salai, and G. Rosenman. Piezoelectric effect in human bones studied in nanometer scale. Nano Lett. 2004:4(7):1253–6.

[11] B. Miara, E. Rohan, M. Zidi, and B. Labat. Piezomaterials for bone regeneration design-homogenization approach. Journal of the Mechanics and Physics of Solids. 2005; 53(11):2529-56.

[12] F.J. O’Brien. Biomaterials and scaffolds for tissue engineering. Mater. Today 2011, 14, 88–95.

[13] C. Ribeiro, D.M. Correia, S. Ribeiro, M.M. Fernandes, and S. Lanceros-Mendez. Piezo- and  magnetoelectric polymers as biomaterials for novel tissue engineering strategies. MRS Adv. 2018, 3, 1671–1676.

[14] S. Ribeiro, A.C. Gomes, I. Etxebarria, S. Lanceros-Mendez, and C. Ribeiro,  Electroactive biomaterial surface engineering effects on muscle cells differentiation. Mater.Sci. Eng. C Mater. Biol. Appl. 2018, 92, 868–874.

[15] J. Fraden. Handbook of Modern Sensors: Physics, Designs, and Applications; Springer Science & Business Media: Berlin/Heidelberg,Germany, 2004.

[16] C. Ribeiro, V. Sencadas, D.M. Correia, and S. Lanceros-Mendez. Piezoelectric polymers as biomaterials for tissue engineering applications. Colloids Surf. B Biointerfaces 2015, 136, 46–55.

[17] L.C. Fernandes, D.M. Correia, C. García-Astrain, N. Pereira, M. Tariq, J.M.S.S. Esperança, and S. Lanceros-Méndez. Ionic-liquid-based printable materials for thermochromic and thermoresistive applications. ACS Appl. Mater. Interfaces 2019, 11, 20316–20324.

[18] J. Jacob, N. More, K. Kalia, and G. Kapusetti. Piezoelectric smart biomaterials for bone and cartilage tissue engineering. Inflamm. Regen. 2018, 38, 2.

[19] C. Ribeiro, J. Pärssinen, V. Sencadas, V. Correia, S. Miettinen, V.P. Hytönen, and S. Lanceros-Méndez. Dynamic piezoelectric stimulation enhances osteogenic differentiation of human adipose stem cells. J. Biomed. Mater. Res.-Part A2015, 103, 2172–2175.

[20] S.W. Blume, and J.R. Curtis, Medical costs of osteoporosis in the elderly medicare population, Osteoporos. Int. 22 (2011) 1835–1844.

[21] E. Hernlund, A. Svedbom, M. Ivergård, J. Compston, C. Cooper, J. Stenmark, E.V. McCloskey, B. Jonsson, and J.A. Kanis, Osteoporosis in the European Union: medical management, Epidemiol. Econ.Burd. 8 (2013) 1–115.

[22] M.U.D.o.H. Office of the Surgeon General %J A Report of the Surgeon General.Rockville, O.o.t.S.G. Human Services, Bone health and osteoporosis, (2004) 68–87.

[23] T.D. Rachner, S. Khosla, and L.C. Hofbauer, Osteoporosis: now and the future, Lancet 377 (2011) 1276–1287.

[24] A.R. Amini, C.T. Laurencin, and S.P. Nukavarapu, Bone tissue engineering: recent advances and challenges, Crit. Rev. Biomed. Eng. 40 (2012) 363–408.

[25] G. Battafarano, M. Rossi, V. De Martino, F. Marampon, L. Borro, A. Secinaro, and A.D. Fattore, Strategies for bone regeneration: from graft to tissue engineering, Int. J. Mol. Sci. 22 (2021) 1–22.

[26] C. Ribeiro, V. Sencadas, D.M. Correia, and S. Lanceros-M´endez, Piezoelectric polymers as biomaterials for tissue engineering applications, Colloids Surf. B: Biointerfaces 136 (2015) 46–55.

[27] M.H. Shamos, L.S. Lavine, and M.I. Shamos, Piezoelectric effect in bone, Nature 197 (1963) 81.

[28] M.M. Fernandes, D.M. Correia, C. Ribeiro, N. Castro, V. Correia, and S. Lanceros-Mendez, Bioinspired three-dimensional magnetoactive scaffolds for bone tissue engineering, ACS Appl. Mater. Interfaces 11 (2019) 45265–45275.

[29] C. Ribeiro, J. Parssinen, V. Sencadas, V. Correia, S. Miettinen, V.P. Hytonen, and S. Lanceros-M´endez, Dynamic piezoelectric stimulation enhances osteogenic differentiation of human adipose stem cells, J. Biomed. Mater. Res. - Part A 103 (2015) 2172–2175.

[30] C. Ribeiro, V. Correia, P. Martins, F.M. Gama, and S. Lanceros-Mendez, Proving the suitability of magnetoelectric stimuli for tissue engineering applications, Colloids Surf. B: Biointerfaces 140 (2016) 430–436.

[31] P.K. Szewczyk, S. Metwally, Z.J. Krysiak, L. Kaniuk, J.E. Karbowniczek, and U. Stachewicz, Enhanced osteoblasts adhesion and collagen formation on biomimetic polyvinylidene fluoride (PVDF) films for bone regeneration, Biomed. Mater.14 (2019).

[32] P.K. Szewczyk, S. Metwally, J.E. Karbowniczek, M.M. Marzec, E. Stodolak-Zych, A. Gruszczynski, A. Bernasik, and U. Stachewicz, Surface-potential-controlled cell proliferation and collagen mineralization on electrospun polyvinylidene fluoride (PVDF) fiber scaffolds for bone regeneration, ACS Biomater. Sci. Eng. 5 (2019) 582–593.

[33] A. Reizabal, R. Brito-Pereira, M.M. Fernandes, N. Castro, V. Correia, C. Ribeiro, C.M. Costa, L. Perez, J.L. Vilas, and S. Lanceros-Mandendez, Silk fibroin magnetoactive nanocomposite films and membranes for dynamic bone tissue engineering strategies, Materialia 12 (2020), 100709.

[34] R. Langer, and J.P. Vacanti, Tissue Engineering, Science 260 (5110) (1993) 920–926, https://doi.org/10.1126/science.8493529.

[35] S.M. Greising, B.T. Corona, C. McGann, J.K. Frankum, and G.L. Warren, Therapeutic approaches for volumetric muscle loss injury: a systematic review and Meta- Analysis, Tissue Eng. Part B Rev. 25 (6) (2019) 510–525, https://doi.org/10.1089/ ten.TEB.2019.0207.

[36] S. Ribeiro, A.C. Gomes, I. Etxebarria, S. Lanceros-Mendez, and C. Ribeiro, Electroactive biomaterial surface engineering effects on muscle cells differentiation, Mater. Sci. Eng., C 92 (2018) 868–874, https://doi.org/10.1016/j.msec.2018.07.044.

[37] S. Jana, S.K.L. Levengood, and M. Zhang.  Anisotropic materials for skeletal-muscle-tissue engineering, Adv. Mater. (Deerfield Beach Fla.) 28 (48) (2016) 10588–10612, https://doi.org/10.1002/adma.201600240.

[38] S. Ribeiro, T. Ribeiro, C. Ribeiro, D.M. Correia, J.P.S. Farinha, A.C. Gomes, C. Baleizao, and S. Lanceros-Mendez, Multifunctional platform based on electroactive polymers and silica nanoparticles for tissue engineering applications, Nanomaterials (Basel, Switzerland) 8 (11) (2018) 933, https://doi.org/10.3390/ nano8110933.

[39] N. Shehata, M.A. Abdelkareem, E.T. Sayed, D.E. Egirani, and A.W. Opukumo, Smart Materials: The next generation, in: reference module in materials science and Materials Engineering, 2021, Elsevier. https://doi.org/10.1016/b978-0-12- 815732-9.00062-0.

[40] C. Ribeiro, C.M. Costa, D.M. Correia, J. Nunes-Pereira, J. Oliveira, P. Martins, R. Gonçalves, V.F. Cardoso, and S. Lanceros-Mendez, Electroactive poly(vinylidene fluoride)-based structures for advanced applications, Nat. Protoc. 13 (4) (2018) 681–704, https://doi.org/10.1038/nprot.2017.157.

[41] B. Hermenegildo, C. Ribeiro, L. Perez-´Alvarez, J.L. Vilas, D.A. Learmonth, R.A. Sousa, P. Martins, and S.  Lanceros-Mendez, Hydrogel-based magnetoelectric microenvironments for tissue stimulation, Colloids Surf., B 181 (2019) 1041–1047, https://doi.org/10.1016/j.colsurfb.2019.06.023.

[42] P. Hitscherich, A. Aphale, R. Gordan, R. Whitaker, P. Singh, L.H. Xie, P. Patra, and E. J. Lee, Electroactive graphene composite scaffolds for cardiac tissue engineering, J. Biomed. Mater. Res. Part A 106 (11) (2018) 2923–2933, https://doi.org/ 10.1002/jbm.a.36481.

[43] P. Gentile, V. Chiono, I. Carmagnola, and P.V. Hatton, An overview of poly(lactic-co-glycolic) acid (PLGA)-based biomaterials for bone tissue engineering, Int. J. Mol. Sci. 15 (3) (2014) 3640–3659, https://doi.org/10.3390/ijms15033640.

[44] K.K. Chereddy, G. Vandermeulen, and V. Preat, PLGA based drug delivery systems: Promising carriers for wound healing activity, Wound Repair Regen. 24 (2) (2016) 223–236, https://doi.org/10.1111/wrr.12404.

[45] C. Martins, F. Sousa, F. Araújo, and B. Sarmento, Functionalizing PLGA and PLGA derivatives for drug delivery and tissue gegeneration applications, Adv. Healthcare Mater. 7 (1) (2017) 1701035, https://doi.org/10.1002/ adhm.201701035.

[46] J.M. Lü, X. Wang, C. Marin-Muller, H. Wang, P.H. Lin, Q. Yao, and C. Chen, Current advances in research and clinical applications of PLGA-based nanotechnology, Expert Rev. Mole. Diagn.9 (4) (2009) 325–341, https://doi.org/10.1586/ erm.09.15.

[47] Z. He, F. Rault, M. Lewandowski, E. Mohsenzadeh, and F. Salaün, Electrospun PVDF nanofibers for piezoelectric applications: a review of the influence of electrospinning parameters on the β-Phase and crystallinity enhancement, Polymers 13 (2) (2021) 174, https://doi.org/10.3390/polym13020174.

[48] J.C. Middleton, and A.J. Tipton, Synthetic biodegradable polymers as orthopedic devices, Biomaterials 21 (23) (2000) 2335–2346, https://doi.org/10.1016/s0142- 9612(00)00101-0.

[49] Y. Wang, Y. Miao, G. Li, M. Su, X. Chen, H. Zhang, Y. Zhang, W. Jiao, Y. He, J. Yi, X. Liu, and H. Fan, Engineering ferrite nanoparticles with enhanced magnetic response for advanced biomedical applications, Mater. Today Adv. 8 (2020) 100119, https://doi.org/10.1016/j.mtadv.2020.100119.

[50] Y. Shen, B.O. Jiang, and Y.I. Xing, Recent advances in the application of magnetic Fe3O4 nanomaterials for the removal of emerging contaminants, Environ. Sci. Pollut. Res. 28 (7) (2021) 7599–7620.

[51] Q. Li, C.W. Kartikowati, S. Horie, T. Ogi, T. Iwaki, and K. Okuyama, Correlation between particle size/domain structure and magnetic properties of highly crystalline Fe(3)O(4) nanoparticles, Sci. Rep. 7 (1) (2017) 9894, https://doi.org/ 10.1038/s41598-017-09897-5.

[52] T.A. Quinn, Cardiac mechano-electric coupling: a role in regulating normal function of the heart? Cardiovasc.Res. 108 (1) (2015) 1–3, https://doi.org/ 10.1093/cvr/cvv203.

[53] World Health Organization, Cardiovascular diseases. https://www.who.int/west ernpacific/health-topics/cardiovascular-diseases, 2022.

[54] M. Mazzola, and E.D. Pasquale, toward cardiac regeneration: combination of pluripotent stem cell-based therapies and bioengineering strategies, Front. Bioeng.Biotechnol. 8 (2020) 455, https://doi.org/10.3389/fbioe.2020.00455.

[55] Y. Huang, T. Wang, M.E.U. Lopez, M. Hirano, A. Hasan, and S.R. Shin, Recent advancements of human iPSC derived cardiomyocytes in drug screening and tissue regeneration, Microphysiol. Syst. 4 (2020), https://doi.org/10.21037/mps- 20-3.

[56] T.C. Suh, A.Y. Amanah, and J.M. Gluck, Electrospun scaffolds and induced pluripotent stem cell-derived cardiomyocytes for cardiac tissue engineering applications, Bioengineering 7 (3) (2020), https://doi.org/10.3390/ bioengineering7030105.

[57] A. Mathew, R. Augustine, N. Kalarikal, and S. Thomas, in: Tissue engineering: principles, recent trends and the future: state of the art and recent trends, 2016, pp. 31–82, https://doi.org/10.1201/b19867-3.

[58] N.F. Huang, Big bottlenecks in cardiovascular tissue engineering, Commun. Biol. 1 (1) (2018), https://doi.org/10.1038/s42003-018-0202-8.

[59] A. Khademhosseini, and R. Langer, A decade of progress in tissue engineering, Nat. Protoc. 11 (10) (2016) 1775–1781, https://doi.org/10.1038/nprot.2016.123.

[60] P.S. Alberte, J. Vaithilingam, J.C. Moore, R.D. Wildman, C.J. Tuck, M. R. Alexander, R.J.M. Hague, and F.J. Rawson, Development of conductive gelatine-methacrylate inks for two-photon polymerisation, Polymers 13 (7) (2021), https://doi.org/10.3390/polym13071038.

[61] J. Vaithilingam, P.S. Alberte, S. Campora, G.A. Rance, L. Jiang, J. Thorpe, L. Burroughs, C.J. Tuck, C. Denning, R.D. Wildman, R.J.M. Hague, M. R. Alexander, and F.J. Rawson, Multifunctional bioinstructive 3D architectures to modulate cellular behavior, Adv. Funct. Mater.29 (38) (2019), https://doi.org/ 10.1002/adfm.201902016.

[62] K. Kapat, Q.T.H. Shubhra, M. Zhou, and S. Leeuwenburgh, Piezoelectric nano-biomaterials for biomedicine and tissue regeneration, Adv. Funct.Mater.30 (44) (2020), https://doi.org/10.1002/adfm.201909045.

[63]K. Kapat, Q.T.H. Shubhra, M. Zhou, and S. Leeuwenburgh, Piezoelectric nanobiomaterials for biomedicine and tissue regeneration, Adv. Funct. Mater.30 (2020) 1909045.

[64]R.A. Surmenev, T. Orlova, R.V. Chernozem, A.A. Ivanova, A. Bartasyte, S. Mathur, and M.A. Surmeneva, Hybrid lead-free polymer-based nanocomposites with improved piezoelectric response for biomedical energy-harvesting applications: a review, Nano Energy 62 (2019) 475–506.

[65]B.W. Walker, R.P. Lara, C.H. Yu, E.S. Sani, W. Kimball, S. Joyce, and N. Annabi, Engineering a naturally-derived adhesive and conductive cardiopatch, Biomaterials 207 (2019) 89–101.

[66]Q. Wang, M. Wu, X. Xu, C. Ding, J. Luo, and J. Li, Direct current stimulation for improved osteogenesis of MC3T3 cells using mineralized conductive polyaniline, ACS Biomater. Sci. Eng. 7 (2021) 852–861.

[67]B. Katz, and R. Miledi, Release of acetylcholine from a nerve terminal by electric pulses of variable strength and duration, Nature 207 (1965) 1097–1098.

[68]S. Ribeiro, C. Puckert, C. Ribeiro, A.C. Gomes, M.J. Higgins, and S. Lanceros-Mendez, Surface charge-mediated cell-surface interaction on piezoelectric materials, ACS Appl. Mater. Interfaces 12 (2020) 191–199.

[69]S. Farzamfar, M. Salehi, S.M. Tavangar, J. Verdi, K. Mansouri, A. Ai, Z.V. Malekshahi, and J. Ai, A novel polycaprolactone/carbon nanofiber composite as a conductive neural guidance channel: an in vitro and in vivo study, Prog. Biomater. 8 (2019) 239–248.

[70]F. Gisbert Roca, J. Mas Estelles, M. Monleon Pradas, and C. Martinez-Ramos, Axonal extension from dorsal root ganglia on fibrillar and highly aligned poly(lactic acid)-polypyrrole substrates obtained by two different techniques: electrospun nanofibres and extruded microfibres, Int. J. Biol. Macromol. 163 (2020) 1959–1969.

[71]A. Wang, Z. Liu, M. Hu, C. Wang, X. Zhang, B. Shi, Y. Fan, Y. Cui, Z. Li, and K. Ren, Piezoelectric nanofibrous scaffolds as in vivo energy harvesters for modifying fibroblast alignment and proliferation in wound healing, Nano Energy 43 (2018) 63–71.

[72]D. Kim, S.A. Han, J.H. Kim, J.H. Lee, S.W. Kim, and S.W. Lee, Biomolecular piezoelectric materials: from amino acids to living tissues, Adv. Mater. 32 (2020) 1906989.

[73]M. Seiti, P. Ginestra, R.M. Ferraro, E. Ceretti, and E. Ferraris, Nebulized jet-based printing of bio-electrical scaffolds for neural tissue engineering: a feasibility study, Biofabrication 12 (2020) 025024.

[74]L. Wang, Y. Wu, T. Hu, P.X. Ma, and B. Guo, Aligned conductive core-shell biomimetic scaffolds based on nanofiber yarns/hydrogel for enhanced 3D neurite outgrowth alignment and elongation, Acta Biomater. 96 (2019) 175–187.

[75]J. Ren, Q. Xu, X. Chen, W. Li, K. Guo, Y. Zhao, Q. Wang, Z. Zhang, H. Peng, Y.G. Li, Adv. Mater. 29 (2017).

[76]N. Adadi, M. Yadid, I. Gal, M. Asulin, R. Feiner, R. Edri, and T. Dvir, Electrospun fibrous PVDF-TrFe scaffolds for cardiac tissue engineering, differentiation, and maturation, Adv. Mater. Technol. 5 (2020) 1900820.

[77]K. Roshanbinfar, L. Vogt, F. Ruther, J.A. Roether, A.R. Boccaccini, F.B. Engel, Adv. Funct. Mater. 30 (2019).

[78]H. Stone, S. Lin, and K. Mequanint, Preparation and characterization of electrospun rGO-poly (ester amide) conductive scaffolds, Mater. Sci. Eng. C Mater. Biol. Appl. 98 (2019) 324–332.

[79]G. Zhao, X. Zhang, B. Li, G. Huang, F. Xu, and X. Zhang, Solvent-free fabrication of carbon nanotube/silk fibroin electrospun matrices for enhancing cardiomyocyte functionalities, ACS Biomater. Sci. Eng. 6 (2020) 1630–1640.

[80]A.A. Marino, and R.O. Becker, Piezoelectricity in hydrated frozen bone and tendon, Nature 253 (1975) 627–628.

[81]H. Cui, Y. Liu, M. Deng, X. Pang, P. Zhang, X. Wang, X. Chen, and Y. Wei, Synthesis of biodegradable and electroactive tetraaniline grafted poly (ester amide) copolymers for bone tissue engineering, Biomacromolecules 13 (2012) 2881–2889.

[82]B. Maharjan, V.K. Kaliannagounder, S.R. Jang, G.P. Awasthi, D.P. Bhattarai, G. Choukrani, C.H. Park, and C.S. Kim, In-situ polymerized polypyrrole nanoparticles immobilized poly (ε-caprolactone) electrospun conductive scaffolds for bone tissue engineering, Mater. Sci. Eng. C Mater.Biol. Appl. 114 (2020) 111056.

[83]H. Nekounam, Z. Allahyari, S. Gholizadeh, E. Mirzaei, M.A. Shokrgozar, and R. Faridi-Majidi, Simple and robust fabrication and characterization of conductive carbonized nanofibers loaded with gold nanoparticles for bone tissue engineering applications, Mater. Sci. Eng. C Mater.Biol. Appl. 117 (2020) 111226.

[84]T. Fu, L. Jiang, Y. Peng, Z. Li, S. Liu, J. Lu, and F. Zhang, Electrical muscle stimulation accelerates functional recovery after nerve injury, Neuroscience 426 (2020) 179–188.

[85]H.Y. Gong, J. Park, W. Kim, J. Kim, J.Y. Lee, and W.G. Koh, A novel conductive and micropatterned PEG-based hydrogel enabling the topographical and electrical stimulation of myoblasts, ACS Appl. Mater. Interfaces 11 (2019) 47695–47706.

[86]K.H. Nakayama, M. Shayan, and N.F. Huang, Engineering biomimetic materials for skeletal muscle repair and regeneration, Adv. Healthc.Mater.8 (2019) 1801168.

[87]M.J. Mulroy, D.W. Altmann, T.F. Weiss, and W.T. Peake, Intracellular electric responses to sound in a vertebrate cochlea, Nature 249 (1974) 482–485.

[88]S. Du, N. Zhou, Y. Gao, G. Xie, H. Du, H. Jiang, L. Zhang, J. Tao, and J. Zhu, Bioinspired hybrid patches with self-adhesive hydrogel and piezoelectric nanogenerator for promoting skin wound healing, Nano Res. 13 (2020) 2525–2533.

[89]P. Moutsatsou, K. Coopman, and S. Georgiadou, Biocompatibility assessment of conducting PANI/chitosan nanofibers for wound healing applications, Polymers 9 (2017).

[90]J. Xue, J. Xie, W. Liu, and Y. Xia, Electrospun nanofibers: new concepts, materials, and applications, Acc. Chem. Res. 50 (2017) 1976–1987.

[91]L. Mohammadi Amirabad, M. Massumi, M. Shamsara, I. Shabani, A. Amari, M. Mossahebi Mohammadi, S. Hosseinzadeh, S. Vakilian, S.K. Steinbach, M.R. Khorramizadeh, M. Soleimani, and J. Barzin, Enhanced cardiac differentiation of human cardiovascular disease patient-specific induced pluripotent stem cells by applying unidirectional electrical pulses using aligned electroactive nanofibrous scaffolds, ACS Appl. Mater. Interfaces 9 (2017) 6849–6864.

[92]C. Zhang, M.H. Hsieh, S.Y. Wu, S.H. Li, J. Wu, S.M. Liu, H.J. Wei, R.D. Weisel, H.W. Sung, and R.K. Li, A self-doping conductive polymer hydrogel that can restore electrical impulse propagation at myocardial infarct to prevent cardiac arrhythmia and preserve ventricular function, Biomaterials 231 (2020) 119672.

[93]G. Thrivikraman, P.S. Lee, R. Hess, V. Haenchen, B. Basu, and D. Scharnweber, Interplay of substrate conductivity, cellular microenvironment, and pulsatile electrical stimulation toward osteogenesis of human mesenchymal stem cells in vitro, ACS Appl. Mater. Interfaces 7 (2015) 23015–23028.

[94]S. Ostrovidov, M. Ebrahimi, H. Bae, H.K. Nguyen, S. Salehi, S.B. Kim, A. Kumatani, T. Matsue, X. Shi, K. Nakajima, S. Hidema, M. Osanai, and A. Khademhosseini, Gelatin-polyaniline composite nanofibers enhanced excitation-contraction coupling system maturation in myotubes, ACS Appl. Mater. Interfaces 9 (2017) 42444–42458.

[95]S. Xu, Y. Qin, C. Xu, Y. Wei, R. Yang, and Z.L. Wang, Self-powered nanowire devices, Nat. Nanotechnol. 5 (2010) 366–373.

[96]Z.L. Wang, towards self-powered nanosystems: from nanogenerators to nanopiezotronics, Adv. Funct. Mater. 18 (2008) 3553–3567.

[97]X. Wang, J. Song, L. Jin, and L.W. Zhong, Direct-current nanogenerator driven by ultrasonic waves, Science 316 (2007) 102–105.

[98]Y. Zhang, Z. Zheng, M. Yu, C. Hsu, E.A. Berthiaume, H. Pan, X. Zhang, A.Z. Stieg, B. Wu, H. Wang, K. Ting, and C. Soo, Using an engineered galvanic redox system to generate positive surface potentials that promote osteogenic functions, ACS Appl. Mater. Interfaces 10 (2018) 15449–15460.

[99]X. Zhang, X. Cui, D. Wang, S. Wang, Z. Liu, G. Zhao, Y. Zhang, Z. Li, Z.L. Wang, and L. Li, Soft acoustic metamaterials: bubble architectures for locally resonant acoustic metamaterials (Adv. Funct. Mater.51/2019), Adv. Funct.Mater.29 (2019) 1970346.

[100]R.V. Chernozem, M.A. Surmeneva, S.N. Shkarina, K. Loza, M. Epple, M. Ulbricht, A. Cecilia, B. Krause, T. Baumbach, A.A. Abalymov, B.V. Parakhonskiy, A.G. Skirtach, and R.A. Surmenev, Piezoelectric 3-D fibrous poly(3-hydroxybutyrate)-based scaffolds ultrasound-mineralized with calcium carbonate for bone tissue engineering: inorganic phase formation, osteoblast cell adhesion, and proliferation, ACS Appl. Mater. Interfaces 11 (2019) 19522–19533.

[101]A. Marino, G.G. Genchi, V. Mattoli, and G. Ciofani, Piezoelectric nanotransducers: the future of neural stimulation, Nano Today 14 (2017) 9–12.

[102]A. Marino, J. Barsotti, G. de Vito, C. Filippeschi, B. Mazzolai, V. Piazza, M. Labardi, V. Mattoli, and G. Ciofani, Two-photon lithography of 3D nanocomposite piezoelectric scaffolds for cell stimulation, ACS Appl. Mater. Interfaces 7 (2015) 25574–25579.

[103]L. Jiang, Y. Yang, R. Chen, G. Lu, R. Li, J. Xing, K.K. Shung, M.S. Humayun, J. Zhu, Y. Chen, Q. Zhou, Adv. Funct. Mater.29 (2019).

[104]D.K. Piech, B.C. Johnson, K. Shen, M.M. Ghanbari, K.Y. Li, R.M. Neely, J.E. Kay, J.M. Carmena, M.M. Maharbiz, and R. Muller, A wireless millimetre-scale implantable neural stimulator with ultrasonically powered bidirectional communication, Nat. Biomed. Eng. 4 (2020) 207–222.

[105]A.C. Wang, M. Hu, L.W. Zhou, and X.Y. Qiang, Phenanthroline-derivative functionalized carbon dots for highly selective and sensitive detection of Cu2+ and S2− and imaging inside live cells, Nanomaterials 8 (2018) 1071.

[106]P.J. Gouveia, S. Rosa, L. Ricotti, B. Abecasis, H.V. Almeida, L. Monteiro, J. Nunes, F.S. Carvalho, M. Serra, S. Luchkin, A.L. Kholkin, P.M. Alves, P.J. Oliveira, R. Carvalho, A. Menciassi, R.P. das Neves, and L.S. Ferreira, Flexible nanofilms coated with aligned piezoelectric microfibers preserve the contractility of cardiomyocytes, Biomaterials 139 (2017) 213–228.

[107]Y. Zou, J. Qin, Z. Huang, G. Yin, X. Pu, and D. He, Fabrication of aligned conducting PPy-PLLA fiber films and their electrically controlled guidance and orientation for neurites, ACS Appl. Mater. Interfaces 8 (2016) 12576–12582.

[108]J. Wang, Y. Cheng, L. Chen, T. Zhu, K. Ye, C. Jia, H. Wang, M. Zhu, C. Fan, and X. Mo, In vitro and in vivo studies of electroactive reduced graphene oxide-modified nanofiber scaffolds for peripheral nerve regeneration, Acta Biomater. 84 (2019) 98–113.

[109]R.F. Valentini, T.G. Vargo, J.A. Gardella, and P. Aebischer, Electrically charged polymeric substrates enhance nerve fibre outgrowth in vitro, Biomaterials 13 (1992) 183–190.

[110]E.G. Fine, R.F. Valentini, R. Bellamkonda, and P. Aebischer, Improved nerve regeneration through piezoelectric vinylidenefluoride-trifluoroethylene copolymer guidance channels, Biomaterials 12 (1991) 775–780.

[111]J.I. Kim, T.I. Hwang, J.C. Lee, C.H. Park,and  C.S. Kim, Springer Proceedings in Physics: Proceedings of the International Conference on “Physics and Mechanics of New Materials and Their Applications”, PHENMA 2018, Adv. Funct. Mater.30 (2019).

[112]Raynald, B. Shu, X.B. Liu, J.F. Zhou, H. Huang, J.Y. Wang, X.D. Sun, C. Qin, and Y.H. An, Polypyrrole/polylactic acid nanofibrous scaffold cotransplanted with bone marrow stromal cells promotes the functional recovery of spinal cord injury in rats, CNS Neurosci. Ther. 25 (2019) 951–964.

[113]N. Grossman, D. Bono, N. Dedic, S.B. Kodandaramaiah, A. Rudenko, H.J. Suk, A.M. Cassara, E. Neufeld, N. Kuster, L.H. Tsai, A. Pascual-Leone, and E.S. Boyden, Noninvasive deep brain stimulation via temporally interfering electric fields, Cell 169 (2017) 1029–1041 e1016.

[114]K.M. Kim, S.Y. Kim, and G.T. Palmore, Axon outgrowth of rat embryonic hippocampal neurons in the presence of an electric field, ACS Chem. Neurosci. 7 (2016) 1325–1330.

[115] D. M. Correia, R. Golcalves, C. Ribeiro, V. Sencadas, G. L. Botelho, J. L. Gomez-Ribelles and s.lanceros-mendez, RSC Adv 4 , 33013-33021 (2014).

[116] D. M. Correia, V. Sencadas, C. Ribeiro, P. M. Martins, P. Martins, F. M. Gama, G. Botelho and S.Lanceros-Méndez, J Colloid Interf Sci 476, 79-86 (2016).

[117] V. Sencadas, R. Gregorio and S. Lanceros-Méndez, J Macromolec Sci B 48 (3), 514-525 (2009).

[118] S. J. Hong, H. S. Yu and H. W. Kim, Acta Biomaterialia 5 (5), 1725-1731 (2009).

[119] V. Sencadas, S. Lanceros-Méndez and J. F. Mano, Thermochimica Acta 424 (1–2), 201-207 (2004).

[120] Z. H. Liu, C. T. Pan, L. W. Lin and H. W. Lai, Sens Actuat A 193 (0), 13-24 (2013).

[121] H. Na, X. Liu, J. Li, Y. Zhao, C. Zhao and X. Yuan, Polymer 50 (26), 6340-6349 (2009).

[122] C. Ribeiro, V. Sencadas, J. L. G. Ribelles and S. Lanceros-Méndez, Soft Mater 8 (3), 274-287 (2010).

[123] D. M. Correia, C. Ribeiro, V. Sencadas, L. Vikingsson, M. Oliver Gasch, J. L. Gómez Ribelles, G.Botelho and S. Lanceros-Méndez, Mater Design 92, 674-681 (2016).

[124] C. Ribeiro, V. Correia, P. Martins, F. M. Gama and S. Lanceros-Mendez, Colloids Surf B 140, 430-436 (2016).

[125] M. N. T.-M. R. Sobreiro-Almeida, E. O. Carvalho, L. Cordón, S. Doria, L. Senent, D. M. Correia, C.Ribeiro, S. Lanceros-Méndez, R. Sabater i Serra, J. L. Gomez Ribelles and A. Sempere, Intern J Molec Sci 18 (11), 2391 (2017).

[126] R. Gonçalves, P. Martins, D. M. Correia, V. Sencadas, J. L. Vilas, L. M. León, G. Botelho and S.Lanceros-Méndez, RSC Adv 5 (45), 35852-35857 (2015).

[127] M. Zamani, M. P. Prabhakaran and S. Ramakrishna, Int J Nanomedicine 8, 2997-3017 (2013).

[128] D. M. Correia, V. Sencadas, C. Ribeiro, P. M. Martins, P. Martins, F. M. Gama, G. Botelho and S.Lanceros-Méndez, J Colloid Interf Sci 476 (Supplement C), 79-86 (2016).

[129] M. P. Prabhakaran, L. Ghasemi-Mobarakeh, G. R. Jin and S. Ramakrishna, J. Biosci.Bioeng.112 (5), 501-507 (2011).

[130] C. Ribeiro, D. M. Correia, S. Ribeiro, V. Sencadas, G. Botelho and S. Lanceros-Méndez, Eng LifeSci 15 (4), 351-356 (2015).

[131] C. Ribeiro, V. Sencadas, C. M. Costa, J. L. Gómez Ribelles and S. Lanceros-Méndez, Sci TechnolAdv Mater 12 (1) (2011).

[132] R. Gonçalves, P. Martins, X. Moya, M. Ghidini, V. Sencadas, G. Botelho, N. D. Mathur and S. Lanceros-Mendez, Nanoscale 7 (17), 8058-8061 (2015).

[133] J. Zheng, A.He, J. Li and C. C. Han, Macromolecular Rapid Commun 28 (22), 2159-2162 (2007).

[134] L. Budyanto, Y. Q. Goh and C. P. Ooi, J Mater Sci: Mater Medicine 20 (1), 105-111 (2009).

[135] A. H. Rajabi, M. Jaffe and T. L. Arinzeh, Acta Biomater.24, 12-23 (2015).

[136] M. T. Rodrigues, M. E. Gomes, J. F. Mano and R. L. Reis, in Advanced Materials Forum Iv, edited by A. T. Marques, A. F. Silva, A. P. M. Baptista, C. Sa, F. Alves, L. F. Malheiros and M. Vieira (Trans Tech Publications Ltd, Stafa-Zurich, 2008), Vol. 587-588, pp. 72-76.

[137]J. Parssinen, H. Hammaren, R. Rahikainen, V. Sencadas, C. Ribeiro, S. Vanhatupa, S. Miettinen, S. Lanceros-Mendez and V. P. Hytonen, J. Biomed. Mater.Res.A 103 (3), 919-928 (2015).

[138] C. Ribeiro, J. Parssinen, V. Sencadas, V. Correia, S. Miettinen, V. P. Hytonen and S. Lanceros-Mendez, J. Biomed. Mater.Res.A 103 (6), 2172-2175 (2015).

[139] C. Ribeiro, S. Moreira, V. Correia, V. Sencadas, J. G. Rocha, F. M. Gama, J. L. G. Ribelles and S.Lanceros-Mendez, RSC Adv. 2 (30), 11504-11509 (2012).

[140] C. Ribeiro, D. M. Correia, I. Rodrigues, L. Guardao, S. Guimaraes, R. Soares and S. Lanceros-Mendez, Mater Letters 209, 118-121 (2017).

[141] A. Ignatius, H. Blessing, A. Liedert, C. Schmidt, C. Neidlinger-Wilke, D. Kaspar, B. Friemert and L.Claes, Biomaterials 26 (3), 311-318 (2005).

[142] R. F. Valentini, T. G. Vargo, J. A. Gardella and P. Aebischer, Biomaterials 13 (3), 183-190 (1992).

[143] H. F. Guo, Z. S. Li, S. W. Dong, W. J. Chen, L. Deng, Y. F. Wang and D. J. Ying, Colloids Surf B96, 29-36 (2012).

[144] P. M. Martins, S. Ribeiro, C. Ribeiro, V. Sencadas, A. C. Gomes, F. M. Gama and S. Lanceros-Méndez, RSC Adv 3 (39), 17938-17944 (2013).

[145] Y. Zhong, and R.V. Bellamkonda, Biomaterials for the central nervous system. J. R. Soc. Interface 2008, 5, 957–975.

[146] O. Jeznach, D. Kołbuk, and P. Sajkiewicz. Injectable hydrogels and nanocomposite hydrogels for cartilage regeneration. J. Biomed. Mater.Res. A 2018, 106, 2762–2776.

[147] B.N. Brown, and S.F. Badylak. Extracellular matrix as an inductive scaffold for functional tissue reconstruction.Transl. Res. 2014, 163, 268–285.

[148] R. Ravichandran, C. Astrand, H.K. Patra, A.P. Turner, V. Chotteau, and J. Phopase. Intelligent ECM mimetic injectable scaffolds based on functional collagen building blocks for tissue engineering and biomedicalapplications. RSC Adv. 2017, 7, 21068–21078.

[149] S.P. Miguel, R.S. Sequeira, A.F. Moreira, C.C. Cabral, A.G. Mendonça,  P. Ferreira,  and I.J. Correia. An overview of electrospun membranes loaded with bioactive molecules for improving the wound healing process. Eur. J. Pharm. Biopharm. 2019, 139, 1–22.

[150] M. Okamoto. The role of scaffolds in tissue engineering. In Handbook of Tissue Engineering Sca_olds; Elsevier:Amsterdam, The Netherlands, 2019; Vo1, pp. 23–49.

[151] P.I. Morgado, A. Aguiar-Ricardo, and I.J. Correia. Asymmetric membranes as ideal wound dressings: An overview on production methods, structure, properties and performance relationship. J. Membr. Sci. 2015,490, 139–151.

[152] A. Subramanian, U.M. Krishnan, and S.  Sethuraman. Development of biomaterial scaffold for nerve tissue engineering: Biomaterial mediated neural regeneration. J. Biomed. Sci. 2009, 16, 108.

[153] F. Shapiro. Overview of Deformities. In Pediatric Orthopedic Deformities; Springer: Cham, Switzerland, 2016, Vol. 1, pp. 159–254.

[154] E. Mercadelli, A. Sanson, and C. Galassi. Porous Piezoelectric Ceramics. In Piezoelectric Ceramics;Suaste-Gomez, E., Ed.; InTech: Rijeka, Croatia, 2010; pp. 111–129.

[155] W. Wersing, W. Lubitz, and J. Mohaupt. Dielectric, elastic and piezoelectric properties of porous PZT ceramics.Ferroelectrics 1986, 68, 77–97.

[156] E. Ringgaard, F. Lautzenhiser, L. Bierregaard, T. Zawada, and E. Molz. Development of porous piezoceramics for medical and sensor applications. Materials 2015, 8, 8877–8889.

[157] C. Xue, N. Hu, Y Gu,  Y. Yang,  Y Liu,  J. Liu, F. Ding,  and X. Gu. Joint use of a chitosan/PLGA scaffold and MSCs to bridge an extra large gap in dog sciatic nerve. Neurorehabil. Neural Repair 2012, 26, 96–106.

[158] N.C. Carville, L. Collins, M. Manzo, K. Gallo, B.I. Lukasz, K.K. McKayed, and B.J. Rodriguez. Biocompatibilityof ferroelectric lithium niobate and the influence of polarization charge on osteoblast proliferation andfunction. J. Biomed. Mater.Res. A 2015, 103, 2540–2548.

[159] K. Furuya, Y. Morita, K. Tanaka, T. Katayama, and E. Nakamachi. Acceleration of osteogenesis by using barium titanate piezoelectric ceramic as an implant material. In Proceedings of the International Society for Opticsand Photonics, San Diego, CA, USA, 3–7 May 2011; Vol. 7975, p. 79750U.

[160] J.P. Ball, B.A. Mound, J.C. Nino, and J.B. Allen. Biocompatible evaluation of barium titanate foamed ceramic structures for orthopedic applications. J. Biomed. Mater. Res. A 2014, 102, 2089–2095.

[161] H.B. Lopes, T.D.S. Santos, F.S. De Oliveira, G.P. Freitas, A.L. De Almeida, R. Gimenes, and M.M. Beloti. Poly (vinylidene-trifluoroethylene)/barium titanate composite for in vivo support of bone formation. J. Biomater. Appl. 2014, 29, 104–112.

[162] X. Zhang, C.  Zhang, Y. Lin, P. Hu, Y. Shen, K. Wang, and Y. Liu. Nanocomposite membranes enhance bone regeneration through restoring physiological electric microenvironment. ACS Nano 2016, 10, 7279–7286.

[163] S. Roberts. Dielectric and piezoelectric properties of barium titanate. Phys. Rev. 1947, 71, 890.

[164] F.R. Baxter, C.R. Bowen, I.G. Turner, and A.C. Dent. Electrically active bioceramics: A review of interfacialresponses. Ann. Biomed. Eng. 2010, 38, 2079–2092.

[165] G. Ciofani, L. Ricotti, C. Canale, D. D’Alessandro, S. Berrettini, B. Mazzolai, and V. Mattoli. Effects of barium titanate nanoparticles on proliferation and differentiation of rat mesenchymal stem cells. Colloids Surf.B Biointerfaces 2013, 102, 312–320.

[166] G. Ciofani, L.  Ricotti, and V. Mattoli. Preparation, characterization and in vitro testing of poly (lactic-co-glycolic)acid/barium titanate nanoparticle composites for enhanced cellular proliferation. Biomed. Microdevices 2011,13, 255–266.

[167] O. Ivanova, C. Williams, and T. Campbell. Additive manufacturing (AM) and nanotechnology: Promises and challenges. Rapid Prototyp. J. 2013, 19, 353–364.

[168] J. Jacob, N. More, K. Kalia, and G. Kapusetti. Piezoelectric smart biomaterials for bone and cartilage tissueengineering.Inflamm. Regen. 2018, 38, 2.

[169] F. Matassi, L. Nistri, D.C. Paez, and M. Innocenti. New biomaterials for bone regeneration. Clin.Cases Miner.Bone Metab. 2011, 8, 21.

[170] P. Ahmad, M.U. Khandaker, Z.R. Khan, and Y.M. Amin. Synthesis of boron nitride nanotubes via chemical vapour deposition: A comprehensive review. Mater. Sci. Eng. R. 2010, 70, 92–111.

[171] D. Lahiri, F. Rouzaud, T. Richard, A.K. Keshri, S.R. Bakshi, L. Kos, and A. Agarwal. Boron nitride nanotube reinforced polylactide–polycaprolactone copolymer composite: Mechanical properties and cytocompatibility with osteoblasts and macrophages in vitro. Acta Biomater.2010, 6, 3524–3533.

[172] D. Lahiri, V. Singh, A.P. Benaduce, S. Seal, L. Kos, and A. Agarwal. Boron nitride nanotube reinforced hydroxyapatite composite: Mechanical and tribological performance and in-vitro biocompatibility toosteoblasts. J. Mech. Behav. Biomed.2011, 4, 44–56.

[173] X. Li, C. Zhi, N. Hanagata, M. Yamaguchi, Y. Bando, and D. Golberg. Boron nitride nanotubes functionalized with mesoporous silica for intracellular delivery of chemotherapy drugs. Chem. Commun. 2013, 49, 7337–7339.

[174] G. Ciofani, S. Danti, G.G. Genchi, B. Mazzolai, and V. Mattoli. Boron nitride nanotubes: Biocompatibility and potential spill-over in nanomedicine. Small 2013, 9, 1672–1685.

[175]  X. Li, N. Hanagata, X. Wang, M. Yamaguchi, W. Yi, Y. Bando, and D. Golberg. Multimodal luminescent-magnetic boron nitride nanotubes@ NaGdF 4: Eu structures for cancer therapy. Chem. Commun.2014, 50, 4371–4374.

[176] Q. Weng, B. Wang, X. Wang, N. Hanagata, X. Li, D. Liu, and D. Golberg. Highly water-soluble, porous, and biocompatible boron nitrides for anticancer drug delivery. ACS Nano 2014, 8, 6123–6130. X

[177] J. Wang, C.H. Lee, and Y.K. Yap. Recent advancements in boron nitride nanotubes. Nanoscale 2010, 2, 2028–2034.

[178] G. Ciofani, V.  Raa, A.  Menciassi, and A. Cuschieri. Boron nitride nanotubes: An innovative tool for nanomedicine. Nano Today 2009, 4, 8–10.

[179] J.W. Rasmussen, E.  Martinez, P. Louka, and D.G. Wingett.  Zinc oxide nanoparticles for selective destruction of tumor cells and potential for drug delivery applications. Expert Opin.Drug Deliv.2010, 7, 1063–1077.

[180] S. Goel, and B. Kumar. A review on piezo-/ferro-electric properties of morphologically diverse ZnO nanostructures. J. Alloys Compd. 2019, 816, 152491.

[181] Y. Yin, Q.  Lin, H. Sun, D. Chen, Q. Wu, X. Chen, and S. Li. Cytotoxic ejects of ZnO hierarchical architectures on RSC96 Schwann cells. Res. Lett. 2012, 7, 439.

[182] M. Safaei, H.A. Sodano, and S.R. Anton. A review of energy harvesting using piezoelectric materials: State-of-the-art a decade later (2008–2018). Smart Mater. Struct.2019, 28, 113001.

[183] C. Ribeiro, D.M. Correia, S. Ribeiro, V. Sencadas, G. Botelho, and S. Lanceros-Méndez. Piezoelectric poly (vinylidene fluoride) microstructure and poling state in active tissue engineering. Eng. Life Sci. 2015, 15, 351–356.

[184] M.R. Aguilar, and J. San Román. Introduction to smart polymers and their applications. in smart polymers and their applications; Woodhead Publishing: Sawston, UK, 2019; pp. 1–11.

[185] E. Piskin. Biodegradable polymers as biomaterials. J. Biomater. Sci. Polym. Ed. 1995, 6, 775–795.

[186] P. Sajkiewicz. Crystallization behavior of poly (vinylidene fluoride). Eur. Polym. J. 1999, 35, 1581–1590.

[187] A. Gradys, P. Sajkiewicz, S. Adamovsky, A.A. Minakov, and C. Schick. Crystallization of poly (vinylidenefluoride) during ultra-fast cooling. Thermochim. Acta 2007, 461, 153–157.

[188] D.M. Esterly, and B.J. Love. Phase transformation to β-poly (vinylidene fluoride) by milling. J. Polym. Sci. BPolym. Phys. 2004, 42, 91–97.

[189] E.S. Cozza,o.  Monticelli, E. Marsano, and S. Cebe. On the Electrospinning of PVDF: Influence of the experimental conditions on the nanofiber properties. Polym. Int. 2013, 62, 41–48.

[190] L. Yu, and P. Cebe. Crystal polymorphism in electrospun composite nanofibers of poly (vinylidene fluoride) with nanoclay. Polymer 2009, 50, 2133–2141. stop

[191] B.E. El Mohajir, and N. Heymans. Changes in structural and mechanical behavior of PVDF with processing and thermomechanical treatments. 1. Change in structure. Polymer 2001, 42, 5661–5667.

[192] R. Imamura, A.B. Silva, and R. Gregorio, Jr. γ→β Phase transformation induced in poly (vinylidene fluoride)by stretching. J. Appl. Polym. Sci. 2008, 110, 3242–3246.

[193] J. Wang, H. Li, J. Liu, Y. Duan, S. Jiang, and Y. Yan. On the α→β Transition of carbon coated highly oriented PVDF ultrathin film induced by melt recrystallization. J. Am. Chem. Soc. 2003, 125, 1496–1497.

[194] T. Kaura, R. Nath, and M.M. Perlman. Simultaneous stretching and corona poling of PVDF films. J. Phys. D: Appl. Phys. 1991, 24, 1848.

[195] A.K. Ramanathan, L.M. Headings, and M.J. Dapino. Design optimization of flexible piezoelectric PVD funimorphs for surface pressure transducer applications. In smart structures and NDE for energy systems and industry 4.0; International Society for Optics and Photonics: Bellingham, WA, USA, 2019; Vol. 10973, p. 1097307.

[196] C. Ellingford, H. Smith, X. Yan, C.  Bowen, L. Figiel, T. McNally, and C. Wan. Electrical dual-percolation in MWCNTs/SBS/PVDF based thermoplastic elastomer (TPE) composites and the effect of mechanical stretching. Eur. Polym. J. 2019, 112, 504–514.

[197] S. Zhang, Z. Jia, T. Liu, G. Wei, and Z. Su. Electrospinning nanoparticles-based materials interface for sensor applications. Sensors 2019, 19, 3977.

[198] Y. Li, C. Liao, and S.C. Tjong. Electrospun polyvinylidene fluoride-based fibrous scaffolds with piezoelectric characteristics for bone and neural eissue Engineering. Nanomaterials 2019, 9, 952.

[199] L. Yu, P. Zhou, D. Wu, L. Wang, L. Lin, and D. Sun. Shoepad nanogenerator based on electrospun PVDF nanofibers. Microsyst. Technol. 2019, 25, 3151–3156.

[200] C. Ribeiro, C.M. Costa, D.M. Correia, J. Nunes-Pereira, J. Oliveira, P. Martins, and S. Lanceros-Méndez. Electroactive poly (vinylidene fluoride)-based structures for advanced applications. Nat. Protoc. 2018, 13, 681.

[201] M. Fortunato, D. Cavallini, G. De Bellis, F. Marra, A. Tamburrano, F. Sarto, and M.S. Sarto. Phase inversion in PVDF films with enhanced piezoresponse through spin-coating and quenching. Polymers 2019, 11, 1096.

[202] Z.H. Liu, C.T. Pan, L.W. Lin, J.C. Huang, and Z.Y. Ou. Direct-write PVDF nonwoven fiber fabric energy harvesters via the hollow cylindrical near-field electrospinning process. Smart Mater.Struct. 2013, 23, 025003.

[203] B. Zaarour, L. Zhu, and X. Jin. Controlling the surface structure, mechanical properties, crystallinity, and piezoelectric properties of electrospun PVDF nanofibers by maneuvering molecular weight. Soft Mater.2019, 17, 181–189.

[204] R.K. Singh, S.W. Lye, and J. Miao. PVDF nanofiber sensor for vibration measurement in a string. Sensors 2019, 19, 3739.

[205] M. Khalifa, S. Janakiraman, S. Ghosh, A. Venimadhav, and S. Anandhan. PVDF/halloysite nanocomposite-basednon-wovens as gel polymer electrolyte for high safety lithium ion battery. Polym.Compos.2019, 40, 2320–2334.

[206] S. Liang, Y. Kang, A. Tiraferri, E.P. Giannelis, X. Huang, and M. Elimelech. Highly hydrophilic polyvinylidenefluoride (PVDF) ultrafiltration membranes via post-fabrication grafting of surface-tailored silica nanoparticles.ACS Appl. Mater. Interfaces 2013, 5, 6694–6703.

[207] D. Mandal, K. Henkel, and D. Schmeißer. The electroactive β-phase formation in poly (vinylidene fluoride) by gold nanoparticles doping. Materials Lett.2012, 73, 123–125.

[208] J.H. Li, X.S. Shao, Q. Zhou, M.Z. Li, and Q.Q. Zhang. The double ejects of silver nanoparticles on the PVDF membrane: Surface hydrophilicity and antifouling performance. App. Surf. Sci. 2013, 265, 663–670.

[209] S. Liang, K. Xiao, Y. Mo, and X. Huang. A novel ZnO nanoparticle blended polyvinylidene fluoride membrane for anti-irreversible fouling. J. Membr. Sci. 2012, 394, 184–192.

[210] Y.H. Teow, A.L. Ahmad, J.K. Lim, and B.S. Ooi. Preparation and characterization of PVDF/TiO2 mixed matrix membrane via in situ colloidal precipitation method. Desalination 2012, 295, 61–69.

[211] J. Zhang, Z. Xu, W. Mai, C. Min, B. Zhou, M. Shan, and  X. Qian. Improved hydrophilicity, permeability, antifouling and mechanical performance of PVDF composite ultrafiltration membranes tailored by oxidizedlow-dimensional carbon nanomaterials. J. Mater. Chem. A 2013, 1, 3101–3111.

[212] H. Song, J. Shao, Y. He, B. Liu, and X. Zhong. Natural organic matter removal and flux decline with PEG–TiO2-doped PVDF membranes by integration of ultrafiltration with photocatalysis. J. Membr. Sci. 2012,405, 48–56.

[213] N. Li, C. Xiao, S. An, and X. Hu. Preparation and properties of PVDF/PVA hollow fiber membranes. Desalination 2010, 250, 530–537.

[214] A.L. Gayen, D. Mondal, D. Roy, P. Bandyopadhyay, S. Manna, R. Basu, and P. Nandy. Improvisation of electrical properties of PVDF-HFP: Use of novel metallic nanoparticles. J. Mater. Sci.: Mater. 2017, 28, 14798–14808.

[215] B. Jaleh, S. Sodagar, A. Momeni, and A. Jabbari. Nanodiamond particles/PVDF nanocomposite flexible films: Thermal, mechanical and physical properties. Mater.Res. Express 2016, 3, 085028.

[216] A. Fraczek-Szczypta. Carbon nanomaterials for nerve tissue stimulation and regeneration. Mater. Sci. Eng. C2014, 34, 35–49.

[217] C. Tsonos, C. Pandis, N. Soin, D. Sakellari, E. Myrovali, S. Kripotou, and E Siores. Multifunctional nanocomposites of poly (vinylidene fluoride) reinforced by carbon nanotubes and magnetite nanoparticles. Express Polym. Lett.2015, 9.

[218] B. Lorber, W.K. Hsiao, I.M. Hutchings, and K.R. Martin. Adult rat retinal ganglion cells and glia can be printed by piezoelectric inkjet printing. Biofabrication 2013, 6, 015001.

[219] T. Inaoka, H. Shintaku, T. Nakagawa, S. Kawano, H. Ogita, T. Sakamoto, and J. Ito. Piezoelectric materials mimic the function of the cochlear sensory epithelium. Proc. Natl. Acad. Sci. USA 2011, 108, 18390–18395.

[220] Y. Gao, and Z.L. Wang. Electrostatic potential in a bent piezoelectric nanowire. The fundamental theory of nanogenerator and nanopiezotronics. Nano Lett. 2007, 7, 2499–2505.

[221] J.F. Walsh, M.E. Manwaring, and P.A. Tresco. Directional neurite outgrowth is enhanced by engineered meningeal cell-coated substrates. Tissue Eng. 2005, 11, 1085–1094.

[222] T. Asano, T. Kubo, and Y. Nishikitani. Electrochemical properties of dye-sensitized solar cells fabricated with PVDF-type polymeric solid electrolytes. J. Photochem. Photobiol.2004, 164, 111–115.

[223] A. Marino, S. Arai, Y. Hou, E. Sinibaldi, M. Pellegrino, B. Chang, V. Mazzolai, M. Mattoli Suzuki, and G. Ciofani. Piezoelectric nanoparticle-assisted wireless neuronal stimulation. ACS Nano 2015, 9, 7678–7689.

[224] G.G. Genchi, L. Ceseracciu, A. Marino, M. Labardi, S. Marras, F. Pignatelli, L. Bruschini, V. Mattoli, and G. Ciofani. P(VDF-TrFE)/BaTiO3 nanoparticle composite films mediate piezoelectric stimulation and promote differentiation of SH-SY5Y neuroblastoma cells. Adv. Healthc. Mater.2016, 5, 1808–1820.

[225] N. Weber, Y.S. Lee, S. Shanmugasundaram, M. Jae, and T.L. Arinzeh. Characterization and in vitrocytocompatibility of piezoelectric electrospun scaffolds.Acta Biomater.2010, 6, 3550–3556.

[226] G.C. De Ruiter, M.J. Malessy, M.J. Yaszemski, A.J. Windebank, and R.J. Spinner. Designing ideal conduits for peripheral nerve repair. Neurosurg. Focus. 2009, 26, E5.

[227] S. Ichihara, Y.  Inada, and T. Nakamura. Artificial nerve tubes and their application for repair of peripheral nerve injury: An update of current concepts. Injury 2008, 39, 29–39.

[228] Y. Ji, R. Jin, X. Zhang, R. Bouchilaoun, J. Fan, R. Zhao, and H. Yang. Electric polarizations in PVDF-TrFE nanorods under lateral nanoshaping. Int. J. Appl. 2019, 126, 174108.

[229] C. Wan, and C.R. Bowen. Multiscale-structuring of polyvinylidene fluoride for energy harvesting: The impact of molecular-, micro- and macro-structure. J. Mater. Chem. A 2017, 5, 3091–3128.

[230] F.C. Sun, A.M. Dongare, A.D. Asandei, S.P. Alpay, and S. Nakhmanson. Temperature dependent structural, elastic, and polar properties of ferroelectric polyvinylidene fluoride (PVDF) and trifluoroethylene (TrFE)copolymers. J. Mater. Chem. C 2015, 3, 8389–8396.

[231] J.S. Belkas, M.S. Shoichet, and R. Midha. Peripheral nerve regeneration through guidance tubes. Neurol. Res.2004, 26, 151–160.

[232] R. Boni, A. Ali, A. Shavandi, and A.N. Clarkson. Current and novel polymeric biomaterials for neural tissue engineering. J Biomed.Sci. 2018, 25, 90.

[233] E.G. Fine, R.F. Valentini, R. Bellamkonda, and P. Aebischer. Influence of surface texture of polymeric sheetsthrought piezoelectric vinylidenefluoride-trifluoroethylene copolymer guidance channels. Biomaterials 1991, 12, 259–263.

[234] P.M. Martins, S. Ribeiro, C. Ribeiro, V. Sencadas, A.C. Gomes, F.M. Gama, and S. Lanceros-Méndez. Effect of poling state and morphology of piezoelectric poly (vinylidene fluoride) membranes for skeletal muscle tissue engineering. RSC Adv. 2013, 3, 17938–17944.

[235] S. Ke, H. Huang, L. Ren, and Y. Wan. Nearly constant dielectric loss behavior in poly (3-hydroxybutyrate-co-3-hydroxyvalerate) biodegradable polyester. J. Appl. Phys. 2009.

[236] K. Numata, H. Abe, and Y. Doi. Enzymatic processes for biodegradation of poly (hydroxyalkanoate) s crystals.Can. J. Chem. 2008, 86, 471–483.

[237] S.M. Willerth, and S.E. Sakiyama-Elbert. Approaches to neural tissue engineering using scaffolds for drug delivery.Adv. Drug Deliv. Rev. 2007, 59, 325–338.

[238] Q. Wu, Y. Wang, and G.O. Chen. Medical application of microbial biopolyesters polyhydroxyalkanoates.Artif.Cells Blood Substit.Immobil.Biotechnol.2009, 37, 1–12.

[239] S.K. Misra, S.P. Valappil, I. Roy, and A.R. Boccaccini. Polyhydroxyalkanoate (PHA)/inorganic phase composites for tissue engineering applications. Biomacromolecules 2006, 7, 2249–2258.

[240] M.P. Prabhakaran, E. Vatankhah, and S. Ramakrishna. Electrospun aligned PHBV/collagen nanofibers assubstrates for nerve tissue engineering. Biotechnol Bioeng. 2013, 110, 2775–2784.

[241] M.S. Rahman, and T. Tsuchiya. Enhancement of chondrogenic differentiation of human articular chondrocytesby biodegradable polymers. Tissue Eng. 2001, 7, 781–790.

[242] W. Chen, and Y.W. Tong. PHBV microspheres as neural tissue engineering scaffold support neuronal cell growth and axon–dendrite polarization. Acta Biomater.2012, 8, 540–548.

[243] A.L. Rivera-Briso, and A. Serrano. Poly (3-Hydroxybutyrate-co-3-Hydroxyvalerate): Enhancement strategies for advanced applications. Polymers 2018, 10, 732.

[244] V. Sencadas, C. Ribeiro, A. Heredia, I.K. Bdikin, A. L. Kholkin, and S. Lanceros-Méndez. Local piezoelectric activity of single poly (L-lactic acid)(PLLA) microfibers. Appl. Phys. A 2012, 109, 51–55.

[245] L. Jin, Z.Q. Feng, M.L. Zhu, T. Wang, M.K. Leach, and Q. Jiang. A novel fluffy conductive polypyrrolenano-layer coated PLLA fibrous sca_old for nerve tissue engineering. J. Biomed. Nanotechnol.2012, 8, 779–785.

[246] K. Zhang, H. Zheng, S. Liang, and C. Gao. Aligned PLLA nanofibrous scaffolds coated with graphene oxide for promoting neural cell growth. Acta Biomater.2016, 37, 131–142.

[247] J.M. Zuidema, C. Provenza, T. Caliendo, S. Dutz, and R.J. Gilbert. Magnetic NGF-releasing PLLA/ironoxide nanoparticles direct extending neurites and preferentially guide neurites along aligned electrospunmicrofibers. ACS Chem. Neurosci. 2015, 6, 1781–1788.

[248] J. Venugopal, Y.Z.  Zhang, and S. Ramakrishna. Electrospun nanofibres: Biomedical applications. Proceedings of the institution of mechanical engineers.N J. Nanoeng.Nanosyst. 2004, 218, 35–45.

[249] B. Philipp, W. Bock, and F. Schierbaum. Application of polysaccharides and their derivatives as supportingmaterials and auxiliary substances in medicine and nutrition. J. Polym. Sci. Polym. Symp.1979, 66, 83–100.

[250] G. Franz. Polysaccharides in pharmacy. Adv. Polym. Sci. 1986, 76, 1–30.

[251] T. Miyamoto, S.I. Takahashi, H. Ito, H. Inagaki, and Y. Noishiki. Tissue biocompatibility of cellulose and its derivatives. J. Biomed. Mater. Res. 1989, 23, 125–133.

[252] Y. Ikada. Biomedical applications of cellulose membranes. in cellulose: structural and functional aspects; Kennedy, J.F., Phillips, G.O.,Williams, P.A., Eds.; Ellis Horwood: Chichester, UK, 1989; pp. 447–455.

[253] C. Barbié, D. Chauveaux, X. Barthe, C. Baquey, and J. Poustis. Biological behavior of cellulosic materials after bone implantation: Preliminary results. Clin.Mater.1990, 5, 251–258.

[254] U. Gross, C. Muller-Mai, and C. Voigt. The tissue response on cellulose cylinders after implantation in the distal femur of rabbits. In Proceedings of the Fourth World Biomaterials Congress, Berlin, Germany,19–24 May 1992; p. 192.

[255] M. Märtson, J. Viljanto, T. Hurme, and P. Saukko. Biocompatibility of cellulose sponge with bone. Eur. Surg. Res.1998, 30, 426–432.

[256] A. Bhatnagar, and M. Sain. Processing of cellulose nanofiber-reinforced composites. J. Reinf. Plast. Comp. 2005, 24, 1259–1268.

[257] J.C. Fricain, P.L. Granja, M.A. Barbosa, B. De Jéso, N. Barthe, and C. Baquey. Cellulose phosphates as biomaterials. In vivo biocompatibility studies. Biomaterials 2002, 23, 971–980.

[258] A. Svensson, E. Nicklasson, T. Harrah, B. Panilaitis, D.L. Kaplan, M. Brittberg, and P. Gatenholm. Bacterial cellulose as a potential sca_old for tissue engineering of cartilage. Biomaterials 2005, 26, 419–431.

[259] M. Märtson, J. Viljanto, P. Laippala, and P. Saukko. Connective tissue formation in subcutaneous cellulose sponge implants in the rat. Eur. Surg. Res. 1998, 30, 419–425.

[260] G. Fundueanu, M. Constantin, E. Esposito, R. Cortesi, C. Nastruzzi, and E. Menegatti. Cellulose acetate butyrate microcapsules containing dextran ion-exchange resins as self-propelled drug release system. Biomaterials2005, 26, 4337–4347.

[261] E. Entcheva, H. Bien, L. Yin, C.Y. Chung, M. Farrell, and Y. Kosto. Functional cardiac cell constructs on cellulose-based scaffolding. Biomaterials 2004, 25, 5753–5762.

[262] M.C. Tate, D.A. Shear, S.W. Hoffman, D.G. Stein, and M.C. LaPlaca. Biocompatibility of methylcellulose-based constructs designed for intracerebral gelation following experimental traumatic brain injury. Biomaterials2001, 22, 1113–1123.

[263] S.M. Hoseini, K. Khosravi-Darani, and M.R. Mozafari. Nutritional and medical applications of spirulina microalgae. Mini Rev. Med. Chem. 2013, 13, 1231–1237.

[264] P.L. Granja, M.A. Barbosa, L. Pouységu, B. De Jéso, F. Rouais, and C. Baquey. Cellulose phosphates as biomaterials. Mineralization of chemically modified regenerated cellulose hydrogels. J. Mater. Sci. 2001,36, 2163–2172.

[265] M. Naseri-Nosar, M. Salehi, and S. Hojjati-Emami. Cellulose acetate/poly lactic acid coaxial wet-electrospun scaffold containing citalopram-loaded gelatin nanocarriers for neural tissue engineering applications. Int. J.Biol. Macromol. 2017, 103, 701–708.

[266] S. Wang, C. Sun, S. Guan, W. Li, J. Xu, D. Ge, and X. Ma. Chitosan/gelatin porous scaffolds assembled with conductive poly (3, 4-ethylenedioxythiophene) nanoparticles for neural tissue engineering. J. Mat. Chem. B2017, 5, 4774–4788.

[267] S.S. Koide. Chitin-chitosan: Properties, benefits and risks. Nutr. Res. 1998, 18, 1091–1101.

[268] M. Rinaudo. Chitin and chitosan: Properties and applications. Prog. Polym. Sci. 2006, 31, 603–632.

[269] S.V. Madihally, and H.W. Matthew. Porous chitosan scaffolds for tissue engineering. Biomaterials 1999, 20, 1133–1142.

[270] K. Ohkawa, D. Cha, H. Kim, A. Nishida, and H. Yamamoto. Electrospinning of chitosan. Macromol.Rapid Commun.2004, 25, 1600–1605.

[271] D. Izzo, B. Palazzo, F. Scalera, F. Gullotta, V. Lapesa, S. Scialla, and F. Gervaso. Chitosan scaffolds for cartilage regeneration: Influence of di_erent ionic crosslinkers on biomaterial properties. Int. J. Polym. Mater.2019, 68, 936–945.

[272] A. Maged, A.A. Abdelkhalek, A.A. Mahmoud, S. Salah, M.M. Ammar, and M.M. Ghorab. Mesenchymalstem cells associated with chitosan sca_olds loaded with rosuvastatin to improve wound healing. Eur. J.Pharm. Sci. 2019, 127, 185–198.

[273] Y. Xue, M. Wu, Z. Liu, J. Song, S. Luo, H. Li, and F. Chen. In vitro and in vivo evaluation of chitosan scaffolds combined with simvastatin-loaded nanoparticles for guided bone regeneration. J. Mater. Sci. Mater. Med. 2019, 30, 47.

[274] N.B. Skop, F. Calderon, S.W. Levison, C.D. Gandhi, and C.H. Cho. Heparin crosslinked chitosan microspheres for the delivery of neural stem cells and growth factors for central nervous system repair. Acta Biomater.2013, 9, 6834–6843.

[275] Y.S.R. Elnaggar, S.M. Etman, and D.A. Abdelmonsif. Intranasal piperine-loaded chitosan nanoparticles as brain-targeted therapy in alzheimer’s disease: optimization, biological efficacy, and potential toxicity. J. Pharm. Sci. 2015, 104, 3544–3556.

[276] R. Raj, S. Wairkar, V. Sridhar, and R. Gaud. Pramipexole dihydrochloride loaded chitosan nanoparticles for noseto brain delivery: Development, characterization and in vivo anti-Parkinson activity. Int. J. Biol. Macromol.2018, 109, 27–35.

[277] S.H. Liu, and P.C. Ho. Intranasal administration of brain-targeted HP-β-CD/chitosan nanoparticles for delivery ofscutellarin, a compound with protective effect in cerebral ischaemia. J. Pharm. Pharmacol. 2017, 69, 1495–1501.

[278] A. Cooper, N. Bhattarai, and M. Zhang. Fabrication and cellular compatibility of aligned chitosan–PCL fibersfor nerve tissue regeneration.Carbohydr.Polym.2011, 85, 149–156.

[279] Y.C. Kuo, C.F. Yeh, and J.T. Yang. Differentiation of bone marrow stromal cells in poly (lactide-co-glycolide)/chitosan scaffolds. Biomaterials 2009, 30, 6604–6613.

[280] V. Marchesano, O. Gennari, L. Mecozzi, S. Grilli, and P. Ferraro. Effects of lithium niobate polarization on cell adhesion and morphology. ACS Appl. Mater. Interfaces.2015, 7, 18113–18119.

[281] A. Tiffany, and B.A. Harley. Sequestration of biomolecules for controlled delivery in mineralized collagen scaffolds. In 42nd society for biomaterials annual meeting and exposition 2019: The pinnacle of biomaterials innovation and excellence. Soc. Biomater. 2019, 40, 1526–7547.

[282] I. Sallent, H. Capella-Monsonís, and D.I. Zeugolis. Production and characterization of chemically cross-linked collagen scaffolds. in collagen; Humana Press: New York, NY, USA, 2019; pp. 23–38.

[283] L. Mohee, G.S. Offeddu, A. Husmann, M. L. Oyen, and R.E. Cameron. Investigation of the intrinsic permeability of ice-templated collagen scaffolds as a function of their structural and mechanical properties. Acta Biomater.2019, 83, 189–198.

[284] Y. Liu, T. Nelson, J. Chakro, B. Cromeens, J. Johnson, J. Lannutti, and G.E. Besner. Comparison of polyglycolic acid, polycaprolactone, and collagen as scaffolds for the production of tissue engineered intestine. J. Biomed.Mater. Res. B 2019, 107, 750–760.

[285] X. Lei, J. Gao, F. Xing, Y. Zhang, Y. Ma, and G. Zhang. Comparative evaluation of the physicochemical properties of nano-hydroxyapatite/collagen and natural bone ceramic/collagen scaffolds and their osteogenesis-promoting effect on MC3T3-E1 cells. Regen. Biomater.2019, 6, 361–371.

[286] S. Radhakrishnan, S. Nagarajan, M. Bechelany, and S.N. Kalkura. Collagen based biomaterials for tissue engineering applications: a review. in processes and phenomena on the boundary between biogenic and abiogenic; Nature; Springer: Cham, Switzerland, 2020; pp. 3-22.

[287] A. Eltom, G. Zhong, and A. Muhammad. Scaffold Techniques and Designs in Tissue Engineering Functions and Purposes: A Review. Adv. Mater. Sci. Eng. 2019.

[288] M. Mohseni, N.J. Castro, H.P. Dang, T.D. Nguyen, H.M. Ho, M.P.N. Tran, and P.A. Tran. Adipose tissue regeneration: scaffold-biomaterial strategies and translational perspectives. in biomaterials in translational medicine; Academic Press: Cambridge, MA, USA, 2019; pp. 291–330.

[289] D. Ceballos, X. Navarro, N. Dubey, G. Wendelschafer-Crabb, W.R. Kennedy, and R.T. Tranquillo. Magnetically Aligned Collagen Gel Filling a Collagen Nerve Guide Improves Peripheral Nerve Regeneration. Exp. Neurol.1999, 158, 290–300.

[290] N. Dubey, P.C. Letourneau, and R.T. Tranquillo. Guided neurite elongation and schwann cell invasion into magnetically aligned collagen in simulated peripheral nerve regeneration. Exp. Neurol. 1999, 158, 338–350.

[291] Y. Eguchi, M. Ogiue-Ikeda, and S. Ueno. Control of orientation of rat schwann cells using an 8-T static magnetic field. Neurosci.Lett.2003, 351, 130–132.